## Slide 1: 3DXP Deck Select Architecture
DerChang, Prashant, Max, 1/25/2019
Deck Select Transistors integrated with Cross Point Array Technology
3 Deck Select TFT ideas – Ω, Fin, Saddle
Fin TFT embodiment
Saddle TFT embodiment

## Slide 2: ½ Kb Array: 8 decks of 8x8 cross point

## Slide 3: 3 ideas
Saddle-TFT
FIN-TFT
Ω-TFT

## Slide 4: FinTFT Process Flow
Array First Cut
First Cut Gap Fill
Deck Select TFT Placeholder:
200~400nm stripe opening,
Selective stack material removal
Optional Spacer to define TFT FinFET width
TFT Fin Channel Material Dep
TFT Fin Height definition

## Slide 5: Fin TFT Process Flow (cont.)
TFT FinFET Oxide Dep
TFT FinFET Gate Dep
FinFET S/D Placeholder
TFT FinFET S/D Dep

## Slide 6: Saddle TFT Process Flow
Array First Cut
First Cut Gap Fill
Deck Select TFT Placeholder:
200~400nm stripe opening,
Selective etch, remaining W
Channel Length Definition
Oxidize W
Saddling up TFT Fin Channel Material

## Slide 7: Saddle TFT Process Flow (cont.)
Saddle Isolation
Saddle TFT Oxide conforming Dep
Saddle TFT Gate Dep
Saddle TFT