Confidential


ISO INVENTION DISCLOSURE FORM
CONFIDENTIAL and ATTORNEY-CLIENT PRIVILEGED COMMUNICATION

Rev. 1 – October 2003

DATE: Feb/11/2007
It is important to provide accurate and detailed information on this form.  The information will be used to evaluate your invention for possible filing as a patent application.  Send Invention Disclosure forms electronically to the ISO eRoom.
	Last Name:  Kau
	First Name: DerChang
	M.I.

	Business Phone Number: +1-408-765-0266
	Business Fax Number: +1-408-765-5775
	Mailstop: RN3-01

	E-mail address: DerChang.Kau@intel.com
	WWID: 10077599

	Citizenship: USA
	
	
	

	Home Address: 10847 Linda Vista Drive

	City: Cupertino
	State: CA
	Zip: 95014
	Country: USA

	Business Address: 2200 Mission College blvd
	
	

	City: Santa Clara
	State: CA
	Zip: 95054
	Country:


	Last Name:  Atwood
	First Name: Greg 
	M.I.

	Business Phone Number: 408-765-9733
	Business Fax Number: +1-408-765-5775
	Mailstop: RN3-01

	E-mail address: greg.atwood@intel.com
	WWID: 10020991

	Citizenship: USA
	
	
	

	Home Address: 18705 Overlook Road 

	City: Los Gatos
	State: CA
	Zip:
	Country:  USA

	Business Address: 2200 Mission College blvd
	
	

	City: Santa Clara
	State: CA
	Zip: 95054
	Country: USA


	2.  Title of Invention:

Damascene Compatible and Pitch Multiplication Enabled Self-Aligned Top Electrode


	3.  What technology/product/process (code name) does your invention relate to (be specific if you can):

A path finding test vehicle for OUMS Memory Array validation and exploration using P894 Process Technology and beyond 


	4.
Include several key words to describe the technology area of the invention in addition to # 3 above:

OUM, OUMS, Phase Change Memory, PCM, Triggered PCM, P-RAM


	5.
Stage of development (i.e. % complete, simulations done, test chips if any, etc.):
Path Finding: Concept exploration.  


	6a.  Has a description of your invention been (or planned to be) published outside of the ISO Collaboration:

If YES, please identify the publication and the date published:
No


	6b.  Has your invention been used/sold or planned to be used/sold by Intel, ST Micro, Ovonyx, or others?

No
If YES, date it was sold or will be sold:


	6d.  If the invention is embodied in a semiconductor device, what is the actual or anticipated date of tapeout?

Q3, 2007 or Q1, 2008


	6e.  If the invention is software, actual or anticipated date of any beta tests or other public distribution outside the ISO Collaboration: N/A


	7.  Is this invention related to any other invention disclosure that you have recently submitted?  If so, please give the title and

     inventors: No



PLEASE READ AND FOLLOW THE DIRECTIONS ON

HOW TO WRITE A DESCRIPTION OF YOUR INVENTION

Please provide a description of the invention and include the following information:

1. Explain the problem being addressed by the invention.
Currently in phase change memory technology, the top electrode and bitline patterning deploy two advanced patterning tools to delivery the required critical dimension as well as registration overylap between bitline metallization, top electrode and underline memory element.  This invention deploy a self aligned patterning scheme compatible with pitch double technique, single damascene and Cu electroplating metallization method. This would reduce patterning complexity and cost from Top Electrode to bitline process module of a memory manufacturing technology.  
2. Identify the closest or most pertinent prior art that you are aware of.

1. What is done today to alleviate the problem solved by the invention?
1. Two critical-dimension patterning scheme with 1) top electrode and 2) column/bitline
2. Larger cell size to tolerate registration overlap requirement between memory element, Top electrode and Bitline.  

 It all results in higher processing cost thereforte chip cost.
.
3. Describe in detail what the components of the invention are and how the invention works.

1. Provide a summary paragraph of what your invention is, and what it does.
2. Next, briefly describe each of the key elements, and how they relate to each other in the overall invention (optional: reference drawings)
The process steps for self aligned top electrode/bitline and Damascene compatible, Cu electroplating enabled scheme are as the follows.

1. (Optional) patterning memory material in one direction and fully planarized. Fig 1.

[image: image1]
Fig 1.  Memory elements patterned in one-direction

2. Deposit Top electrode material and sacrificial material and sacrificial material patterning.   Fig 2. illustrates the top electrode material consists of a OTS layer and Top metallic layer.  Sacrificial patterning can deploy either direct patterning or pitch doubled patterning technique.  Sacrificial material can be deployed with high etch selectivity to the underline and sounding material for step 5 below. 

[image: image2]
Fig 2.  A poly sacrificial layer is deposited on the top of electrode.

3. The underline memory elements are segmented by the bitline pattern therefore self-aligned. Step 2 and Step 3 can be combined with mask direct patterning techniques.

[image: image3]
Fig 3.   Self-aligned top electrodes to memory elements.  
Picture illustrated consists of Med-Electrod, OTS and Top-Electrode for OUMS memory array.
4. Deploys gap fill with dielectric and planarized by using CMP stopping on the top sacrificial layer.

[image: image4]
Fig. 4.  Gap Fill and Polish

5. Removing sacrificial layer and electroplates Cu and CMP stopping at dielectric.

.


[image: image5]
4. Describe advantage(s) of your invention over what is currently being done.
· Enable the smallest possible cell without using complicated self alignment schem 

· Enable pitch doubling where [N-2] Generation tool is suggested in this proposal
5. Include at least one figure illustrating the invention.  If the invention relates to 


software, include a flowchart or pseudo-code representation of the algorithm.
[image: image6.emf]This Damascenne compatible, Self-Aligned TE/Bitline scheme is applicable to PCM, Fig 9, or PCMS, Fig 10.
[image: image7.emf]

Fig 9.  Nano-Cross-Point in PCM technology
   Fig. 10 Nano-Cross-Point in PCMS Technology
6. How would infringement be detected?
· Identify how use of the invention would be visible, measurable, provable
· Examples of Detection Methods: Visual Examination, Reading Product literature, Reading Programming Reference Manuals, Reading Data Sheets, Reverse Engineering
Self-Aligned Top Electrode can be detected by woldline direction slicing through storage element

Replacement Bitline can be detected by cross section in both bitline and wordline directions 

DATE:    Feb/17/2007
INVENTOR:   DerChang Kau


DATE:    Feb/17/2007
INVENTOR:   Greg Atwood


OPTIONAL WITNESS SIGNATURE

DATE:    


WITNESS:   



BY THIS SIGNING, I (WITNESS) ACKNOWLEDGE THAT I HAVE READ AND UNDERSTAND THIS 

DISCLOSURE.



























[image: image8.emf][image: image9.emf][image: image10.emf][image: image11.emf]OUM

Heater

Top

Electrode

[image: image12.emf]Row

Column

OUM

Heater

or

Mid

Electrode

Top

Electrode

OTS

