Confidential


ISO INVENTION DISCLOSURE FORM
CONFIDENTIAL and ATTORNEY-CLIENT PRIVILEGED COMMUNICATION

Rev. 1 – October 2003

DATE: July/6/2007
It is important to provide accurate and detailed information on this form.  The information will be used to evaluate your invention for possible filing as a patent application.  Send Invention Disclosure forms electronically to t changeIS
	Last Name:  Atwood
	First Name: Greg 
	M.I.

	Business Phone Number: 408-765-9733
	Business Fax Number: +1-408-765-5775
	Mailstop: RN3-01

	E-mail address: greg.atwood@intel.com
	WWID: 10020991

	Citizenship: USA
	
	
	

	Home Address: 18705 Overlook Road 

	City: Los Gatos
	State: CA
	Zip:
	Country:  USA

	Business Address: 2200 Mission College blvd
	
	

	City: Santa Clara
	State: CA
	Zip: 95054
	Country: USA


	Last Name:  Kau
	First Name: DerChang
	M.I.

	Business Phone Number: +1-408-765-0266
	Business Fax Number: +1-408-765-5775
	Mailstop: RN3-01

	E-mail address: DerChang.Kau@intel.com
	WWID: 10077599

	Citizenship: USA
	
	
	

	Home Address: 10847 Linda Vista Drive

	City: Cupertino
	State: CA
	Zip: 95014
	Country: USA

	Business Address: 2200 Mission College blvd
	
	

	City: Santa Clara
	State: CA
	Zip: 95054
	Country:


	Last Name:  Kim
	First Name: Yudong
	M.I. 

	Business Phone Number: +1-408-765-6997
	Business Fax Number: + 1-408-765-5775
	Mailstop: RN3-01

	E-mail address: Yudong.kim@intel.com
	WWID: 10056409

	Citizenship: USA
	
	
	

	Home Address: 18812 Loree Ave

	City: Cupertino
	State:CA
	Zip: 95014
	Country: US

	Business Address: 2200 Mission College blvd
	
	

	City: Santa Clara
	State: CA
	Zip: 95054
	Country: US


	2.  Title of Invention:

Nano Pillar Phase Change Memory


	3.  What technology/product/process (code name) does your invention relate to (be specific if you can):

A path finding test vehicle for OUMS Memory Array validation and exploration using P894/P897 Process Technology and beyond 


	4.
Include several key words to describe the technology area of the invention in addition to # 3 above:

OUM, OUMS, Phase Change Memory, PCM, Triggered PCM, P-RAM


	5.
Stage of development (i.e. % complete, simulations done, test chips if any, etc.):
Path Finding: Concept exploration.  


	6a.  Has a description of your invention been (or planned to be) published outside of the ISO Collaboration:

If YES, please identify the publication and the date published:
No


	6b.  Has your invention been used/sold or planned to be used/sold by Intel, ST Micro, Ovonyx, or others?

No
If YES, date it was sold or will be sold:


	6d.  If the invention is embodied in a semiconductor device, what is the actual or anticipated date of tapeout?

Not Planned Yet.


	6e.  If the invention is software, actual or anticipated date of any beta tests or other public distribution outside the ISO Collaboration: N/A


	7.  Is this invention related to any other invention disclosure that you have recently submitted?  If so, please give the title and

     inventors: No



PLEASE READ AND FOLLOW THE DIRECTIONS ON

HOW TO WRITE A DESCRIPTION OF YOUR INVENTION

Please provide a description of the invention and include the following information:

1. Explain the problem being addressed by the invention.
· Write current reduction using narrowed cross section structure ( nano-pillar
· Robust process flow for manufacturablility and low variability to produce nano-pillar geometry (width and height)

· Pitch multiplication capable self-aligned technology for low cost manufacturing.
· Scalability beyond u-trench patterning limitation   

2. Identify the closest or most pertinent prior art that you are aware of.

· What is done today to alleviate the problem solved by the invention?
· Structural confinement such as Damascene Lance Architecture or other confined structure demonstrated by Taiwan Phase Change Memory Consortium published in VLSI-TSA/2007.
· Reduced Heater/Memory interface such as µ-Trench Architecture and Ringed heater Architecture.
3. Describe in detail what the components of the invention are and how the invention works.

· Provide a summary paragraph of what your invention is, and what it does.
· Next, briefly describe each of the key elements, and how they relate to each other in the overall invention (optional: reference drawings)
The technology is applicable to both single crystalline diode/BJT selector based PCM technology and thin film selector such as OTS based technology.  Key features of the disclosed invention are

· Bottom electrode of the disclosed nano-pillar can be a side wall heater, a side wall pcm or line/space patterned wordline/row which includes bottom electrode, an optional heater and a PCM.
· Nano-pillar formation is defined the hard mask formed by spacer using pitch doubled patterning technique.   
· Nano-pillar dimensions, width, height and depth, are precisely control through 3 independent process capability. 

· Nano-pillar width: Spacer width defines width of nano pillar
· Nano-pillar height: either timed etch or etch stop mechanism or both defined the height of nano-pillar.  Dual or triple layered dielectric stacks in the first dielectric stack defines nano-pillar height as etch stop during nano pillar patterning or etching. 
· Nano-pillar depth: defined by wall heater/memory or line patterned width of a row or bottom electrode 

· Nano-Pillar with phase change material as active channel of phase changing region (fire-ball)
· Planarized PCM layer gives a compatible platform for Bi-PCM and OUMS processes.

The nano-pillar Bi-OUM flow is exhibited in Fig 1.  


[image: image1]
The Nano-Pillar OUMS flow is exhibited in Fig 2.


[image: image2]
4. Describe advantage(s) of your invention over what is currently being done.
Phase Change Memory cross section with a sub-lithography capability is delivered with a simpler and robust process flow:  
· Sub lithography dimension is delivered by non-litho-patterning limited technique.  Pillar width is defined by spacer width.  Pillar height is defined by Time etch and/or etch stop precision ( Scalability
· Deposition of Phase Change Memory on forming nano pillar requires no gap fill challenge. ( Scalability and material tune-ability.
· Pitch multiplication compatible ( lower cost

· Self-aligned feature reduces process induced variability of cells physical dimension in the array ( Scalability and cost
5. Include at least one figure illustrating the invention.  If the invention relates to 


software, include a flowchart or pseudo-code representation of the algorithm.

6. How would infringement be detected?
· Identify how use of the invention would be visible, measurable, provable
· Examples of Detection Methods: Visual Examination, Reading Product literature, Reading Programming Reference Manuals, Reading Data Sheets, Reverse Engineering
· Reverse Engineering seeking for sublithography capability,  
DATE:    July/6/2007
INVENTOR:   Greg Atwood


DATE:    July/6/2007
INVENTOR:   DerChang Kau


DATE:    July/6/2007
INVENTOR:   Yudong Kim


OPTIONAL WITNESS SIGNATURE

DATE:    


WITNESS:   



BY THIS SIGNING, I (WITNESS) ACKNOWLEDGE THAT I HAVE READ AND UNDERSTAND THIS 

DISCLOSURE.
Fig. 1: Nano-Pillar Process Flow for BiPCM or Diode-PCM compatible Process flow





Self-Algined Column formation �(replacement Col compatible)





Lower Electrode or PCM Formation








dielectrics dep





Nano-Pillar patterning�NP width = spacer width








Nano-Pillar Etch, Etch Stop compatible





Gap Fill, CMP at the top of Nano Pillar








Memory, Electrode Dep





Fig. 2: Nano-Pillar Process Flow for OUMS compatible Process flow





Gap Fill, CMP at the top of Nano Pillar





Memory, Electrode (and Selector) Dep





Self-Algined Column formation �(replacement Col compatible)





Lower Electrode & row Formation








dielectrics dep





Nano-Pillar patterning�NP width = spacer width








Nano-Pillar Etch, Etch Stop compatible











[image: image3.emf]Spacer Heater or PCM

[image: image4.emf][image: image5.emf][image: image6.emf][image: image7.emf][image: image8.emf]Upper

Electrode

PCM

[image: image9.emf][image: image10.emf]Line Patterned

PCM or Heater

[image: image11.emf][image: image12.emf][image: image13.emf][image: image14.emf][image: image15.emf]PCM

OTS

Mid-Electrode

Upper

Electrode

[image: image16.emf]