Confidential


ISO INVENTION DISCLOSURE FORM
CONFIDENTIAL and ATTORNEY-CLIENT PRIVILEGED COMMUNICATION

Rev. 1 – October 2003

DATE: May/1/2007
It is important to provide accurate and detailed information on this form.  The information will be used to evaluate your invention for possible filing as a patent application.  Send Invention Disclosure forms electronically to the ISO eRoom.
	Last Name:  Kau
	First Name: DerChang
	M.I.

	Business Phone Number: +1-408-765-0266
	Business Fax Number: +1-408-765-5775
	Mailstop: RN3-01

	E-mail address: DerChang.Kau@intel.com
	WWID: 10077599

	Citizenship: USA
	
	
	

	Home Address: 10847 Linda Vista Drive

	City: Cupertino
	State: CA
	Zip: 95014
	Country: USA

	Business Address: 2200 Mission College blvd
	
	

	City: Santa Clara
	State: CA
	Zip: 95054
	Country:


	Last Name:  Atwood
	First Name: Greg 
	M.I.

	Business Phone Number: 408-765-9733
	Business Fax Number: +1-408-765-5775
	Mailstop: RN3-01

	E-mail address: greg.atwood@intel.com
	WWID: 10020991

	Citizenship: USA
	
	
	

	Home Address: 18705 Overlook Road 

	City: Los Gatos
	State: CA
	Zip:
	Country:  USA

	Business Address: 2200 Mission College blvd
	
	

	City: Santa Clara
	State: CA
	Zip: 95054
	Country: USA


	Last Name:  Kim
	First Name: Yudong
	M.I. 

	Business Phone Number: +1-408-765-6997
	Business Fax Number: + 1-408-765-5775
	Mailstop: RN3-01

	E-mail address: Yudong.kim@intel.com
	WWID: 10056409

	Citizenship: USA
	
	
	

	Home Address: 18812 Loree Ave

	City: Cupertino
	State:CA
	Zip: 95014
	Country: US

	Business Address: 2200 Mission College blvd
	
	

	City: Santa Clara
	State: CA
	Zip: 95054
	Country: US


	2.  Title of Invention:

Nano Trench Phase Change Memory


	3.  What technology/product/process (code name) does your invention relate to (be specific if you can):

A path finding test vehicle for OUMS Memory Array validation and exploration using P894/P897 Process Technology and beyond 


	4.
Include several key words to describe the technology area of the invention in addition to # 3 above:

OUM, OUMS, Phase Change Memory, PCM, Triggered PCM, P-RAM


	5.
Stage of development (i.e. % complete, simulations done, test chips if any, etc.):
Path Finding: Concept exploration.  


	6a.  Has a description of your invention been (or planned to be) published outside of the ISO Collaboration:

If YES, please identify the publication and the date published:
No


	6b.  Has your invention been used/sold or planned to be used/sold by Intel, ST Micro, Ovonyx, or others?

No
If YES, date it was sold or will be sold:


	6d.  If the invention is embodied in a semiconductor device, what is the actual or anticipated date of tapeout?

Not Planned Yet.


	6e.  If the invention is software, actual or anticipated date of any beta tests or other public distribution outside the ISO Collaboration: N/A


	7.  Is this invention related to any other invention disclosure that you have recently submitted?  If so, please give the title and

     inventors: No



PLEASE READ AND FOLLOW THE DIRECTIONS ON

HOW TO WRITE A DESCRIPTION OF YOUR INVENTION

Please provide a description of the invention and include the following information:

1. Explain the problem being addressed by the invention.
· Write current reduction using narrowed cross section structure ( nano-trench. 

· Robust process flow for manufacturablility and low variability to produce nano-trench geometry (width and height)

· Pitch multiplication capable self-aligned technology for low cost manufacturing.
· Scalability beyond u-trench patterning limitation   

2. Identify the closest or most pertinent prior art that you are aware of.

· What is done today to alleviate the problem solved by the invention?
· Structural confinement such as Damascene Lance Architecture or other confined structure demonstrated by Taiwan Phase Change Memory Consortium published in VLSI-TSA/2007.
· Reduced Heater/Memory interface such as µ-Trench Architecture and Ringed heater Architecture.
3. Describe in detail what the components of the invention are and how the invention works.

· Provide a summary paragraph of what your invention is, and what it does.
· Next, briefly describe each of the key elements, and how they relate to each other in the overall invention (optional: reference drawings)
The technology is applicable to both single crystalline diode/BJT selector based PCM technology and thin film selector such as OTS based technology.  Key features of the disclosed invention are

· Bottom electrode of the disclosed nano-trench can be a side wall heater or  line/space patterned wordline/row

· Nano-trench formation is based on sacrificial spacer using pitch doubled patterning technique.   
· Sacrificial spacer width defines nano-trench width

· Dual or triple layered dielectric stacks define nano-trench height.  Multiple layers are used for precision CMP stopping therefore thickness and nano-trench height control

· Gap filled nano-trench with phase change material as active channel of phase changing region (fire-ball)
· Planarized PCM layer gives a compatible platform for Bi-PCM and OUMS processes.

The nano-trench Bi-OUM flow is exhibited in Fig 1.  


[image: image1]
The nano-trench OUMS flow is exhibited in Fig 2.


[image: image2]
4. Describe advantage(s) of your invention over what is currently being done.
Phase Change Memory cross section with a sub-lithography capability is delivered with a simpler and robust process flow:  
· Sub lithography dimension is delivered by non-patterning limited technique.  Trench width is defined by spacer width.  Trench height is defined by dielectric dep and CMP stopping capability.  ( Scalability
· Deposition of Phase Change Memory on nano trench requires little gap fill challenge. ( Scalability
· Pitch multiplication compatible ( lower cost

· Self-aligned feature reduces process induced variability of cells physical dimension in the array ( Scalability and cost
5. Include at least one figure illustrating the invention.  If the invention relates to 


software, include a flowchart or pseudo-code representation of the algorithm.

6. How would infringement be detected?
· Identify how use of the invention would be visible, measurable, provable
· Examples of Detection Methods: Visual Examination, Reading Product literature, Reading Programming Reference Manuals, Reading Data Sheets, Reverse Engineering
· Reverse Engineering seeking for subliography capability,  
DATE:    May/1/2007
INVENTOR:   DerChang Kau


DATE:    May/1/2007
INVENTOR:   Greg Atwood


DATE:    May/1/2007
INVENTOR:   Yudong Kim


OPTIONAL WITNESS SIGNATURE

DATE:    


WITNESS:   



BY THIS SIGNING, I (WITNESS) ACKNOWLEDGE THAT I HAVE READ AND UNDERSTAND THIS 

DISCLOSURE.
Fig. 1: Nano-Tench Process Flow for BiPCM or Diode-PCM compatible Process flow





Self-Algined Column formation �(replacement Col compatible)





Lower Electrode Formation








Layered dielectrics dep





Nano-Trech patterning�NT width = spacer width








Dielectric III Gap Fill





CMP at Etch Stop, remove Spacer








Memory, Electrode (and Selector) Dep





Fig. 2: Nano-Tench Process Flow for OUMS compatible Process flow





CMP at Etch Stop, remove Spacer








Memory, Electrode (and Selector) Dep





Self-Algined Column formation �(replacement Col compatible)





Lower Electrode & row Formation








Layered dielectrics dep





Nano-Trech patterning�NT width = spacer width








Dielectric III Gap Fill








[image: image3.emf]PCM or Heater

[image: image4.emf]Dieletric I defines height of Nano-trench

CMP 

stopping

layer

Dielectric III

Can be the same

As the CMP Stop 

[image: image5.emf][image: image6.emf][image: image7.emf]Spacer Heater

[image: image8.emf][image: image9.emf]Dieletric I 

Defines height

of Nano-trench

CMP 

stopping

layer

Dielectric III

Can be the same

As the CMP Stop 

[image: image10.emf]PCM

OTS

Mid-Electrode

Upper

Electrode

[image: image11.emf][image: image12.emf][image: image13.emf][image: image14.emf]Upper

Electrode

PCM

[image: image15.emf][image: image16.emf]