Instructions:

- Do not remove this page. The Brevetto Web application will reject this document if this page is removed.

- You must enable macros so the embedded checkboxes and radio buttons are enabled.

- Fill in your invention description on the following pages.  It is important to provide accurate and detailed information and that you answer ALL of the questions.  This information will be appended to the questions answered online and will be used to evaluate your invention for potential filing as a patent application.

- Review this document with your co-inventors.

- Once complete, edit your Disclosure in the Brevetto Web application. Use the “Upload IDF Document” button on the “Upload IDF Document” tab to upload this document to your disclosure.  You may upload revisions of this document prior to submitting it for approval to enable your co-inventors to view the document online while it is still being edited.  Uploading revisions will overwrite what is currently on file in Brevetto.

PLEASE NOTE:  Contact the TAC for any issues relating to the Brevetto application by phone (e.g. your local prefix +-1234, choose language then option 2, 6, 4) OR online (ServiceDesk.intel.com)

    Click [Submit/View A Request]
    Category="Application Software" 
    Sub-Category="L",
    Item="Legal Applications"

Please provide a description of the invention and include the following information:

A.	THE INVENTION

- Describe your invention:

- What problem(s) does your invention solve?

Reduce IC pin capacitance for high speed data transfer I/Os without degrading ESD performance.

- What is the invention, what are the components, and how does it work?

State of the art electrostatic discharge, ESD, protection uses diodes, D1, D2, D3, D4 shown in Fig. 1, for input only and input/output pins.   Per ESD requirement,

- HBM peak current at 1000V must be 0.68A ± 10%.

- MM peak current at 200V must be 2.9A ± 20%

- CDM peak current at 400V must be 2.1A ± 20%

Due to high transient current discharge requirement subject to ESD events, the ESD protection diode requires large footprint.  Therefore, the pin capacitance is high.

In this invention, a layer of metal-insulator transition, a.k.a. MIT, material is serially connected between the bond-pad and each of ESD diodes, shown in Fig 2.   The MIT material can be

- An Ovonic Threshold Switch, a.k.a. OTS, material or

- A Mott Transition material, typical a transition metal oxide (TMO) such as Ti doped V2O3, Li doped CoO2, or MnO.

At ESD events, MIT material is threshold switching in high conductance state and ESD diode is forward biased.  In one embodiment, an OTS material is used as part of ESD protection scheme for an input pin.   Post threshold/snapback OTS material has current carrying capability > 50MA/cm2, Fig. 3.   To discharge 5Amps of ESD transient current, the area needed is 10um2 or less.  With the OTS at 30nm thick, the ESD event will be triggered at 1uA at 3 volts or less, including OTS threshold switching at 2~2.5V (Fig. 4) plus addition ~0.5V diode forward bias.

During the normal operation, MIT material remains in insulating state.  Pin leakage remains low due to low reverse bias leakage current of the ESD diodes.   With the same embodiment, the OTS capacitance is 30fF, at 10um2 in area and 30nm thick with the dielectric constant =10.  Since the OTS capacitor is connected to ESD diode in series.   The pin capacitance is thus reduced.

- How is your invention new:

- How is the problem currently being solved?

Reduce diode footprint to reduce capacitance for high speed data transfer.  However, this high speed design exposes higher risks subject to ESD events damage.

- What does your invention do to solve the problem differently from current solutions?

Reduce pin capacitance without degrading pin leakage yet maintain a robust ESD protection capability for high speed data transfer applications.

- What specific components/features of your invention are not present in current solutions?

A layer of metal-insulating transition, a.k.a. MIT, material is serially connected between a pad and a ESD diode.

- To the best of your knowledge, identify any other pertinent information related to your invention.

OTS for ESD disclosure co-invented by Stephen Tang, DerChang Kau and Charles Kuo (~2007)

- Describe any aspect(s) of your invention relating to unusual results or unusual functions of the components/techniques in the invention, OR check the box below.

- You MUST include at least one figure illustrating the invention.  If the invention relates to software, include a flowchart or pseudo-code representation of the algorithm.

Fig1. Example ESD protection circuit using silicon diodes .

C4MIT

C3MIT

C2MIT

C1MIT

Fig 2.  This invention; MIT capacitors, C1, C2, C3 and C4, are inserted between pad and ESD protectin diodes, D1, D2, D3 and D4, correspondingly.

Fig 3.  J-V characteristics of MIT material such as OTS.

Fig 3.  Threshold Switching of MIT material such as OTS.

B.	VALUE PROPOSITIONS AND DETECTABILITY

- Value of your invention to Intel (how will it be used by Intel or a competitor).

Provide a robust ESD protection capability for low capacitance high speed data transfer pin.

- Who is likely to want to make, use or sell this invention?

Semiconductor manufacturers.

- How would use of the technology by others be detected (i.e. how would you determine whether someone else was using your invention)?

Physical (SEM/TEM) die analysis