## Slide 1
MetalN
MetalN-1
A
A’
High κ
ILDN+1
MetalN-1
MetalN-1
Inter Layer Dielectric
ILDN Oxide/Nitride
MetalN-1
ILDN Ox/Nit
MetalN-1
ILDN Oxide/Nitride Stack .
MetalN
MetalN-1
ILDN Ox/Nit
MetalN
ILDN+1
MetalN-1
MetalN-1
ILDN
MetalN-1
ILDN Ox/Nit
MetalN-1
ILDN Oxide/Nitride Stack .
MetalN
MetalN-1
ILDN Ox/Nit
MetalN
High κ dielectric film
High κ
Current Art
This disclosure
High κ

## Slide 2
MetalN
MetalN-1
A
A’
ILDN+1
MetalN-1
MetalN-1
Inter Layer Dielectric
ILDN Oxide/Nitride
MetalN-1
ILDN Ox/Nit
MetalN-1
ILDN Oxide/Nitride Stack .
MetalN
MetalN-1
ILDN Ox/Nit
MetalN
MetalN-1
MetalN-1
ILDN
MetalN-1
ILDN Ox/Nit
MetalN-1
ILDN Oxide/Nitride Stack .
MetalN
ILDN+1
MetalN-1
ILDN Ox/Nit
MetalN
High κ
Current Art
This disclosure

## Slide 3
ILD1 (TID)
ILD0 (TID)
Applicable to SOI technology:
Effective removal of thermal energy generated by joule heating
at Transistors on insulator through HTCD layer shown below
Gate
oxide
Gate
oxide
M1
M1
M1
HTCD
Buried Oxide Insulator (A TID layer)
Contact
Contact
M2
M2

## Slide 4
Gap Fill
Dielectric
(TID)
Applicable to Cross Point Memory Technology such as 3D XPointTM
or ReRAM with similar layout topology.
Cross section thru Wordline or BL. HTCD layer may be deployed
either on the top of BL or right below WL.
WL
WL
WL
WL
WL
WL
HTCD
M
S
M
S
M
S
M
S
M
S
M
S
Gap Fill
Dielectric
(TID)
BL
BL
BL
BL
BL
BL
HTCD
M
S
M
S
M
S
M
S
M
S
M
S
WL Metal
WL Metal