## Slide 1
To 3DXP TD/MCD team,
Our IP disclosure filings are extremely sparse. While we are confronting with numerous problems every day, your relentless efforts solves the problems creatively in real time. However, the innovations are not reflected in IP disclosure. Optane technology is Intel’s strategical critical business. Sparse IP disclosures do not align with the execution of the business strategy. Hence, we simplify IP filing initiation with an one-page summary. Before entering the ideas in Aurora system, you can use the problem solving slides from your day-in-day-out technical presentation, condense it to a single page form, see attached file.
This simplified one-page IP disclosure illustrates your innovation to the hot topics you’re fighting. Discretionarily, You can also include one supplementary page as the abstract of your ideas as well as adding annotated exhibits. We expect this one-page summary speed up IP filing, feedback and decision process. Once decision made (in monthly comm meeting), Alan Aldous, IP comm PM, will work with you on Aurora system to start the formal process (and you can be recognized.) You can also go to Aurora web site, file IP directly if you choose so.
Committee members will call for IP harvest sessions in the next few weeks at Folsom by Kiran and Sandeep and at Rio Rancho by Max, Alan and DerChang.
In the meantime, please let us know any questions and suggestions you have. Please also waterfall this message to your team.
Thanks,
DerChang on behalf of 3D XPoint™ IP Committee.

## Slide 2: Lanthanum oxide liner
Hari Chandrasekaran, Hudson Chung
3DxP Optane
4/27/2020
Object of this invention is to protect the active device from deterioration during wafer processing and device operation with the following properties:
  Hermitically tight
  Electrical Insulating
  Uniform conformal film for high aspect ratio structures
  Film deposition at temperatures </= 300C
Currently the active device cross-section area is reduced by > 50% due to deterioration of the active device periphery during wafer processing.
The essential concept for the proposed invention is:
  Thermal atomic layer deposition (ALD)
  High density
  Multilayer thin film with
  LaO close to the device and
  Al2O3/HfO covering the
  LaO layer
A cross-section of the device will reveal the material and technique used to deposit the film.
Advantages of this invention
  Uniform and conformal coverage
  Post process densification not required.
  Repair the oxidation damage to the active device.
Presently, due to temperature constraints plasma CVD technique is used to deposit a film to protect the periphery of the active device. This film is the subsequently densified by Helium plasma.
For high aspect ratio structures
the present techniques have the
following short falls:
  Non-conformal
  Low density
HfO and Al2O3have also been tried with some success
Lichtenwalner D.J. (2013) Lanthanide-Based High-k Gate Dielectric Materials. In: Kar S. (eds) High Permittivity Gate Dielectric Materials. Springer Series in Advanced Microelectronics, vol 43. Springer, Berlin, Heidelberg
Bottom carbon
Top contact
Top Carbon
PM
Middle carbon
SD
Bottom contact
Liner
Bottom carbon
Top contact
Top Carbon
PM
Middle carbon
SD
Bottom contact
Liner

## Slide 3
Introduction –
  There is a need for a higher quality conformal liner to protect the chalcogenide with during processing and operation of the device.
The ideas –
  Lanthanum oxide is thermodynamically more favored than chalcogenide oxides.
  This material can be used to getter the oxygen and repair the oxidation damage to the chalcogenides.
  Potentially, increases the active cross-section and reduce the foot print of the device.
  This idea
What’s new –
  HfO2 and Al2O3 have been tried with success in good coverage. This invention leverages the advantages of metal oxides along with Oxygen gettering that repairs to the device.
Detectability –
  If the device is cross-sectioned it will be trivial to see the material used by composition analysis.
  How do you know your invention is used on a product.

## Slide 4: Other Embodiments
This scheme can also be used to vary the composition and stoichiometry
Doping with other cations ( including but not limited to Sr, Er, Hf) during deposition to vary the properties of the film to suit the device needs.