## Slide 1: High Resistance Interface as a Scalable Joule Heater to Reduce Reset Current and Write Energy for Phase Change Memory
Lu Liu, Ananth Kaushik, Davide Fuga
Optane, 3D Xpoint, Phase Change Memory
4/27/2020
Reset current is defined as the minimal required current for phase change memory to complete set to reset transition. Reduction of reset current is crucial to improve write energy performance in phase change memory.
instead of using one electrode material, a high resistance tunnel junction sandwiched by two thin compound layer, is used in this invention. The two compound interface yields >100x higher resistance than bulk (ρ=0.01~0.4Ohm*cm) at 1nm thickness.
Compared to current solution: <1> The Joule heat is closer to PM. This help reduce reset current by >=25uA <2> The Joule heat relies on interface instead of bulk resistance. The total electrode thickness can be aggressively reduced from 10-18nm to <5nm.
Usage of this invention in competitor’s product can be detected by unpackaging and analysis by TEM/EDX.
The known approach introduces dopant species into electrode or use more resistive material, to increase the bulk electrode resistivity. The achievable range of resistance range is 0.01~0.4Ohm*cm @ 300K.
The current solution requires a decent thickness (10-18nm) of the electrode since joule heating is generated from bulk material. This is not favorable for vertical scaling of memory cell stack.

## Slide 2: Figures
Phase Change Memory
Phase Change Memory
High resistance Interface
Thin compound 1
Thin compound 2
current solution
this invention
 | Electrode1 Thickness [nm] | Electrode 2 Thickness [nm] | Electrode1 rho @ 300K [Ohm*cm] | Electrode2 rho @ 300K [Ohm*cm] | Electrode interface rho @ 300K [Ohm*cm] | Typical Ireset value [uA]
Existing stack | 10~16 | N/A | 0.01-0.4 | N/A | N/A | 105-118
This Invention | 1-2 | 1-3 | 0.01-0.4 | 0.1-0.4 | 100-1100* | 75-89
* Interface resistance is converted to rho at 1nm equivalent thickness for comparison with bulk rho
High resistance Interface
Thin compound 1

## Slide 3
Please start with a clear objective to establish the context of problem solving.
Problem statement is a clear & concise statement on the specific observations of an undesired result.
Please include the essential concept, elements in short bullet points
Please include at least one figure
Please describe how each of the bullet points above would be detected in a competitor’s product (e.g., teardown, reverse engineering, can be seen using ___ technique, likely in product literature…)
Please briefly describe why your solution is better than other solutions (if relevant)
Concise articulation to reflect the known solutions
Current art may come from literatures or other media format in public domain, or Internal comparative analysis and benchmark.
Intel employees must not write about or discuss non-Intel patents or patent applications with anyone without first talking with Intel lawyers as explained in Intel’s policy for reading patents and applications of other companies included at Intellectual Property.

## Slide 4
The supplementary page is the abstract of your invention.
Example shown below uses four attributes to characterize your invention.
Introduction –
  this is the ‘hook’ to IP reviewers. The best hook is to illustrate the live problem you are solving.
The ideas –
  Brief description of invention. Illustrate your originality in solving the problem.
  What are the key elements? Use next page to annotate the exhibits of invention.
What’s new –
  Are there known solutions? Contrast the differences to yours.
Detectability –
  The best way to protect your invention is detectability.
  How do you know your invention is used on a product.
Please use font size 18 or bigger. If you are to provide more information to fit in a page, chances are, another IP disclosure can serve the purpose.