## Slide 1: Cubic Architecture for Cross Point Memory Array
Prashant Majhi, Khaled Hasnat & DerChang Kau
3D NAND, 3DXP, 3D XPoint, 1S1R, Replacement Metal, Subtractive Process
Aug/14/2018
Context:
  Effective cell size of cross point memory cell = [Cell Pitch]2 / [number of memory stacks]
Problem Statement:
  The best known or best technically feasible number of memory stacks is 6. Scaling path will be limited to memory pitch (lateral dimension) when maximum number of memory stack is reached.
This invention opens up the scaling path to increase number of stack without multiplying critical patterning process cost.
The access of memory cell in this new cubic array deploys 3-dimensional select with a unique set of wordline (WL), bitline (BL) and tier (TE) addresses while inhibit the rest of WLs, BLs and TEs, as illustrated in Fig.1 below. See also attached example in slide 2 for random access of cubic array.
The constructs of the cubic array are achieved either by subtractive or replacement processes. The embodiments of replacement process flow is illustrated in the slides 3 to 18. The constructed array is shown in Fig. 2.
Teardown or reverse engineering to detect infringement.
Current 3DXP increases bit density by pitch scaling and stacking layers. But these also increase wafer cost due to multiplying the numbers of critical litho steps when increase number of stack
Intel Optane™ technology delivers 4 decks of memory at pitch of 41nm. The effective cell size is (41nm)2/4=420nm2.
Fig. 1 Cubic Array Schematics
WL0
WL1
WL2
WL3
BL0
BL1
BL2
BL3
BL4
BL5
BL6
BL7
Tier0
Tier1
Tier2
Tier3
Fig.2 Cubic Array Final Construction
Connect to
Tier Decoder
Pillar decoded by WLxBL

## Slide 2: Random Access of Cubic Cross Point Memory Array
VBL,sel
VWL,sel
VWL,desel
VBL,desel
VTier,sel
VWL,sel
VBL,sel
VBL,desel
VWL,desel,
VTier,desel
0V
VT,Set
VT,Reset
SET
RESET
READ
For ISET
For IRESET
For IREAD
VWL,sel illustrated is used as a current clamp for RESET/SET/READ operations.
It can be a simple on/off switch with additional current control circuity outside array
VTier,desel can also use high impedance float by
Switching off the deselected Tier bias circuit
Accessing bit with single
Tier, WL and BL selected
4-Tier XOR 2WLX4BL mini Array
WL0
WL1
BL0
BL1
BL2
BL3
Tier0
Tier1
Tier2
Tier3
VBL,desel
VTier,desel
VTier,desel
VTier,desel
VTier,sel

## Slide 3: 3D XPoint™ Cubic Array Architecture
3D XPoint
XOR array architecture –
Dielectric isolation removed for
Tier to Pillar 3D connectivity visual purpose

## Slide 4: Replacement Tier/Pillar Process Flow

## Slide 5: Memory Tier Stack – 4 Tiers in the exhibit
Silicon Pillar
BL Poly
Memory Tier
Cell 1st Cut
Cell 2nd Cut
WL Poly
Alternate stacking sacrificial layer and dielectric layer to build memory tiers.
Sacrificial material, eg. silicon
Dielectric, eg, oxide

## Slide 6: Tier Stair Formation – an 8-tier exhibit
Mask
Tier Stair Etch
Mask
Mask
Mask

## Slide 7: 1st Cut: Opening for Cell Stack Materials
Silicon Pillar
BL Poly
Memory Tier
Cell 1st Cut
Cell 2nd Cut
WL Poly
A
A’
A
A’
Tier Stair not shown

## Slide 8: Tier Sacrificial Layer Recess Etch
A
A’
A
A’

## Slide 9: 1st Electrode
First Electrode Conformal Dep
First Electrode Recess Etch
A
A’
A
A’

## Slide 10: SD
SD Conformal Dep
SD Recess Etch
A
A’
A
A’

## Slide 11: 2nd Electrode & PM
PM Etch
2nd Electrode dep/etch, PM Conformal Dep
PM Etch
A
A’
A
A’

## Slide 12: 3rd Electrode & Fill: Replacement for Pillar
2nd Electrode Dep/Etch
Sacrificial Pillar Nitride Dep Etch/CMP
A
A’
A
A’

## Slide 13: End of 1st Cut module
A
A’
A
A’
Tier Dielectric, eg. Oxide
Sacrificial material for Tier metal (WordLine), eg. amorphous Silicon
Sacrificial material for Pillar metal (BitLine), eg. Nitride
1st, 2nd, 3rd Electrode,
Selector
Memory

## Slide 14: 2nd Cut definition
Silicon Pillar
BL Poly
Memory Tier
Cell 1st Cut
Cell 2nd Cut
WL Poly

## Slide 15: 2nd Cut
Top Dielectric Removed

## Slide 16: Tier Metal Replacement
Isotropic sacrificial tier material (eg. amorphous silicon) etch then conformal Metal dep (eg. ALD W) fill the gap,
followed by anisotropic
metal etch removing
metal in the 2nd cut
opening region then gap
filled with oxide(not shown)
With
top dielectric
removed, Array with
Tier Stair (termination)

## Slide 17: Pillar Metal Replacement
Isotropic sacrificial pillar material (eg. nitride) removed then Metal (eg. W) fill the gap
gap filled oxide and top tier dielectric are not shown
(not shown)

## Slide 18: Array Interconnect connecting Tier and Pillar to Periphery Control Circuit