## Slide 1: Optane 1.5-BPC ResearcH update
Sanjay Rangan, Hemant Rao, Saad Monasa, Mohammad-Hadi Sorabi, Rouhollah Mousavi Iraei, Shashank Chandrashekara, Sandeep Chekuri

## Slide 2
Objective – Review current understanding of 1.5b/cell and discuss next steps
Current status –
  Focus over the last quarter has been on establishing viability on two areas for the intermediate state
    Placement –
      SD memory effect set back with no PM disturb (nucleation/growth)
    Disturbs –
      Ability to do multiple back to back reads without disturbing PM (nucleation/growth), while setting back the SD after each read
  Results
    We are able to set back the SD for both reads and writes without disturbing the PM through appropriate current and time values
      These values line up well with our understanding of PM nucleation and growth providing confidence on viability (details in key learning slide)
This presentation will discuss the details on the different phases of validation/implementation and further review key data to recommend moving forward on 1.5bpc. There are no fundamental cell/device show stoppers.

## Slide 3: Background: Key challenges for read and placement for middle state
Writing to the intermediate state requires PM to be amorphous and SD in the low VT (setback) state
  Challenges: SD prefers a low current/short time to SET while PM nucleation currents are also in the similar range. Need to manage the current/time window budget properly [discussed in next slide]
We need to threshold switch the intermediate state similar to the POR SET state so read should be able to do a similar behavior on both SD(setback state) /PM (amorphous) same as placement pulse
  Challenges: sensing current/time window needs to be managed similar to writing pulse
Intermediate/middle state
PM : Amorphous
SD : is in lowVT (setback) state
PM: Xtal
SD: lowVT state
PM: Amorphous
SD: highVT state

## Slide 4
Summary table of the phases and status for 1.5bpc

## Slide 5: Key learning
Write (intermediate state placement):
  No (single) read disturb observed for intermediate state
Read disturb:
  Sensing - If Sense current is >=growth, then read disturb is a non-issue; far current delivery needs management
  Set back/term – Time/current optimization minimizes RD RBER
(1)
(2)
(3)
Currents
Time
Log(Currents)
Log(Time)
low current
t_low current
Sense current outside the low current window
t_sen
Rate
Temp
Set time distribution
Seed window
Current
Probability
Low curr
Issr
Issr
Issr
Holdcurr
Set back
Read
Write and read

## Slide 6: Placement to the middle state : Setback time dependence
Requirement: Single pulse enabling max memory effect without PM disturb
Results: No PM disturb observed (validated through reads upto 20ns SB PW)
Histo artifact
Histo artifact
Increasing TSB
Fraction of bits
Fraction of bits

## Slide 7: Placement to the middle state : Precondition effect
Requirement: Single pulse enabling max memory effect without PM disturb
Results: No PM disturb observed and no prior pattern dependency observed
Fraction of bits
Fraction of bits
Fraction of bits
Fraction of bits
Histo artifact
Histo artifact
Notes: 1) Next slide has the read related segmentation for validating PM is not disturbed

## Slide 8: Read disturb on middle state: Issr dependence
Requirement: 1k reads < 1e-4 RBER at 50ns Tsense with setback
Results: Meets requirements at Issr >= Igrowth
4D0, ED1
4D0, ED4
4D0, ED8
4D3, ED1
4D3, ED4
4D3, ED8
0 read setup:
RST, intermediate state
Read pulse
Higher Issr
Post 1k reads on intermediate state
Current delivery related optimized is WIP
Notes: 1) Tsense longer for margin building

## Slide 9: Read disturb on middle state : Tsense dependence
Requirement: 1k reads < 1e-4 RBER at 50ns Tsense with setback
Results: Meets requirements at Issr >= Igrowth and Tsense@50ns

## Slide 10: Summary
No fundamental cell show stopper
Key Linchpins to viability –
  Current delivery capability needs to be resolved
2020 results required to step up/down
  With 20.5nm cell, recommendation is to step up
    Validation on 14nm is needed, but no clear issues identified
  RWB evaluation – window budget and drift to define MM policies
Needs from Process/Integration
  New SD with larger memory effect needed for stack validation and RWB

## Slide 11: Back-up