## Slide 1: Design-Tech CoPathfinding: HVT Experimental Targets
CMOS Pathfinding, WW16.1/2021
Device Design
Window Exploration
Experimental Target and corners
MTS/DTS Risk and Mitigation
DTCP Schedule and NF

## Slide 2: High Voltage Transistor Design
PHV | N-Well/PTS/VT imp | Enh Imp. | Enh Imp2. | Tip Imp
Pitch X’tor LG=5λ | P31 1.3E13 @700KeV P31 6.0E12 @290KeV P31 1E12 @86KeV | As75 1.5e13, 200KeV | P31 1.2E13 @86KeV | BF2 5E13@65KeV Tilt45/Twist0 X4 BF2 2E13@75KeV Tilt0
SVT LG≥7.6λ |  |  |  | 
LVT LG≥9.7λ |  |  |  | 
NHV | P-Well/PTS/VT imp | Enh Imp. | SSH/SLDD | Tip Imp
Pitch X’tor LG=5λ | B11 2.7E13 @340KeV B11 9.0e12 @110KeV B11 3.5e12 @32KeV |  | B11 2.2E13 @25KeV tilt 30 twist 0 X4 P31 2e14, 10KeV, tilt 38 twist 22 X4 | P31 4e13, 55KeV, tilt 45 twist 0 X4
SVT LG≥7.6λ |  | B11 3.0e12 @32KeV |  | 
LG | Type | VT | IS,OFF | ID,lin | ID,sat | GIDL, GISL | Isub,max
(Spec/TCAD Projection) |  | V | pA/μm | μA/μm | μA/μm | pA/μm | μA/μm
5λ | NHV | .621/.822 | 1000/100 | 82.6/82.7 | 637/643 | 0.7,6/0.1,10.2 | 16/37.1
 | PHV | .409/.728 | 8E4/3.6E4 | 24.4/24.4 | 349/296 | 1/4.3 | 0.35/4.26
7.6λ | NHV | .666/.692 | 13/22.8 | 67/64 | 507/513 | .7/.11 | 14/26.2
 | PHV | .561/.638 | 3/1.72 | 18.1/21.7 | 241/221 | .63/.63 | 0.35/1.15

## Slide 3: HV Poly Sizing and Window Exploration
TGT: 225nm, meeting ID,lin Spec
LSL: 215nm limited by PHV leakage
USL: +5nm from target, consistent with pitch cell design rule in stack gate configuration
Fast
Tgt
200
210
220
230
240
250
HVP Poly CD [nm]
Min Poly CD
@ max Ioff spec
~70mV/5nm
~5%/5nm
~10X/5nm
225nm
DR Target
@ ATF sizing
200
210
220
230
240
250
HVN Poly CD [nm]
Fast
Tgt
225nm
~22mV/5nm
~1.7%/5nm
~5X/5nm
DR Target
@ ATF sizing
Min Poly CD
@ max Ioff spec

## Slide 4: Pitch X’tor Target and Corners
 | TCAD | Target | ATF spec | FN/FP | SN/SP | FN/SP | SN/FP
Tox [Å] | 100 | 100 | < 2 | –2/–2 | +2/+2 | 0 | 0
LG [nm] | 228 | 225 | 3 | –10/–10 | +5/+5 | 0 | 0
ZD [nm] | 132 | 132 | < 2 | +3/+3 | –3/–3 | 0 | 0
Spacer | 70 | 70 | 1 | –1/–1 | +1/+1 | 0 | 0
Well/PTS | Model | Model | <2% | NA | NA | NA | NA
VT/Halo | Model | Model | <2% | –2%/–2% | +2%/+2% | –5%/+5% | +5%/–5%
Tip/SD | Model | Model | <2% | +2%/+2% | –2%/–2% | +2%/–2% | –2%/+2%
√D·t | Model | Model |  | NA | NA | NA | NA
RTA | Model | Model |  | NA | NA | NA | NA
μ0 | Model | Model |  | +3%/+3% | –3%/–3% | +3%/–5% | –3%/+5%
Deviation from Target

## Slide 5: Problem #1: Uncalibrated Arsenic doping profile
Risk Level – 2.5 (no data) / Stage – 4 to 5 (Segmentation and Validation)
Mitigation Strategy and action plan –
  Prioritize L0 skew on implant energy/dose and root D·t ; SIMS movies for TCAD calibration. Fast learning cycle; also leverage appliable collateral from 3D-NAND
  In parallel starting 1 cycle of L2 learning on As75 implant optimization
Si-SiO2 Interface
Maximum
depletion Width
Ideal SSR doping
Profile for PHV
As75 6E13
400KeV
As75 2E13
200KeV
As75 1.5E13
200KeV
Calibrated
Uncalibrated
Uncalibrated

## Slide 6: Problem #2: 2X~10X impact ionization (hot carrier damage) Accelerated VT, ID,lin, ID,sat degradation
Model: Accelerated VT, ID degradation at higher impact ionization during hot switching due to 1) 10nm spacer reduction and 2) Steepened LDD doping profile for 30% LG scaling
Risk level – 2.5 (no data) / Stage 3 – Speculation with limited data (TCAD based LDD doping and spacer)
Segmentation Strategy:
  Spec validation
    Correlate device metrics to circuit reliability – device hot switching parameter vs. decoder aging
    Silicon base aging emulation – such as VT, ID aging at operating points
  TCAD based DOE on LATI S/D and SSR Channel to reduce I2; follow up with silicon validation
  Stack gate design rule true spec
PHV Pitch x’tor
NHV Pitch x’tor

## Slide 7: P1250/BWF DTCP
 | 2020 |  |  |  | 2021 |  |  |  | 2022 |  |  | 
 | Q1 | Q2 | Q3 | Q4 | Q1 | Q2 | Q3 | Q4 | Q1 | Q2 | Q3 | Q4
BWF NPI/NTI |  |  |  |  |  |  |  |  |  |  |  | X
Module definition |  |  |  |  |  |  |  |  |  |  |  | 
Experimental Collateral |  |  |  |  |  | X |  |  |  |  |  | 
Speculative Collateral |  |  |  |  |  |  |  | X |  |  |  | 
MTS/DTS for Tapeout |  |  |  |  |  |  |  |  |  | X |  | 
Experimental Design Collateral development.
2 cycle of silicon learning to validate W/L scaling and to calibrate TCAD for target and skew projection
Key results preliminary alignment completed between design rule, MTS and DTS. Experimental process file
Experimental Process File will serve DE-TD alignment for speculative collateral development. ~5WNF
Speculative Design Collateral development
Tech-Design Co Pathfinding use experimental model to flesh out mis-alignment, identify issues and mitigate risk
3~5 cycle of si learning is expected to narrow down DTS spec corner; however, HCI (risk 2.5) may impact Idlin and Idsat.
Key results 70% MTS and DTS validated by silicon. Speculative design collateral is used for component level simulation
CMOS MTS and DTS development
TC04 based MTS and DTS risk are assessed. Full RA/RM and gap closure planned deemed med to low risk.
S/D epi evaluation (at BWF design rule) will be planned.
Process File and design rule will be used for Tapeout.
Module definition to scope out changes from ATF to BWF.
Assumption and POR: 75% $/GB, 15% CoT, 26.5p,space scaling, ATF cell DTS.
Key results 2Kx4K, interlock tile, +1 PD socket, planar CMOS, pitch cell design rule for die size, transistor MTS/DTS and options for Read/Write functionality.

## Slide 8: Supporting Material

## Slide 10: NHV Impact Ionization
ATF LG=350nm, 80nm Spacer
Exp1: 250nm LG, 80nm Spacer
Exp2: 250nm LG, 65nm LG
ATF
Exp1
Exp2
Exp1