1.6.5. Diffusivity of miscellaneous dopants in silicon

In the preceding four sections the diffusivity of the four most common silicon dopants was discussed in detail. There are a a variety of other impurities whose diffusivity may be of inter- est. Table 1.4 presents a compilation of diffusivity values.

Table 1.4: Diffusivity of miscellaneous impurities in silicon.

| Impurity | Temperature range (°C) | D0 (cm2/s) | Ea(eV) | Mechanism | Reference |
| --- | --- | --- | --- | --- | --- |
| B (intrinsic) |  | 0.76 | 3.46 | Vacancy | 6 |
| Ga |  | 225 | 4.12 |  |  |
| In |  | 16.5 269 | 3.9 4.19 |  |  |
| P |  | 3.85 | 3.66 | Vacancy |  |
| Sb |  | 0.214 | 3.65 | Vacancy |  |
| As (intrinsic) |  | 22.9 | 4.1 | Vacancy | 6 |