## Slide 1
Teardown S15 (2 Deck)
Stack Metal
Single Metal
Schematic (4 Deck)
Array WL BL Metals

## Slide 2: Towards Low Resistance WL BL Metals
Assess POR Line Resistance (RL) P1241, P1242
  from RL and BL dimensions, extract r
Benchmark alternative materials (r vs CD, AR) for potential scaling/energy benefits

## Slide 3: DTS (from Sachin)
WL BL Metals |  |  |  |  |  |  | 
Feature | Units | S26 WL0 (single) | S26 BL (stack) | P1241 (WL0 single) | P1241 (BL stack) | P1242 (WL0 single) | P1242 (BL stack)
Width W (nm) | nm | 20.00 | 20.00 | 14.00 | 14.00 | 14.00 | 14.00
Height H (nm) | nm | 35.00 | 80.00 | 30.00 | 60.00 | 30.00 | 60.00
AR | NA | 1.75 | 4.00 | 2.14 | 4.29 | 2.14 | 4.29
X-section Area | nm2 | 700.00 | 1600.00 | 420.00 | 840.00 | 420.00 | 840.00
Cell Pitch | nm | 40.50 | 40.50 | 33.50 | 33.50 | 26.50 | 26.50
Lenth L for 4K cells (nm) | um | 165.89 | 165.89 | 137.22 | 137.22 | 108.54 | 108.54
R (cell) | ohm | 9.30 | 5.40 | 16.87 | 11.13 | 13.34 | 8.80
R line | ohm/micron | 229.63 | 133.33 | 503.58 | 332.24 | 503.58 | 332.24
Resistivity calc | uohm.cm | 16.07 | 21.33 | 21.15 | 27.91 | 21.15 | 27.91
RL for Length with 4K cells | Kohm | 38.09 | 22.12 | 69.10 | 45.59 | 54.66 | 36.06
Capacitance/cell/side | aF | 5.80 | 14.00 | 4.74 | 10.67 |  | 
Capacitance/line | aF/um | 286.42 | 691.36 | 282.99 | 637.01 |  | 
Capacitance for 4K cells line | fF | 47.51 | 114.69 | 38.83 | 87.41 |  | 

## Slide 4: Ru vs W POR
Ru Subtractive Etch |  |  |  | 
CD (nm) | Height (nm) | AR | Line R (ohm/micron) | Resistivity (uohm.cm)
10 | 24 | 2.40 | 1100 | 26.40
12 | 24 | 2.00 | 640 | 18.43
14 | 24 | 1.71 | 520 | 17.47
16 | 24 | 1.50 | 440 | 16.90
10 | 36 | 3.60 | 550 | 19.80
12 | 36 | 3.00 | 390 | 16.85
14 | 36 | 2.57 | 310 | 15.62
16 | 36 | 2.25 | 260 | 14.98
10 | 60 | 6.00 | 250 | 15.00
12 | 60 | 5.00 | 170 | 12.24
14 | 60 | 4.29 | 120 | 10.08
Chart: CD vs Resistivity
| 10 | 12 | 14 | 16
 | 26.4 | 18.432 | 17.472 | 16.896
 | 19.8 | 16.848 | 15.624 | 14.976
 | 15 | 12.24 | 10.08
H: 24 nm
H: 36 nm
H: 60 nm
r: 21.5 [30nm]
[p1241]
R: 503 ohm/um[30nm]
[p1241]
CD [nm]
r [uohm.cm]
CD 14nm and H 24 closest to matching DTS => Potential for ~ 17% capacitance reduction @ H 25nm

## Slide 5: Status of Ru Work @ IMEC
Best IMEC Ru data suggest potential line capacitance reduction of ~17%
IMEC mainly focused on ALD/CVD for semi-damascene
  Early (limited) work on PVD; Anelva tool
  Blanket films Rsh vs thickness
  Preliminary assessment of grain size vs thickness [no grain size modulation expts]
Note: Most of IMEC work subjected to w/ 420C FG anneal
Follow-up AR’s:
  Assess line capacitance/reduction reduction based on 1242 DTS
  Assess Electromigration of Ru (vs W)
  Work on proposal (Max) for RTD Process Modules to start internal project
    Engage vendors and/or IMEC on Custom Work etc?

## Slide 6: Methodology for DTS Capacitance
Line Capacitance known for S26
S26  ATF Capacitance
  Si data available for line cap vs W height at 40nm Pitch
  Based on this and known W height, Pitch changes, ATF capacitance estimated for DTS
  WIP:
    Addressing concerns about data of Cap vs W thickness
    Use more recent / normalized experimental data
    Develop TCAD based assessment of Cap vs Line P/H
ATF  BWF Capacitance
  Use calibrated TCAD and estimate of effective K to extrapolate line capacitance
  TCAD based BWL Capacitance vs Metal Height

## Slide 7: Ratio Math Based Capacitance Estimate
W
W
19.5nm
30nm
W
W
12.5nm
30nm
Ru
Ru
12.5nm
25 nm
 |  | P1241 (W) | P1242 (W) | P1242 (Ru)
Line CD | nm | 14 | 14.00 | 14.00
Line Height | nm | 30 | 30.00 | 25.00
Line Pitch | nm | 33.5 | 26.50 | 26.50
Line Space | nm | 19.5 | 12.50 | 12.50
Keff Space |  | 8 | 8.00 | 8.00
Cap / Cell / Side | aF | 4.74 | 5.85 | 4.87
Cap / 4K Cells | fF | 37.92 | 46.79 | 39.00
Cap / um | aF/um | 282.99 | 441.46 | 367.88
change vs 1241 |  | 1 | 1.23 | 1.03
change vs 1242 (W) |  |  | 1.00 | 0.83
P1241 (W)
P1242 (W)
P1242 (Ru)
P1241 (W)  P1242 (W) Line Cap/Cell inc ~23%
P1242 (W)  P1242 (Ru) Line Cap/Cell dec ~17%
P1241 (W)  P1242 (Ru) Line Cap/Cell inc ~3%
These rough estimates to be updated with TCAD calibrated to expt data and realistic Keff for P1242

## Slide 8: Electromigration of Ru lines
Ru expected to be resilient to EM, based on material properties
Recent experiments suggest that the onset of EM in scaled Ru line occur at high current densities [300MA/cm2 @ 250C induces failure after 9000 sec]
EM not expected to be show-stopper if Ru used for P1242

## Slide 9: Backup

## Slide 10: Early Work on PVD Ru