## Slide 1: Ideas for Operating Current Reduction
 | P1240 | WiSN Removal | CNx TE | W-WSiN Lamella | W-WSiN Double Lam.
Normalized Reset Current [TCAD based] | 100% | 130% | 100% | 78% | 60%*
Physical Change |  | WiSN Removal | TE resistivity Change | Add Barrier (Hot Spot) | Hot Spot Balancing
C
PM
ME
W
PM
ME
W
PM
ME
W
5nm
WiSN
C
PM
ME
W
CNx
PM
ME
W
2.5nm WiSN
2.5nm WiSN
*: 1st order estimate

## Slide 2: WL/BL Physical Electrical and Ru Current Status
Data used is based on the best IMEC Ru data with 420°C FGA
  ALD/CVD for semi-damascene and some early (limited) work with Anelva PVD;
  Preliminary assessment of grain size vs thickness [no grain size modulation semengation]
Next meeting with CR (team Mauro) in WW29 on Ru PVD and etch process learning
Feature | Units | S26 WL0 | P1241 WL0 | P1242 WL0 | 
Width | nm | 20 | 14 | 14 | 
Height H | nm | 35 | 30 | 30 | 
WL/BL length | µm | 166 | 137.22 | 108.54 | 
Metal |  | W |  |  | Ru
Resistivity | Ω/cell | 9.30 | 16.87 | 13.34 | 10.09
 | Ω/µm | 229.63 | 503.58 | 503.58 | 380.96
 | µΩ·cm | 16.07 | 21.15 | 21.15 | 16
WL/BL Resistance | KΩ | 38.09 | 69.10 | 54.66 | 41.35
Ru Subtractive Etch |  |  | 
CD (nm) | Height (nm) | [Ω/µm] | [µΩ·cm]
10 | 24 | 1100 | 26.40
12 | 24 | 640 | 18.43
14 | 24 | 520 | 17.47
16 | 24 | 440 | 16.90
10 | 36 | 550 | 19.80
12 | 36 | 390 | 16.85
14 | 36 | 310 | 15.62
16 | 36 | 260 | 14.98
10 | 60 | 250 | 15.00
12 | 60 | 170 | 12.24
14 | 60 | 120 | 10.08