## Slide 1: SXP vs. BiSM Performance
Description | Target | Ideal | Commit | Drive to | Ideal
Selection | 45ns | 45ns | 45ns | 45ns | 45ns
Nuc, c-cell or endurance | 145ns | 80ns | 145ns | 85~110ns (65ns C-cell) | 20ns demo’d 45ns in SR71
 | 130ns |  |  |  | 
Growth | 60ns | 50ns | n/a | n/a | n/a
Termination/sb | 20ns | 20ns | 20ns | 0ns | 0ns
Setup/Restore | 30ns | 30ns | 30ns | 30ns | 30ns
W2W Cycle time | 300ns | 225ns | 240ns | 160~185ns | 95~120ns
BiSM
BWF
26.5nm BiSM assumes 8% array process cost saving used for energy reduction (eg. Interconnect displacement energy and etc.)
 | Capacity [GB] | SXP Full Stack SLC |  |  |  |  | BiSM |  |  |  | 
 |  | Power | W2W | BW | BWDensity | BWmax | Power | W2W | BW | BWDensity | BWmax
 |  | W | nsec | MB/s | MB/s/GB | GB/s@W | W | nsec | MB/s | MB/s/GB | GB/s@W
ALF32 41nm | 32 | 0.916 | 465 | 1101 | 34 | 1.1@0.9 | 1.300 | 240 | 1563 | 67 | 2.1@1.8
ATF32-A 33.5nm | 32 | 1.012 | 340 | 1506 | 47 | 1.5@1.0 | 1.300 | 240 | 1935 | 67 | 2.1@1.4
ATF32-B 33.5nm | 32 | 1.147 | 300 | 1707 | 53 | 1.7@1.1 | 1.300 | 185 | 1935 | 86 | 2.8@1.9
BWF 64GB 26.5nm | 64 | 1.300 | 300 | 2955 | 53 | 3.4@1.5 | 1.300 | 185 | 3693 | 86 | 5.5@1.9
BWF 32GB 25.5nm | 32 | 0.751 | 300 | 1707 | 53 | 1.7@0.8 | 0.974 | 185 | 2768 | 86 | 2.8@1.0

## Slide 3: Supporting Materials

## Slide 4: 3DXP POR vs. SSM-41p
 | Capacity [GB] | SXP Full Stack SLC |  |  |  |  | BiSM |  |  |  | 
 |  | Power | W2W | BW | BWDensity | BWmax | Power | W2W | BW | BWDensity | BWmax
 |  | W | nsec | MB/s | MB/s/GB | GB/s@W | W | nsec | MB/s | MB/s/GB | GB/s@W
ALF32 41nm | 32 | 0.916 | 465 | 1101 | 34 | 1.1@0.9 | 1.300 | 240 | 1563 | 67 | 2.1@1.8
ATF32-A 33.5nm | 32 | 1.012 | 340 | 1506 | 47 | 1.5@1.0 | 1.300 | 240 | 1935 | 67 | 2.1@1.4
ATF32-B 33.5nm | 32 | 1.147 | 300 | 1707 | 53 | 1.7@1.1 | 1.300 | 185 | 1935 | 86 | 2.8@1.9
BWF 64GB 26.5nm | 64 | 1.300 | 300 | 2955 | 53 | 3.4@1.5 | 1.300 | 185 | 3693 | 86 | 5.5@1.9
BWF 32GB 25.5nm | 32 | 0.751 | 300 | 1707 | 53 | 1.7@0.8 | 0.974 | 185 | 2768 | 86 | 2.8@1.0

## Slide 5: 3DXP POR vs. SSM-41p
 | Pitch [nm] | Partition [GB] | # Partition | Capacity [GB] | Die Size [mm2] | Write [pJ/b] | MW2MW [nsec] | Density [Gb/mm2] | Power [W] | BW [MB/s] | BW Limiter
S26 | 41 | 1 | 32 | 32 | 199 | 104 | 465 | 1.29 |  | 800 | Power
ATF32-A | 33.5 | 1 | 32 | 32 | 133 | 84 | 340 | 1.92 | 1.012 | 1506 | tcycle
ATF32-B | 33.5 | 1 | 32 | 32 | 133 | 84 | 300 | 1.92 | 1.147 | 1707 | tcycle
BWF 64GB LRP | 26.5 | 1 | 64 | 64 | 175 | 55 | 300 | 2.93 | 1.300 | 2955 | Power
 |  |  |  |  |  |  |  |  | 1.502 | 3413 | tcycle
BWF 32GB die chop | 26.5 | 1 | 32 | 32 | 95 | 55 | 300 | 2.69 | 0.751 | 1707 | tcycle
SSM-41p: 32GB Commit | 41 | 1 | 32 | 32 | 199 | 104 | 240 | 1.29 | 1.300 | 1563 | Power
 |  |  |  |  |  |  |  |  | 1.775 | 2133 | tcycle
SSM-41p: Chop Commit | 41 | 1 | 16 | 16 | 110 | 104 | 240 | 1.16 | 0.887 | 1067 | tcycle
SSM-41p: 32GB Drive-to | 41 | 1 | 32 | 32 | 199 | 104 | 160 | 1.29 | 1.300 | 1563 | Power
 |  |  |  |  |  |  |  |  | 2.662 | 3200 | tcycle
SSM-41p: Chop Drive-to | 41 | 1 | 16 | 16 | 110 | 104 | 160 | 1.16 | 1.300 | 1563 | Power
 |  |  |  |  |  |  |  |  | 1.331 | 1600 | tcycle

## Slide 6: 3DXP POR vs. BiSM-ATF
 | Pitch [nm] | Partition [GB] | # Partition | Capacity [GB] | Die Size [mm2] | Write [pJ/b] | MW2MW [nsec] | Density [Gb/mm2] | Power [W] | BW [MB/s] | BW Limiter
S26 | 41 | 1 | 32 | 32 | 199 | 104 | 465 | 1.29 |  | 800 | Power
ATF32-A | 33.5 | 1 | 32 | 32 | 133 | 84 | 340 | 1.92 | 1.012 | 1506 | tcycle
ATF32-B | 33.5 | 1 | 32 | 32 | 133 | 84 | 300 | 1.92 | 1.147 | 1707 | tcycle
BWF 64GB LRP | 26.5 | 1 | 64 | 64 | 175 | 55 | 300 | 2.93 | 1.300 | 2955 | Power
 |  |  |  |  |  |  |  |  | 1.502 | 3413 | tcycle
BWF 32GB die chop | 26.5 | 1 | 32 | 32 | 95 | 55 | 300 | 2.69 | 0.751 | 1707 | tcycle
BiSM-ATF: 32GB Commit | 33.5 | 1 | 32 | 32 | 133 | 84 | 240 | 1.92 | 1.300 | 1935 | Power
 |  |  |  |  |  |  |  |  | 1.434 | 2133 | tcycle
BiSM-ATF: 32GB Drive-to | 33.5 | 1 | 16 | 16 | 133 | 84 | 160 | 1.92 | 1.300 | 1935 | Power
 |  |  |  |  |  |  |  |  | 2.150 | 3200 | tcycle

## Slide 7: 3DXP POR vs. BiSM-28p
 | Pitch [nm] | Partition [GB] | # Partition | Capacity [GB] | Die Size [mm2] | Write [pJ/b] | MW2MW [nsec] | Density [Gb/mm2] | Power [W] | BW [MB/s] | BW Limiter
S26 | 41 | 1 | 32 | 32 | 199 | 104 | 465 | 1.29 |  | 800 | Power
ATF32-A | 33.5 | 1 | 32 | 32 | 133 | 84 | 340 | 1.92 | 1.012 | 1506 | tcycle
ATF32-B | 33.5 | 1 | 32 | 32 | 133 | 84 | 300 | 1.92 | 1.147 | 1707 | tcycle
BWF 64GB LRP | 26.5 | 1 | 64 | 64 | 175 | 55 | 300 | 2.93 | 1.300 | 2955 | Power
 |  |  |  |  |  |  |  |  | 1.502 | 3413 | tcycle
BWF 32GB die chop | 26.5 | 1 | 32 | 32 | 95 | 55 | 300 | 2.69 | 0.751 | 1707 | tcycle
BiSM-28p: 64GB Commit | 28 | 1 | 64 | 64 | 190 | 55 | 240 | 2.69 | 1.300 | 2955 | Power
 |  |  |  |  |  |  |  |  | 1.877 | 4267 | tcycle
BiSM-28p: Chop Commit | 28 | 1 | 32 | 32 | 103 | 55 | 240 | 2.49 | 0.919 | 2133 | tcycle
BiSM-28p: 64GB Drive to | 28 | 1 | 64 | 64 | 190 | 55 | 240 | 2.69 | 1.300 | 2955 | Power
 |  |  |  |  |  |  |  |  | 2.816 | 6400 | tcycle
BiSM-28p: Chop Drive-to | 28 | 1 | 32 | 32 | 103 | 55 | 160 | 2.49 | 1.300 | 2955 | Power
 |  |  |  |  |  |  |  |  | 1.408 | 3200 | tcycle

## Slide 8: 3DXP POR vs. BiSM-26.5p
 | Pitch [nm] | Partition [GB] | # Partition | Capacity [GB] | Die Size [mm2] | Write [pJ/b] | MW2MW [nsec] | Density [Gb/mm2] | Power [W] | BW [MB/s] | BW Limiter
S26 | 41 | 1 | 32 | 32 | 199 | 104 | 465 | 1.29 |  | 800 | Power
ATF32-A | 33.5 | 1 | 32 | 32 | 133 | 84 | 340 | 1.92 | 1.012 | 1506 | tcycle
ATF32-B | 33.5 | 1 | 32 | 32 | 133 | 84 | 300 | 1.92 | 1.147 | 1707 | tcycle
BWF 64GB LRP | 26.5 | 1 | 64 | 64 | 175 | 55 | 300 | 2.93 | 1.300 | 2955 | Power
 |  |  |  |  |  |  |  |  | 1.502 | 3413 | tcycle
BWF 32GB die chop | 26.5 | 1 | 32 | 32 | 95 | 55 | 300 | 2.69 | 0.751 | 1707 | tcycle
BiSM-26.5p: 64GB Commit | 26.5 | 1 | 64 | 64 | 190 | 44 | 240 | 2.93 | 1.300 | 3693 | Power
 |  |  |  |  |  |  |  |  | 1.502 | 4267 | tcycle
BiSM-26.5p: Chop Commit | 26.5 | 1 | 32 | 32 | 103 | 44 | 240 | 2.69 | 0.751 | 2133 | tcycle
BiSM-26.5p: 64GB Drive to | 26.5 | 1 | 64 | 64 | 190 | 44 | 240 | 2.93 | 1.300 | 3693 | Power
 |  |  |  |  |  |  |  |  | 2.253 | 6400 | tcycle
BiSM-26.5p: Chop Drive-to | 26.5 | 1 | 32 | 32 | 103 | 44 | 160 | 2.69 | 1.126 | 3200 | tcycle

## Slide 9: CR Performance Trend and need for Write BW
DCPMM performance trend [2R:1W] vs. DRAM shows ~5X gains from 1st gen to 4th gen with ATF Commit of 1100MB/s.
ATF drive-to of wrt2wrt_same_part of 320ns or 1600MB/s provides further ~18% gain reducing gap to DRAM.
  Monotonic trend of improvement in DCPMM performance at 80% return on Media BW gains up to ~2200MB/s
Source: Ben Graniello
DCPMM BW [GB/s]
ATF Media Write BW [GB/s]
DCPMM
DRAM

## Slide 10: Optane Media Write BW Breakdown
Write BW = Min of {# of Partitions/wrt2wrt_timing OR Power limit/Write Energy}
Concurrency especially read and writes combination allowed is additional factor DCPMM performance
Partition count = Function (Array pitch, Tile size)
ATF32 = 32 partitions
Wrt2wrt timing = Primarily limited by Set Algorithm (details next)
ATF32 = 465ns (Commit), 320ns (Drive to)
Die Power Limit = Function (Power bus, Thermal dissipation)
ATF32 = 1.2W w/ TM1 and TM2
Write Energy = Function (Algorithm features, Bias and Currents)
ATF32 = 84 pJ/b for MWR or 95 pJ/b for NWR (TT)

## Slide 11: MWrite BW [Mwrt2Mwrt timing] Breakdown and Forward Path
Description | Why | Ideal State | Line of Sight on ATF A0 (reference numbers) | Line of Sight on ATF B0
Selection | Endurance | 45ns | 45ns (65ns) | 45ns
Nucleation | E4/Shelf-life Capability | 0ns [3X lower cell leakage or 2X lower Drift SD material/Integ. ] | 165s (220ns) [Partition offset, No writeV, Cell tweak] | 150ns [Partition offset, No writeV, Cell tweak, C-cell patch]
 | Endurance | 80ns [2X faster time0 or No cycling degradation] | 130ns (220ns) [Scaled PM, Electrode/seal] | 130ns [Scaled PM, Electrode/seal]
Growth | Endurance | 50ns [No cycling degradation] | 60ns (60ns) [Scaled PM, Electrode/seal] | 60ns [Scaled PM, Electrode/seal]
Termination | Drift/Retention | 20ns | 20ns (40ns) | 20ns
Overhead | Accounting, Setup | 30ns | 55ns (55ns) | 30ns [PCL optimization]
Net time |  | 225ns | 345ns (440ns) | 305ns
Write BW |  | 2200MB/s | 1480MB/s (1100MB/s) | 1600MB/s

## Slide 12: Strategy and timeline
ATF Start-up/ES0/ES1 at 465ns or 1100 MB/s which has medium to high confidence with S26A based validation (Cell + Algo features) and assuming nucleation time is 2X of S26A
ATF ES2 (~100K cycles) drive to ~345 ns or ~1480 MB/s for Q3’21 output based on 3-4 4D info-turns post 1st Silicon. (need to decide what es2 is, need to avoid late changes that make time larger, need to avoid interim goals at the same time, need to discuss the strategy)
  Implement bin/monitor at Sort/WLR/WLM to provide technology learning feedback and transition to faster write timing when yield at faster timing >10%
  Subsequently drive Endurance (100K to 2M) to deliver QS in Q1’22
Further design improvements including PCL optimization and C-cell patch decode to enable wrt2wrt_sampepart <320ns or 1600 MB/s  Push to Bow Falls

## Slide 13: Write timing Scaling Further Details, Validation
Design Stepping | Pareto Item | Impact | Gain | How | Collateral | When
A0 | Nucleation | E4 | 10ns | Partition Offset | S26A Emulation | Done
 |  |  | 30ns | Eliminate WriteV | S26A Emulation ATF Spider lkg | 
 |  |  | 25ns | Thk liner Seal/Smooth BEC N2 pass SiGe CMOS | ATF41 | 
 |  | Endurance* | 90ns* | Scaled PM Electrode/Seal for seg. | ATF41 | 
 | Growth | Endurance | 30ns | Scaled PM Electrode/Seal for seg. | ATF41 | 
 | Termination | Drift | 20ns | Match Read | S26A Emulation | 
 | Selection | Endurance | 20ns | Remove 2nd cut WSiN | ATF41 | 
 | Overhead | Accounting | 15ns | Rev3 full chip SIMs | ATF Rev3 | 
B0 | Overhead | None | 25ns | PCL Redesign | TBQ | 
 | Nucleation | E4 | 15ns | C-cell patch | TBQ | 
~345ns
<320ns
* Minimum of gain for Nucleation between E4 and Endurance