## Slide 1: CV DOT L1E
Three single mask flows with two types of masks
  Opt.1 – Etch/Ring: (5-10um width at 25-100um diameters)
  Opt.2 – Etch/Square (10-100um)
  Opt.3 – Liftoff/Square (10-100um)
   Preferred flow: Opt. 3
Three coupon lines.
  Mark Doczy’s ALD film integration line @ CR
  Van Le’s thin film transistor line @ CR
  Larry Wong’s captive external research line @ Lotus
  Lotus seems a preferred option; it’s FIFO for work requests with 1 to 1.5week cycle time, with options maturity. And they also has large variety of TE material for square dot.
Stack Options
 |  |  | TE metal from CV dot lab
 |  |  | Seal: POR Carbon or Nitride or HiK 5nm
 |  |  | Chal Film 10 to 40nm
 |  |  | With or without BE 5nm max
 |  |  | P type, 8Ω·cm (B11, 1E15/cc and 1mΩ·cm B11, 1E20/cc)