## Slide 1: 3DIC Optionality & Decision Tree
Building Common Metrics through Modularity
Jan 25, 2022
Prashant, Max, Jason and DerChang
Contains or derived from supplier Confidential Information

## Slide 2: 3DIC High Level Scope
(Under Development)
3DIC Cookbook –
  Develop common metrics-based ingredients book to quantify 3DIC modularity
  Apr/2022
STCO – Design Automation to shrink wrap 3DIC Cookbook
  SPICE Model development reflect MTS and DTS in 3DIC cookbook
  Aug/2022
“Hard IP” development – Library cell standardization (power and size scaling)
  CXi extension (from mm of 2.xD to µm of 3D)
  I/O protocol vs. signal signal propagation
  ECD tbd

## Slide 3: Executive Summary:
Setup framework for 2.5D/3DIC Pathfinding
  2.XD
      benchmarked key 2.XD internal/external options
      developing insights on scalability based on key metrics for modular designs
  3D
      Identified key 3D internal/external options to benchmark (WIP)
      developing insights on scalability based on key metrics for modular designs (WIP)
This meeting to discuss strategy, framework, status…

## Slide 4: 2.XD/3DIC Pathfinding: Objective and Key Results
Objective: Develop common metrics-based ingredients book and use it to quantify 2.xD and 3DIC modularity
Key Results:
Produce common metric cook book and benchmark options
Test chip design using learnings from cookbook to evaluate/validate KPI
Guide product exploration of 3dic technology choice (ex: bzm, arn, cor, ptl, flatrock, lch-ecf, …)
KPI (D2D connection density, delay, bandwidth density, energy/bit, thermal and power routing) based scoring of 2.xD and 3DiC options for improved D2D and D2Package connectivity

## Slide 5: 2.XD/3DIC Pathfinding Focus Team: Charter, Milestones

## Slide 6: Chips/Chip, Wafer 3D Stacking (FE 3D connects chiplets by stacking)
Logic
Transistors
Interconnects
Memory
Transistors
Interconnects
Substrate
Bonding Interface T
Bonding Interface B
Bonding Interface B-S
Adaptor (TSV)
Chips/Substrate 2.X D Stacking
(BE 3D is an adaptor technology in Packaging)
Memory
Transistors
Interconnects
Bonding Interface
Logic
Transistors
Interconnects
Si
Adaptor
Substrate
Memory
Transistors
Interconnects
Logic
Transistors
Interconnects
Substrate
Si
CoWoS
EFB
EMIB
Memory
Transistors
Interconnects
Logic
Transistors
Interconnects
Substrate
Si
3DIC

## Slide 7: Ingredients of BE 3D (2.x D Stacking)

## Slide 8: Connectivity for Electronic Components
Each adaptor possesses two basic functions
Bonding Interface (and/or Plug) serves an interface of the component connecting to the other
Connector serves for
  Wiring for signal and power routing (parasitics),
  Impedance matching or signal filtering (passives) Function augmentation (passives and/or active)

## Slide 9: A Parallel to 3DIC
Adaptor
IP Blocks

## Slide 10: Yet another parallel to 3DIC
SoC
Memory
Memory
Memory
Memory
Memory
Memory
Memory
Memory
AJ Su, et.al., ECTC 2019 (https://ieeexplore.ieee.org/document/8811022)
Adaptor-on Adaptor

## Slide 11: Features of “Adaptor” for 3DIC connectivity
Bonding Interface: front and back interfaces (ie. C4, µB and HB) connecting chiplets and substrate
Stacking: lateral and vertical layering capability
Interconnect: wiring (ie. ReDistribution Layer and Thru-Mold-Via) for signal and power routing
Embedding: including
  bridges for fine pitch routing
  passives for impedance balancing and/or signal filtering
  actives for functionality augmentation

## Slide 12: Genealogy of 2.x D
Si Interposer
Substrate
2.5D
Bridge-Less
2.3 D
Embedded Bridge
EMIB
Elevated Bridge
FO-EB-T

## Slide 13: Genealogy of 2.x D
Start [Cu Post => Emb-Chip => RDL => Chiplets]
Finish
FOV-ODI
Start [RDL => Cu Post => Emb-Chip => RDL => Chiplets]
Finish
FO-EB-T
Start [Chiplets => Emb-Chip => Cu Post => RDL => Substrate]
Finish
INFO-L
Substrate
Emb-Chip
Chiplet 1
Chiplet 2
RDL
Cu Post
Substrate
bridge
Chiplet 1
Chiplet 2
Cu

## Slide 14: Adaptor (2.x D) Cookbook
Adaptor 2.xD Technology | Name | Foveros Omni | FO-EB-T | InfO_LSI
 | Supplier | Intel | SPIL | TSMC
 | Substrate Size | 100·100mm2 | 100·100mm2 | 65·65mm2
 | Readiness (yield trajectory TBD) | 2025 | 2024 | 2021
Bonding Interface | Module Size | 700mm2 | 3000mm2 | 1700mm2
 | Process | Chip Last | Chip Last | Chip First
 | Chiplet i/f | µB | µB | µB / Cu Via
 | Pitch [µm] | 25 | 20 | 25
 | Subst i/f | C4 | C4 | C4
 | Pitch [µm] | 110 | 80 | 90
 | distancemax to edgemold | 750µm |  | 
Stacking | # of Die placement | No Limitation | No limitation | No limitation
 | thickness | 160 µm | up to 700µm (HBM) | 100µm
Interconnect | RDL material | Cu in PBO or Polyimide | Cu in Polyimide | Cu in Polyimide
 | # of RDL layers | 1 top Layer No bottom Layer | 3 Top layers 2 bott layers | No Top RDL 2 bott Layers
 | RDL Design Rules | 5/5µm L/S | 5/5µm L/S 7/14µm via/landing | 5/5µm L/S
 | Post material | Cu | Cu | Cu
 | Post Diameter | 70/64/58 µm | 60µm | 
 | Post Pitch | 110µm | 90µm | 
 | Post height | 112µm | 105µm | 
 | Post keep out zone | 40µm |  | 
Embedding capability | Integrated Passives | Cache, VR etc | MiMCap, StackCap | DT Cap, MiM cap, Inductor
 | Lateral aspect ratio | <10 | <4 | <10
 | Chiplet min. spacing | 40µm |  | 
 | Materials | Si | Si/Oxide | 
 | Thickness | 50µm | 50µm | 
 | TSV | YES | Yes | 
FO-EB-T
Foveros Omni

## Slide 15: Key Takeaways from 2.x D Cookbook Analysis
Key Metrics for Modular Designs: Scalability for (A) # of chiplets/package and (B) connectivity [improved d2d (and d2package) connection density, BW and Energy/Bit]
For (A)  All 3 options (FV-ODI, FO-EB-T, Info-L) are scalable for large #dies/package
For (B)  Which of these options provide best scaling for connection density and is compatible to HBI?  Post First or Post Last [a.k.a Chip-First or Last]?
Other considerations: FV-ODI total stack thickness <300um complicates HBM like integration
Follow-up’s: Identify dependency (and flexibility) based on integration flow
  Chip-First vs Chip-Last
  Cu Post before (or after) base Chip attach
  Flexible control of base chip and top chip thickness
  …

## Slide 16: Can 2.xD Support Hybrid Bonding?
Substrate
bridge
Chiplet 1
Chiplet 2
Cu
Scaling Connection density and energy via hybrid bonding?
WIP: Max’s First Pass Assessment

## Slide 17: Ingredients of FE 3D (Chiplet Stacking)

## Slide 18: 3DIC: Decision Tree
Substrate/Package
Si (Bottom):
Transistors
Interconnects
Transistors
Interconnects
Memory/Logic
Bonding Interface T
Bonding Interface B
Bonding Interface D2P/S
ubump
Hybrid bonding
L0
Die Last
Die First
L1
TSV
CD/H; AR
Isolated, Bundle
Integration: Mid, Last
Routing [dedicated for HB; Testing pad KGD]
3D Stacking
Logic-Logic; Logic-Memory
Same node; Mixed Node
F2F, F2B; TD > = < BD
Res
Cap
Ind
3DIC Decision Tree
Key Takeaways
Multiple configurations of 3D stacking possible
Power, Signal and Thermals are key considerations
3DIC Hybrid Bonding is Front-End Process and hence RDL (routing) is Cu DD process
Base/Bottom Die is critical for 3DIC configs
  Die thickness, TSV and HB Pitch critical
  Need to quantify
    Bonding Layer: uBump/HB [R, C, L]
    TSV [R, C, L]
    Consider 1st and 2nd order impact based on complete routing path [Elmore]
Assess pros/cons of different stacking to guide high ROI modular designs

## Slide 19: 3D Stacking (Chiplet Technology) Cookbook
3D Technology | Name | Foveros Direct (F2F) | SoIC-CoW (F2B) | SoIC-CoW (F2F) | SoIC-WoW (F2F)
 | Supplier | Intel | TSMC | TSMC | TSMC
 | Die Size (Max/Min for Top or Base) |  |  |  | 
 | Readiness (Yield trajectory) | 2025 | 2022 | 2022 | 2017
Surface Bonding Interface (Top to Base) | Process (T2B) | F2F | F2B | F2F | F2F
 | Chiplet i/f | HB | HB | HB | HB
 | Pitch [µm] | 9 | 9 (21), 6(22), 4.5(24) | TBD | TBD
 | RDL Top Surface | Cu DD | Cu DD | Cu DD | Cu DD
 | RDL Base Surface | Cu DD | -- | Cu DD | Cu DD
Stacking | # of Die placement (Top) | No Limitation | No limitation | No limitation | 1
 | # of Die placement (Base) | No Limitation | No limitation | No limitation | 1
 | Die thickness (Top) | 50-100 | Scalable down to ~10um | TBD | No limitation
 | Die thickness (Base) | 50-100 | Scalable down to ~10um | TBD | Scalable < 2 um
 | Chiplet min. spacing and gap fill | ?, mold | 1-5 um?, oxide |  | 
 | Embedding capability | Yes | Yes | Yes | NA
Base Die Characteristics | TSV CD | 8? | 2 (21), XYZ (22+) | TBD | Scalable to n-TSV
 | TSV Pitch | 15? | = HB Pitch (9, 6, 4.5) | TBD | Scalable
 | TSV Height | 80? | 8 (21), XYZ (22+) | TBD | Scalable
 | TSV Material | Cu | Cu | Cu | Cu, W
 | TSV Process (First, Mid, Last) | Mid | Mid | Mid | Mid and Last
 | TSV KOZ | 8? | TBD | TBD | Scalable
Base Die capability | BD Function | Logic, Cache, DRAM | Logic, Cache, DRAM | Logic, Cache, DRAM | DTC, Logic, Cache, DRAM, NVM
 | Size or Shape Restriction |  |  |  | 
WIP

## Slide 20: Advanced Process Node Readiness for 3D
Chiplet | Technology | P1222 | 10FV | 7FV | Intel 4 | Intel 3 | Intel 20A | Intel 18A | N7 | N5 | N3B | N3E | N2 | 3GAP | 4LP
 | Supplier | Intel | Intel | Intel | Intel | Intel | Intel | Intel | TSMC | TSMC | TSMC | TSMC | TSMC | Samsung | Samsung
 | Technology type | logic/edram/ms | logic/ms | logic/ms | Logic | Logic | Logic | Logic | logic/SRAM | Logic/SRAM | Logic | Logic | Logic | Logic | Logic/SRAM
 | Bonding Side | Surface + Back | Surface +Back | Surface + Back | Surface | Surface | Surface | Surface | Surface/Backside | Surface/Backside | Surface | Surface | Surface | Surface | Surface/Backside
 | Chiplet thickness | ~80 µm | ~70 µm | ~50 µm | TBD | TBD | TBD | TBD | Scale ~ 10 µm | Scale ~ 10 µm | TBD | TBD | TBD | TBD | TBD
 | Readiness | 2020 | 2022 | 2023 | 2023 | 2024 | 2025 | 2025 | 2021 | 2022 | 2024 | 2024 | TBD | TBD | TBD
Surface bonding | Bonding Interface | µB | µB | µB | µB | µB | µB/HB | µB/HB | µB/HB | µB/HB | HB | HB | HB |  | 
 | Pitch [µm] | 25 | 25 | 25 | 25 | 25 | 25/9 | 25/9 | 9 µm | 6 µm | 4.5 µm | 4.5 µm | TBD |  | 
 | # of RDL layers |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 | RDL Design Rule |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 | KGD capability | Yes | Yes | Yes | Yes | Yes |  |  | Yes | Yes | Yes | Yes |  |  | 
Back Side bonding | Bonding Interface | µB | µB | µB |  |  |  |  | HB | HB | TBD | TBD | TBD |  | 
 | Pitch [µm] |  |  |  |  |  |  |  | 9 µm | 6 µm | 4.5 µm | 4.5 µm | TBD |  | 
 | # of RDL Layers |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 | RDL Design Rule |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 | TSV material |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 | TSV Diameter |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 | TSV Pitch |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 | TSV Height |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 | Keep Out |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Captured in Chiplet Technology Cookbook
WIP

## Slide 21
Si (Bottom):
Transistors
Interconnects
Si (Top):
Transistors
Interconnects
Substrate
Si (Top):
Transistors
Interconnects
Si (Bottom):
Transistors
Interconnects
Substrate
Si (Top):
Transistors
Interconnects
Transistors
Interconnects
Substrate
F2B(std)
F2F (BS-PDN)
Feature | F2F (std) | F2B (std) | F2F (ODI) | F2B (ODI) | F2F (BS-PDN)
Bonding Interface T | Bump/Pad [R,L,C] | Bump/Pad [R,L,C] | Bump/Pad [R,L,C] | Bump/Pad [R,L,C] | Bump/Pad [R,L,C]
Adaptor T-B | --NA-- | TSV (B): micro-TSV | --NA-- | TSV (B): micro-TSV | --NA--
Bonding Interface B | Bump/Pad [R,L,C] | Bump/Pad [R,L,C] | Bump/Pad [R,L,C] | Bump/Pad [R,L,C] | Bump/Pad [R,L,C]
Additional routing T-S | TSV (B) | TSV (B) | TMV | TMV | nano-TSV(B) + IC(B)
Adaptor B-S | TSV (B) | --NA-- | TSV (B) | --NA-- | nano-TSV (B)
Bonding Interface B-S | C4 bump | C4 bump | C4 bump | C4 bump | C4 bump
F2F (ODI)
Si (Top):
Transistors
Interconnects
Si (Bottom):
Transistors
Interconnects
Substrate
Si (Top):
Transistors
Interconnects
Substrate
Si (Bottom):
Transistors
Interconnects
F2B (ODI)
Bonding Interface T
Bonding Interface B
Bonding Interface B-S
RDL like Routing to HB pads
prashant majhi, FTE
F2F(std)
3DIC-HBI Options to Benchmark

## Slide 22: Key Takeaways from 3DIC HBI Cookbook Analysis
Key Metrics for Modular Designs: Scalability for (A) # of chiplets/package and (B) connectivity [improved d2d (and d2package) connection density, BW and Energy/Bit]
3DIC focused on (B); while (A) is supported by 2.xD in combination with 3D
Scaling bond pitch and TSV size critical to improve d2d connectivity => HBI and thin dies
Backside PDN has noteworthy implications to 3D stacking
Quantification of pros/cons between options is WIP …. Need more rigorous assessment  DTS/MTS/IP/Logic-Memory/Test/Cost
Follow-up’s: Identify dependency (and flexibility) based on integration flow
  CoW vs WoW
  CoW: Collective vs Pick n Place; Re-constituted with RDL into wafer form?
  F2F, F2B, process flows with temporary carriers;
  Yield dependence on process flow
  …
Contains or derived from supplier Confidential Information

## Slide 23: Building the 3DIC PF Framework and Ingredient Book
Scope | Topics to address | Resources
MTS | Design rules for HB as f(Pitch) Pad size/shape; F2F/F2B; TSV DR and KOZ; Wafer/Die thinning and spec for CoW (direct or collective) and WoW | Internal Assessment; Process Vendor engagements; IMEC simulations/Experiments; PTD/ATTD assessment;
DTS | Interconnect density; HB and TSV parasitics for different F2F/F2B configurations; Stack d2d signal latency from Tx-to-Rx; power/bit; | Internal Assessment; EDA Vendor engagements; IMEC simulations/Experiments; PTD/ATTD assessment;
IP & Collaterals for Library | I/O-Free or I/O-light based routing considerations; HB pad as f(Mx) and KOZ for routing considerations; HB vs uBump D2D connectivity benchmarking (CXI in 3D) | Internal Assessment; EDA/Foundry engagements;
Memory and Sub-System | SRAM cache sub-system disaggregation; DRAM cache or memory sub-system disaggregation; PMEM NVM-Storage | Internal Assessment; EDA Vendor engagements; IMEC simulations/Experiments; PTD/ATTD assessment;
3DIC Cost and Yield Analysis | Process Cost Analysis from bottom-up; Total Cost of Ownership including Yield impact | Internal Assessment; Sponsored engagements; IMEC assessments;
Note: Did not include test considerations and TFM with EDA readiness for 3D APR, although they are critical components for 3DIC ecosystem

## Slide 24: 3DIC Modularity Scorecard
Use the common metrics of the ingredients book to quantify 3DIC modularity
A Modular system consists of independent modules with clearly defined interfaces that can be specified and verified.
Besides benchmarking the technical merit of the common metrics, we should use a modularity scorecard to address
  Cohesion – dissimilarity of functions in one module, ie. function overload (ADM in MTL)
  Coupling – interaction within and between modules
Other Figures of Merit in modularity¶ include
  Change Control – Reconfigurability, Adaptability.
  Latitude & Roadmap – Reusability, Alterability, Scalability
  Cost & Projection – Complexity, Standardization.
  Compatibility – Commonality, Customization, Substitutability
  ¶: https://ieeexplore.ieee.org/document/7069975, Regine Dörbecker et.al., 2015 48th Hawaii International Conference on System Sciences

## Slide 25: Backup

## Slide 26: F2F(Std)
Si (Bottom):
Transistors
Interconnects
Si (Top):
Transistors
Interconnects
Substrate
Si (Top):
Transistors
Interconnects
Si (Bottom):
Transistors
Interconnects
Substrate
Si (Top):
Transistors
Interconnects
Transistors
Interconnects
Substrate
F2B(std)
F2F (BS-PDN)
Feature | F2F (std) | F2B (std) | F2F (ODI) | F2B (ODI) | F2F (BS-PDN)
Socket T | Bump/Pad [R,L,C] | Bump/Pad [R,L,C] | Bump/Pad [R,L,C] | Bump/Pad [R,L,C] | Bump/Pad [R,L,C]
Adaptor T-B | --NA-- | TSV (B): micro-TSV | --NA-- | TSV (B): micro-TSV | --NA--
Socket B | Bump/Pad [R,L,C] | Bump/Pad [R,L,C] | Bump/Pad [R,L,C] | Bump/Pad [R,L,C] | Bump/Pad [R,L,C]
Additional routing T-S | TSV (B) | TSV (B) | TMV | TMV | nano-TSV(B) + IC(B)
Adaptor B-S | TSV (B) | --NA-- | TSV (B) | --NA-- | nano-TSV (B)
Socket B-S | C4 bump | C4 bump | C4 bump | C4 bump | C4 bump
F2F (ODI)
Si (Top):
Transistors
Interconnects
Si (Bottom):
Transistors
Interconnects
Substrate
Si (Top):
Transistors
Interconnects
Substrate
Si (Bottom):
Transistors
Interconnects
F2B (ODI)
Socket T
Socket B
Socket B-S
RDL like Routing to HB pads
Key Process Features | Electrical Spec | Physical Spec | Comments
Bonding Pads | R, L, C as f(Pitch) | # connections/mm2; DR layout | 
TSV for F2F | R, L, C as f(Size) | # TSV/mm2; AR; KOZ | 
TSV (micro) for F2B |  |  | 
TDV/TMV (for ODI) | R as f(Pitch/Size) | # TDV/mm2; | 
RDL like layer for HB |  |  | 

## Slide 27: Bonding Layer: uBump / HB Considerations
R, L, C as function of Pitch
Routability [especially for fine P]
Testing for KGD?
ESD need/strategy?

## Slide 28
3DIC: uBump  HB: Guesstimating Parasitics [Only Pads]
 |  | E0 (F/cm) = | 8.85E-14 | E0 (fF/um) = | 8.85E-03 |  | 
 |  | Capacitance= | A*E0*Er/D |  |  |  | 
 | Square Pad | Simple Math |  |  |  |  | 
 | P | CD | A | D | Er | Pad C | 
 | Pad Pitch (um) | Pad Size (um) | Pad Area (um2) | Pad to Ground Plane Thickness (um) | Dielectric K | Pad Capacitance (fF) | Total Pad Capacitance (fF)
 | 1 | 0.5 | 0.25 | 1 | 3.9 | 8.63E-03 | 1.73E-02
 | 2 | 1 | 1 | 1 | 3.9 | 3.45E-02 | 6.90E-02
 | 4 | 2 | 4 | 1 | 3.9 | 1.38E-01 | 2.76E-01
 | 6 | 3 | 9 | 1 | 3.9 | 3.11E-01 | 6.21E-01
 | 9 | 4.5 | 20.25 | 1 | 3.9 | 6.99E-01 | 1.40E+00
 | 10 | 5 | 25 | 1 | 3.9 | 8.63E-01 | 1.73E+00
 | 16 | 8 | 64 | 1 | 3.9 | 2.21E+00 | 4.42E+00
 | 20 | 10 | 100 | 1 | 3.9 | 3.45E+00 | 6.90E+00
 | 26 | 13 | 169 | 1 | 3.9 | 5.83E+00 | 1.17E+01
 | 36 | 18 | 324 | 1 | 3.9 | 1.12E+01 | 2.24E+01
 |  | Resistance = | r*L/A | Cu rho (ohm.um)= | 1.70E-02 |  | 
 |  | CD | L |  |  |  | 
 | Pad Pitch (um) | Pad Size (um) | Pad Height (um) | Metal rho (ohm.um) | Pad Resistance (ohm) | total Pad R (ohm) | 
 | 1 | 0.5 | 1 | 1.70E-02 | 6.80E-02 | 1.36E-01 | 
 | 2 | 1 | 1 | 1.70E-02 | 1.70E-02 | 3.40E-02 | 
 | 4 | 2 | 1 | 1.70E-02 | 4.25E-03 | 8.50E-03 | 
 | 6 | 3 | 1 | 1.70E-02 | 1.89E-03 | 3.78E-03 | 
 | 9 | 4.5 | 1 | 1.70E-02 | 8.40E-04 | 1.68E-03 | 
 | 10 | 5 | 1 | 1.70E-02 | 6.80E-04 | 1.36E-03 | 
 | 16 | 8 | 1 | 1.70E-02 | 2.66E-04 | 5.31E-04 | 
 | 20 | 10 | 1 | 1.70E-02 | 1.70E-04 | 3.40E-04 | 
 | 26 | 13 | 1 | 1.70E-02 | 1.01E-04 | 2.01E-04 | 
 | 36 | 18 | 1 | 1.70E-02 | 5.25E-05 | 1.05E-04 | 
 | Pad Pitch (um) | Total Pad Capacitance (fF) |  |  |  |  | 
 | 1 | 0.0172575 |  |  |  |  | 
 | 2 | 0.06903 |  |  |  |  | 
 | 4 | 0.27612 |  |  |  |  | 
 | 6 | 0.62127 |  |  |  |  | 
 | 9 | 1.3978575 |  |  |  |  | 
 | 10 | 1.72575 |  |  |  |  | 
 | 16 | 4.41792 |  |  |  |  | 
 | 20 | 6.903 |  |  |  |  | 
 | 26 | 11.66607 |  |  |  |  | 
 | 36 | 22.36572 |  |  |  |  | 
 | Pad Pitch (um) | total Pad R (ohm) |  |  |  |  | 
 | 1 | 0.136 |  |  |  |  | 
 | 2 | 0.034 |  |  |  |  | 
 | 4 | 0.0085 |  |  |  |  | 
 | 6 | 0.003777778 |  |  |  |  | 
 | 9 | 0.001679012 |  |  |  |  | 
 | 10 | 0.00136 |  |  |  |  | 
 | 16 | 0.00053125 |  |  |  |  | 
 | 20 | 0.00034 |  |  |  |  | 
 | 26 | 0.000201183 |  |  |  |  | 
 | 36 | 0.000104938 |  |  |  |  | 
 | Pad Pitch (um) | RC Delay (fs) |  |  |  |  | 
 | 1 | 0.00234702 |  |  |  |  | 
 | 2 | 0.00234702 |  |  |  |  | 
 | 4 | 0.00234702 |  |  |  |  | 
 | 6 | 0.00234702 |  |  |  |  | 
 | 9 | 0.00234702 |  |  |  |  | 
 | 10 | 0.00234702 |  |  |  |  | 
 | 16 | 0.00234702 |  |  |  |  | 
 | 20 | 0.00234702 |  |  |  |  | 
 | 26 | 0.00234702 |  |  |  |  | 
 | 36 | 0.00234702 |  |  |  |  | 
Chart: Total Pad Capacitance (fF)
| 1 | 2 | 4 | 6 | 9 | 10 | 16 | 20 | 26 | 36
Total Pad Capacitance (fF) | 0.017257 | 0.06903 | 0.27612 | 0.62127 | 1.3979 | 1.7257 | 4.4179 | 6.903 | 11.6661 | 22.3657
Chart: total Pad R (ohm)
| 1 | 2 | 4 | 6 | 9 | 10 | 16 | 20 | 26 | 36
total Pad R (ohm) | 0.136 | 0.034 | 0.0085 | 0.0037778 | 0.001679 | 0.00136 | 0.00053125 | 0.00034 | 0.00020118 | 0.00010494
Pitch(um)
Cap reduces significantly with Pitch scaling
R increases with Pitch scaling but still lower than 1ohm
Energy/bit reduces significantly (~CV2)
RC delay not limiting (<1fs)
Crude: Excel Math
IMEC Simulations (Partial Calibration)
prashant majhi

## Slide 29: TSV Considerations
TSV 1st/Mid/Last Options [F2F, F2B]
R, L, C as function of Dimensions and Materials
KOZ considerations and its impact on density-loss for base die
Bumpless (only TSV: multi height) option
TSV free: With Tyche as base die
F2F
F2B
F2F-Tyche

## Slide 30: TSV Parasitics: R & C
prashant majhi
 | Resistance (ohm): Cu |  |  | rho | 3.00E-02 | Height (Micron) |  |  |  |  |  |  |  |  |  |  | 
 |  | 2 | 4 | 6 | 8 | 10 | 12 | 14 | 16 | 18 | 20 | 22 | 24 | 26 | 28 | 30 | 50
CD (Micron) | 1 | 7.64E-02 | 1.53E-01 | 2.29E-01 | 3.06E-01 | 3.82E-01 | 4.58E-01 | 5.35E-01 | 6.11E-01 | 6.88E-01 | 7.64E-01 | 8.40E-01 | 9.17E-01 | 9.93E-01 | 1.07E+00 | 1.15E+00 | 1.91E+00
 | 2 | 1.91E-02 | 3.82E-02 | 5.73E-02 | 7.64E-02 | 9.55E-02 | 1.15E-01 | 1.34E-01 | 1.53E-01 | 1.72E-01 | 1.91E-01 | 2.10E-01 | 2.29E-01 | 2.48E-01 | 2.67E-01 | 2.86E-01 | 4.77E-01
 | 3 | 8.49E-03 | 1.70E-02 | 2.55E-02 | 3.40E-02 | 4.24E-02 | 5.09E-02 | 5.94E-02 | 6.79E-02 | 7.64E-02 | 8.49E-02 | 9.34E-02 | 1.02E-01 | 1.10E-01 | 1.19E-01 | 1.27E-01 | 2.12E-01
 | 4 | 4.77E-03 | 9.55E-03 | 1.43E-02 | 1.91E-02 | 2.39E-02 | 2.86E-02 | 3.34E-02 | 3.82E-02 | 4.30E-02 | 4.77E-02 | 5.25E-02 | 5.73E-02 | 6.21E-02 | 6.68E-02 | 7.16E-02 | 1.19E-01
 | 5 | 3.06E-03 | 6.11E-03 | 9.17E-03 | 1.22E-02 | 1.53E-02 | 1.83E-02 | 2.14E-02 | 2.44E-02 | 2.75E-02 | 3.06E-02 | 3.36E-02 | 3.67E-02 | 3.97E-02 | 4.28E-02 | 4.58E-02 | 7.64E-02
 | 6 | 2.12E-03 | 4.24E-03 | 6.37E-03 | 8.49E-03 | 1.06E-02 | 1.27E-02 | 1.49E-02 | 1.70E-02 | 1.91E-02 | 2.12E-02 | 2.33E-02 | 2.55E-02 | 2.76E-02 | 2.97E-02 | 3.18E-02 | 5.31E-02
 | 7 | 1.56E-03 | 3.12E-03 | 4.68E-03 | 6.24E-03 | 7.80E-03 | 9.35E-03 | 1.09E-02 | 1.25E-02 | 1.40E-02 | 1.56E-02 | 1.72E-02 | 1.87E-02 | 2.03E-02 | 2.18E-02 | 2.34E-02 | 3.90E-02
 | 8 | 1.19E-03 | 2.39E-03 | 3.58E-03 | 4.77E-03 | 5.97E-03 | 7.16E-03 | 8.36E-03 | 9.55E-03 | 1.07E-02 | 1.19E-02 | 1.31E-02 | 1.43E-02 | 1.55E-02 | 1.67E-02 | 1.79E-02 | 2.98E-02
 | 9 | 9.43E-04 | 1.89E-03 | 2.83E-03 | 3.77E-03 | 4.72E-03 | 5.66E-03 | 6.60E-03 | 7.55E-03 | 8.49E-03 | 9.43E-03 | 1.04E-02 | 1.13E-02 | 1.23E-02 | 1.32E-02 | 1.41E-02 | 2.36E-02
 | 10 | 7.64E-04 | 1.53E-03 | 2.29E-03 | 3.06E-03 | 3.82E-03 | 4.58E-03 | 5.35E-03 | 6.11E-03 | 6.88E-03 | 7.64E-03 | 8.40E-03 | 9.17E-03 | 9.93E-03 | 1.07E-02 | 1.15E-02 | 1.91E-02
 | Resistance (ohm): W |  |  | rho | 1.00E-01 | Height (Micron) |  |  |  |  |  |  |  |  |  |  | 
 |  | 2 | 4 | 6 | 8 | 10 | 12 | 14 | 16 | 18 | 20 | 22 | 24 | 26 | 28 | 30 | 50
CD (Micron) | 1 | 2.55E-01 | 5.09E-01 | 7.64E-01 | 1.02E+00 | 1.27E+00 | 1.53E+00 | 1.78E+00 | 2.04E+00 | 2.29E+00 | 2.55E+00 | 2.80E+00 | 3.06E+00 | 3.31E+00 | 3.57E+00 | 3.82E+00 | 6.37E+00
 | 2 | 6.37E-02 | 1.27E-01 | 1.91E-01 | 2.55E-01 | 3.18E-01 | 3.82E-01 | 4.46E-01 | 5.09E-01 | 5.73E-01 | 6.37E-01 | 7.00E-01 | 7.64E-01 | 8.28E-01 | 8.91E-01 | 9.55E-01 | 1.59E+00
 | 3 | 2.83E-02 | 5.66E-02 | 8.49E-02 | 1.13E-01 | 1.41E-01 | 1.70E-01 | 1.98E-01 | 2.26E-01 | 2.55E-01 | 2.83E-01 | 3.11E-01 | 3.40E-01 | 3.68E-01 | 3.96E-01 | 4.24E-01 | 7.07E-01
 | 4 | 1.59E-02 | 3.18E-02 | 4.77E-02 | 6.37E-02 | 7.96E-02 | 9.55E-02 | 1.11E-01 | 1.27E-01 | 1.43E-01 | 1.59E-01 | 1.75E-01 | 1.91E-01 | 2.07E-01 | 2.23E-01 | 2.39E-01 | 3.98E-01
 | 5 | 1.02E-02 | 2.04E-02 | 3.06E-02 | 4.07E-02 | 5.09E-02 | 6.11E-02 | 7.13E-02 | 8.15E-02 | 9.17E-02 | 1.02E-01 | 1.12E-01 | 1.22E-01 | 1.32E-01 | 1.43E-01 | 1.53E-01 | 2.55E-01
 | 6 | 7.07E-03 | 1.41E-02 | 2.12E-02 | 2.83E-02 | 3.54E-02 | 4.24E-02 | 4.95E-02 | 5.66E-02 | 6.37E-02 | 7.07E-02 | 7.78E-02 | 8.49E-02 | 9.20E-02 | 9.90E-02 | 1.06E-01 | 1.77E-01
 | 7 | 5.20E-03 | 1.04E-02 | 1.56E-02 | 2.08E-02 | 2.60E-02 | 3.12E-02 | 3.64E-02 | 4.16E-02 | 4.68E-02 | 5.20E-02 | 5.72E-02 | 6.24E-02 | 6.76E-02 | 7.28E-02 | 7.80E-02 | 1.30E-01
 | 8 | 3.98E-03 | 7.96E-03 | 1.19E-02 | 1.59E-02 | 1.99E-02 | 2.39E-02 | 2.79E-02 | 3.18E-02 | 3.58E-02 | 3.98E-02 | 4.38E-02 | 4.77E-02 | 5.17E-02 | 5.57E-02 | 5.97E-02 | 9.95E-02
 | 9 | 3.14E-03 | 6.29E-03 | 9.43E-03 | 1.26E-02 | 1.57E-02 | 1.89E-02 | 2.20E-02 | 2.52E-02 | 2.83E-02 | 3.14E-02 | 3.46E-02 | 3.77E-02 | 4.09E-02 | 4.40E-02 | 4.72E-02 | 7.86E-02
 | 10 | 2.55E-03 | 5.09E-03 | 7.64E-03 | 1.02E-02 | 1.27E-02 | 1.53E-02 | 1.78E-02 | 2.04E-02 | 2.29E-02 | 2.55E-02 | 2.80E-02 | 3.06E-02 | 3.31E-02 | 3.57E-02 | 3.82E-02 | 6.37E-02
Property | Unit | Tungsten | Copper
Bulk Resistivity | uohm.cm | 6 | 1.7
Microscale Resistivity | uohm.cm | 10 | 3
Process |  | CVD/ALD | EP
Process Temp | oC | ~400 | RT
Aspect Ratio Fill | H/CD | ~30 | ~10
CTE [Note Si = 2.6] | ppm.K-1 | 4.6 | 17
Barrier/Liner |  | TiN | TaN/Cu Seed
Thermal Stability |  | good | poor
Electro Migration |  | good | ok
Melting Point | oK | 6000 | 2000
TSV resistance low [compared to MEOL] even for W (lower for Cu)
TSV Resistance not limiter – need to analyze for Reliability

## Slide 31: TSV Parasitics: R & C
 | TSV |  | insulation thk (um) |  | 0.2 |  |  |  |  |  |  |  |  |  |  |  | 
 | Capacitance (fF) |  |  |  |  | Height (Micron) |  |  |  |  |  |  |  |  |  |  | 
 |  | 2 | 4 | 6 | 8 | 10 | 12 | 14 | 16 | 18 | 20 | 22 | 24 | 26 | 28 | 30 | 50
CD (Micron) | 1 | 0.3 | 0.5 | 0.8 | 1.1 | 1.4 | 1.6 | 1.9 | 2.2 | 2.4 | 2.7 | 3.0 | 3.3 | 3.5 | 3.8 | 4.1 | 6.8
 | 2 | 1.1 | 2.2 | 3.3 | 4.3 | 5.4 | 6.5 | 7.6 | 8.7 | 9.8 | 10.8 | 11.9 | 13.0 | 14.1 | 15.2 | 16.3 | 27.1
 | 3 | 2.4 | 4.9 | 7.3 | 9.8 | 12.2 | 14.6 | 17.1 | 19.5 | 22.0 | 24.4 | 26.8 | 29.3 | 31.7 | 34.2 | 36.6 | 61.0
 | 4 | 4.3 | 8.7 | 13.0 | 17.3 | 21.7 | 26.0 | 30.4 | 34.7 | 39.0 | 43.4 | 47.7 | 52.0 | 56.4 | 60.7 | 65.1 | 108.4
 | 5 | 6.8 | 13.6 | 20.3 | 27.1 | 33.9 | 40.7 | 47.4 | 54.2 | 61.0 | 67.8 | 74.5 | 81.3 | 88.1 | 94.9 | 101.7 | 169.4
 | 6 | 9.8 | 19.5 | 29.3 | 39.0 | 48.8 | 58.6 | 68.3 | 78.1 | 87.8 | 97.6 | 107.3 | 117.1 | 126.9 | 136.6 | 146.4 | 244.0
 | 7 | 13.3 | 26.6 | 39.8 | 53.1 | 66.4 | 79.7 | 93.0 | 106.3 | 119.5 | 132.8 | 146.1 | 159.4 | 172.7 | 186.0 | 199.2 | 332.1
 | 8 | 17.3 | 34.7 | 52.0 | 69.4 | 86.7 | 104.1 | 121.4 | 138.8 | 156.1 | 173.5 | 190.8 | 208.2 | 225.5 | 242.9 | 260.2 | 433.7
 | 9 | 22.0 | 43.9 | 65.9 | 87.8 | 109.8 | 131.7 | 153.7 | 175.7 | 197.6 | 219.6 | 241.5 | 263.5 | 285.4 | 307.4 | 329.4 | 548.9
 | 10 | 27.1 | 54.2 | 81.3 | 108.4 | 135.5 | 162.6 | 189.8 | 216.9 | 244.0 | 271.1 | 298.2 | 325.3 | 352.4 | 379.5 | 406.6 | 677.7
prashant majhi
TSV Capacitance dependent on dimensions (and insulator thickness) and can get high
TSV Capacitance can be limiter/decider

## Slide 32: TSV Considerations
TSV 1st/Mid/Last Options [F2F, F2B]
R, L, C as function of Dimensions and Materials
KOZ considerations and its impact on density-loss for base die
  WIP in progress to quantify KOZ… but for now assume KOZ ~ TSV CD [IMEC recommendation]
Bumpless (only TSV: multi height) option
TSV free: With Tyche as base die

## Slide 33: Closer Look at TSV Connection Options
TSV @ M7 of Base
TSV @ M1 of Base

## Slide 34: How can elements of 3DIC decision matrix help?
Case studies:
  BZM:
    Logic+Logic
    WoW or CoW?; F2F or F2B?; TSV-free with BS-PDN?;
  COR:
    3D: SRAM+XPU; DRAM+SoC;
    2.xD: XPU stack with I/O Hub
    WoW or CoW?; F2F or F2B?; TSV-free with BS-PDN?;
  Networking Chip: Flatrock (Tofino 4+)
    Logic(HP)+SRAM(&LP logic)
    WoW or CoW?; F2F or F2B?;
  3DIC for MIM+XPU/GPU [Power Integrity]: DG case
    Monolithic –vs- 3DIC DTC/ISC
    WoW or CoW?;
  CCG-LCH ECF: Logic to NVM
    2.xD Logic to NVM (MRAM)
    3D Logic to NVM (NOR)
  3D-NAND:
    CMOS + Array
    New considerations with CoW