## Slide 1: A Survey of Cross Point Phase Change Memory Technologies
DerChang Kau
Intel Corporation
Santa Clara, CA
Sematech International Symposium on Advanced Gate Stack Technology
Sep/30/2010
Hilton Garden Inn, Troy, NY

## Slide 2: Outline
Overview and Motive
  Storage Elements
  Selector Elements
  Why thin film based Cross Point Array
Cross Point Phase Change Memory Array
  Thin film two-terminal switches
  Array operations
PCMS in Computing Memory Hierarchy
  PCMS characteristics
  Performance benchmark
Summary

## Slide 3: Outline
Overview and Motive
  Storage Elements
  Selector Elements
  Why thin film based Cross Point Array
Cross Point Phase Change Memory Array
  Thin film two-terminal switches
  Array operations
PCMS in Computing Memory Hierarchy
  PCMS characteristics
  Performance benchmark
Summary

## Slide 4: Storage Element
Simple resistor 1-D steady state approximation:
Fourier’s Law .
Ohm’s Law .
+ Continuity Equation .
Line Position , nm
Temp, K
Martijn Lankhorst, et.al., Nature materials, 2005
Structure
Material

## Slide 5: Structure Engineering
A. Schrott, et.al., VLSI-TSA, 2007
C. Jeong, et.al., JJAP, 2006
G. Servalli, IEDM 2009
Chung Lam, LETI Workshop on MT, 2009
Critical Area = [a•l]2
l: Technology half pitch
a: Sub-lithographic technique required
by the pairing selector

## Slide 6: Phase Change Material Engineering
SET Energy-Bandwidth
Retention and Disturb
G. Bruns, et.al., APL July, 2009
Nanosecond switching in GeTe
T. Morikawa, et.al, iedm 2007,
Good Data Retention in In-Ge-Te

## Slide 7: Heater, Electrode and Interface
Heater vs. Self-heat
Thermal Boundary Resistance and Electrical Interface Barrier
Reset temperature along center axis with (solid line) and without (dotted line) interfaces
David Kencke, et.al., IEDM 2007, The Role of Interfaces in PCM

## Slide 8: Vertically Integrated PCM
Top electrode
Bottom
electrode
Chalcogenide
Y. Chen, et. al.,
IEDM ’03, S37P4
Y.N. Hwang, et. al.,
VLSI ’03, T12B3
F. Pellizzer, et. al.,
VLSI ’06, T15P3
J.H. Oh, et. al.,
IEDM ’06, S2P6
Y. Sasago, et. al.,
VLSI, ’09. T2B-1
Bottom Electrode
PCM
Middle Electrode
OTS
Top Electrode
Column
D. Kau, et. al.,
IEDM ’09. S27.1

## Slide 9: Why thin film Cross Point PCM Architecture
True Cross Point Array
  Cell dimension: 4 l2
  Strapless to simplify routing and process
Stackable
  Low temperature process
  CMOS under the memory
  Compatible with mainstream backend process
  Multiple decks feasible
Bitline
Wordline
Wordlines
Bitlines

## Slide 10: Outline
Overview and Motive
  Storage Elements
  Selector Elements
  Why thin film based Cross Point Array
Cross Point Phase Change Memory Array
  Thin film two-terminal switches
  Array operations
PCMS in Computing Memory Hierarchy
  PCMS characteristics
  Performance benchmark
Summary

## Slide 11: “A Survey of Semiconductor Devices”
Diode: two terminals and exhibiting a nonlinear I-V (IEEE Standard Dictionary)
Kowk Ng, TED Oct., ’96 p1760
Rectifiers
N-Shape
S-Shape
Transient
Kwok Ng, IEEE EDS Distinguished Lecture
SCV Chapter, 11/7/05

## Slide 12: Thin Film Diode Candidates for Cross Point PCM
Y. Sasago, et. al.,
VLSI ’09. T2B-1
Bottom Electrode
PCM
Middle Electrode
OTS
Top Electrode
Column
D. Kau, et. al.,
IEDM ’09. S27.1
K. Gopalakrishnan, et. al.,
VLSI ’10. TS19.41
M. Lee, et.al.,
IEDM ‘07, S30.2
W Y Park, et.al., Nanotechnology 21 (2010) 195201

## Slide 13: I-V Phenomenology
Poly Junction | Oxide Junction | Oxide Rectifier | MIEC | OTS
Si PN junction | Ox PN junction | Pt/TiO2/Ti | Cu+ in SE | Chalcogenide
Minority carrier; drift + diffusion | Minority carrier; drift + diffusion | Schottky barrier + Filamentary | Schottky barrier modulated by Ionic motion. | Ovonic Threshold Switching
Sub nsec | 10 to 100 nsec* | Forming/dissolving required ? | ~100ns forming ~200ns dissolving | nsec switching & recovery
Unidirectional | Unidirectional | Unidirectional | Bidirectional | Bidirectional
< 10MA/cm2 | < 0.1MA/cm2 | < 1MA/cm2 | 50MA/cm2 | Match PCM
Y. Sasago, et. al., VLSI ’09. T2B-1 | M. Lee, et.al., IEDM ‘07, S30.2 | W. Park, et.al., Nanotechnology ’10 | K. Gopalakrishnan, et. al., VLSI ’10. TS19.41 | D. Kau, et. al., IEDM ’09. S27.1
*: Huang et.al., Sci. in China, Physics, Mechanics & Astronomy 2005 Vol.48 No.3 pp.381--384

## Slide 14: Advances in Thin Film Switches Beyond “Traditional Rectifier”
Competency – Semiconductor fabrication maturity improves device reproducibility and cumulative learning
Challenge – The switching transient such as filamentation requires proper DUT design using non-equilibrium characterization technique .
Novelty – The physics of resistive switching mechanisms fuel innovations on the new classes of selectors

## Slide 15: Cross Point Array Operations: Access
Unidirectional Rectifier
A rectifying selector turns on one bit with forward bias and isolates others with reverse bias.
Bidirectional Switch
Subject to the potential drop at each cross points, the selected bit is triggered and the unselected bits are blocked.
…
…
Vaccess
0
Vaccess
0
…
…
Vaccess
0
½ Vaccess
½ Vacces

## Slide 16: Reading a PCM in Cross Point Array
To interrogate PCM state, PN diode or MIEC is turned ON to sense the current
With a S-Shape Selector like OTS, threshold demarcation is used for Read
MLC is perceived easier with a non-NDR selector; however, variability of bias points needs to be carefully controlled due to superlinear I-V characteristics
Demarcation Read with a S-Shape Cell is inherently faster due to NDR
VDM
PCM IV; 4 levels programmed
PCMS IV

## Slide 17: Writing a PCM in Cross Point Array
Sub-lithographic features have been deployed to reduce IRESET
  Manufacturing latitude of those innovations becomes increasingly restricted as technology scales.
  IRESET is converging with various device structures
Areas of focus:
  Electrical interface and thermal boundary properties such as cell confinement and architecture
  SET Kinetics in Nano-geometry for energy efficiency
  PCM’s high speed vitrification capability must not be hindered by the thin-film selector in series.
  Selector and electrodes becomes the liability to endurance as RESET current density increases.

## Slide 18: Array Parasitics
The parasitic R and C consume operating energy.
Displacement current during access is dissipated mostly on the intra layer capacitance and decoding circuit
Array consumes leakage power when unselected cells are biased
 | Unidirectional Rectifier |  |  | Bidirectional Switch |  | 
 | Sel. WL | Sel. BL | DeSel Cells | Sel. WL | Sel. BL | DeSel Cells
# of Cell | C-1 | R-1 | (C-1)•(R-1) | C-1 | R-1 | (C-1)•(R-1)
Switching | 0 | 1 col | (R-1) rows | 1 row | 1 col | 0
leakage | 0 | 0 | (C-1)•(R-1) | C-1 | R-1 | 0
Example: Single deck Cross Point PCM array with “C” bit-lines and “R” word-lines

## Slide 19: Outline
Overview and Motive
  Storage Elements
  Selector Elements
  Why thin film based Cross Point Array
Cross Point Phase Change Memory Array
  Thin film two-terminal switches
  Array operations
PCMS in Computing Memory Hierarchy
  PCMS characteristics
  Performance benchmark
Summary

## Slide 20: State of the Art Computing Memory Hierarchy
Imperatives on cost vs. performance in memory subsystem
  performance increases as it moves closer to processors
  Capacity of each subsequent level increases by roughly one order
Challenges to a disruptive innovation between NAND & DRAM
  DRAM latency will be sustained and throughput will improve.
  NAND will maintain or improve performance with cost leadership
Memory Subsystem | Normalized Parameters |  | 
 | Cost | Thruput | Latency
On-chip SRAM | > 10 | > 10 | < 0.01
Component DRAM | 1 | 1 | 1
SSD NAND | 0.1 | 0.1 | 1,000
Form factor HDD | < 0.01 | < 0.01 | > 100,000

## Slide 21: PCMS Array Construction
M2
M1
Poly
D. Kau, et.al.,
IEDM ’09, S27.1

## Slide 22: PCM vs. PCMS
OTS improves PCM RESET effectiveness
DOE Split:
with vs. without OTS

## Slide 23: PCMS Cross Point Array RESET Speed
High speed RESET capability is validated with Cross Point Array

## Slide 24: PCMS Array Cycling Endurance
Degradation tails (3.5σ) developed after
1 million S/R cycles.

## Slide 25: Program Distribution
A good candidate for high density components

## Slide 26: Benchmark of Computing Memory
34nm NAND vs. DDR3 DRAM vs. projected 34nm PCMS
Memory |  | NAND | PCMS | DRAM
Normalized Cost |  | 0.1 | 0.1 | 1
Normalized Bandwidth | READ | 1 | 1 | 1
 | RESET | 0.05 | 0.5 | 
 | SET | > 10 | 0.1 | 
Normalized Latency | READ | 1K | 1 | 1
 | RESET | 20K | 3~5 | 
 | SET | 60K | 10 | 
Endurances (cycles) |  | 10K | > 1M | >1E15
Disturb (cycles) |  | 10K | > 1E12 | N/A

## Slide 27: Summary
Thin film PCM Cross Point Arrays possess cost advantages
  “Cross Point” means 4 l2 / Cell for each deck of memory
  “Thin film” enables multi-deck to amortize cell size.
  “Thin-film-Cross-Point” array is stackable over CMOS to reduce die size
The Physics on resistive switching fuel innovations on thin-film diodes
  OTS is a strong contender among all the thin film diodes;
  It’s a bidirectional threshold switching element to isolate PCM cell;
  it scales with PCM, physically, chemically & electrically
Cross Point PCMS Array demonstrates
  Near DRAM performance with good NVM reliability
  Cost comparable to NAND
PCMS fits well between NAND & DRAM in computing memory hierarchy

## Slide 28: Acknowledgement
I would like to thank to Intel NVM team for helpful discussions
I would also like to acknowledge the authors of the literature referred here