## Slide 1: Emerging Memory: Competitive Landscape
Prashant Majhi, Derchang Kau, Al Fazio

## Slide 2: Exec Summary
Emerging memories positioned as scaling option for SRAM, DRAM, SCM and NAND
  Critical challenges (variability) in filamentary RRAM/CBRAM limiting its potential for high density NVM
  Significant R&D on Cross-Point based alternative memories for Storage Class Memory
Emerging memory gaining traction for embedded NVM and ML/AI applications
INTEL CONFIDENTIAL

## Slide 3
Resistance Change ReRAM[1D, 2D], PCM [3D]
Ferroelectrics
(FeRAM, FeFET)
3D SRAM (monolithic)
3D DRAM (monolithic)
DNA inspired (Archival memory)
Magnetic
[MRAM, STT(SOT)MRAM]
Memory Products Landscape and R&D
Emerging Memory R&D
Sources: Publications from Industry, Academia and Consortia R&D
Cost, Capacity or Density, Retention
Speed, Bandwidth, Endurance
SRAM
DRAM
Storage Class Memory
NAND
HDD
Intel 3D NAND
Intel 3D Cross-point
Samsung 1x nm DRAM
Intel 14nm SRAM
Mature R&D and early HVM
Early R&D
Concept Stage
INTEL CONFIDENTIAL

## Slide 4
Resistance Change ReRAM[1D, 2D], PCM [3D]
Ferroelectrics
(FeRAM, FeFET)
3D SRAM (monolithic)
3D DRAM (monolithic)
DNA inspired (Archival memory)
Magnetic
[MRAM, STT(SOT)MRAM]
Memory Products Landscape and R&D
Emerging Memory R&D
Sources: Publications from Industry, Academia and Consortia R&D
Cost, Capacity or Density, Retention
Speed, Bandwidth, Endurance
SRAM
DRAM
Storage Class Memory
NAND
HDD
Intel 3D NAND
Intel 3D Cross-point
Samsung 1x nm DRAM
Intel 14nm SRAM
Mature R&D and early HVM
Early R&D
Concept Stage
INTEL CONFIDENTIAL

## Slide 5: SRAM Scaling Slows.. Opportunity for Emerging Memory?
Ann Steegen, ITF 2017/18
SRAM Scaling Increasingly Challenging
Novel 3D architecture such as CFET enable scaling
STT/SOT-MRAM in research for LLC [challenge: scaling and reliability]
INTEL CONFIDENTIAL

## Slide 6
DRAM Scaling Also Slowing…
Opportunity for Emerging Memory?
ICInsights
1Y
1z
INTEL CONFIDENTIAL

## Slide 7: DRAM Scaling Options
Transistor Innovations
Vertical transistor (4f2)
Low leakage non-Si TFT
Capacitor Innovations
Cylinder to pillar
Higher K (perovskite?)
Ferroelectrics?
Periphery Innovations
Fin w/ HKMG
Structure Innovations
2D to 3D stacked (inc MRAM)
Note: Startups like TC labs (Thyristor based 3D) and Nantero (CNT based XP with 3D) also targeting DRAM
Sources: ITF, Various Publications and Press Releases
INTEL CONFIDENTIAL

## Slide 8: DRAM/SRAM Going 3D (Adv Packaging)
Tokyo Ins Tech, IMW 2019
Product Landscape
3D Bumpless Value Proposition
Bumpless Bonding Technology Readiness
INTEL CONFIDENTIAL

## Slide 9
Resistance Change (RRAM)
Ferroelectrics (FeRAM, FeFET)
3D SRAM (monolithic)
3D DRAM (monolithic)
DNA inspired (Archival memory)
Magnetic (MRAM, STTRAM)
Memory Products Landscape and R&D
Emerging Memory R&D
Sources: Publications from Industry, Academia and Consortia R&D
Cost, Capacity or Density, Retention
Speed, Bandwidth, Endurance
SRAM
DRAM
Storage Class Memory
NAND
HDD
Intel 3D NAND
Intel 3D Cross-point
Samsung 1x nm DRAM
Intel 14nm SRAM
Mature R&D and early HVM
Early R&D
Concept Stage
INTEL CONFIDENTIAL

## Slide 10: Emerging Memory (3D RRAM) for Beyond 3D NAND?
Samsung, International Workshop of Innovative Memory 2013
Samsung, IEDM, 2011

## Slide 11: RRAM has Long History (Including Promises)
Samsung IEDM 2004
Samsung, IEDM, 2011
Several announcements, but no major high density NVM product …. yet

## Slide 12: Operation & Characteristics of Filamentary RRAM
1
2
3
Oxide RRAM Cell (Filamentary): Typical Operation
Need Sub-Stoichiometric Oxide
Forming (soft-breakdown) and First RESET very critical
Switching motion of Oxygen Vacancy and Redox
Oxygen vacancies
V
I
(B)
(C)
(F)
(G)
(I)
V(forming)
V(SET)
V(RESET..Stop)
I(Compliance)
I(RESET….start)
I(RESET … stop)
I(SET…..stop)
I(SET…..start)
V(Read)
I(read-ON)
I(read-OFF)
V(RESET..Start)
(D), (J)
(A), (E), (H)
1
2
3
INTEL CONFIDENTIAL

## Slide 13
Ireset (max) variation
LRS variation
V(set) variation
HRS variation
Significant Variability at Low Currents (Stochastic)
Note: Variability/Instability in RRAM more critical in 1S1R [cross-point architecture]
Operation & Characteristics of Filamentary RRAM
IMEC, IMW 2013
INTEL CONFIDENTIAL

## Slide 14: 3D NAND Scaling Continues …. Scope for Emerging Memory?
Continued Bit Density Growth [2D => 3D ….]
Source: Techinsights
INTEL CONFIDENTIAL

## Slide 15: Emerging Memory for Beyond 3D NAND?
Not Many Recent Publications Positioning 3D RRAM for Beyond 3D NAND Scaling
INTEL CONFIDENTIAL

## Slide 16: Emerging Memories for SCM in 3D XP Architectures
Key Challenge: Appropriate Memory+Selector Combination
Cost, Capacity or Density, Retention
Speed, Bandwidth, Endurance
SRAM
DRAM
Storage Class Memory
NAND
HDD
Intel 3D Cross-point
Resistance Change ReRAM[1D, 2D], PCM [3D]
Ferroelectrics
Magnetic
[MRAM, STT(SOT)MRAM]
Volatile filament
Ovonic Threshold
Thermionic
[diode, MIEC, ..]
Metal-Insulator Transition
INTEL CONFIDENTIAL

## Slide 17: Many Industry Players Pursuing 3D XP Options (Select Examples of RRAM and OTS+PCM Based)
Company | Memory Type | Memory Mechanism | Pros | Cons?* | R&D Effort
Sandisk/WD/Unity/Rambus/4DS | 1R (filament / interfacial) | (Non) linear RRAM | Stackable 4f2; 3D RRAM (Selector-less) | Variability(stochastic); High R at scale | University Collab and internal R&D; Limited Array Demo
Hynix/HP | 1S1R | SiOx(S)/ ox-RRAM NbOx Selector | 3D RRAM; Scaled (filament) | Variability(stochastic); RRAM compatibility | Internal R&D; Array demo
Crossbar/SMIC | 1T-nR; 1S1R | Oxide (S) | Stackable 4f2; High NL; FAAST selector | Disturb; Variability; Integration Compatibility | Internal R&D; Array demo
Sony / Micron | 1T1R => 1S1R | OTS(s)+CBRAM | Stackable 4f2; High NL; | Complex integration for Cu; Disturb; Variability; | Internal R&D; device Level
Nantero | 1T-1R; 1R | CNT based RRAM | Selector-less 4F2; High Speed; | Low NL; Inhibit / Disturb; Variability; | Univ and Internal R&D; Limited Array Demo
* Perception based on understanding of memory switching mechanism and published data
Company | Memory Type | Memory Mechanism | Pros | Cons?* | R&D Effort
IBM / Macronix | 1T1R => 1S1R | OTS+PCM | 3D stackable; Engineering composition for thermal stability | Limited operating window (Variability?) | Internal R&D; Small array demo
Hynix | 1S1R | OTS + PCM | 3D stackable; Engineering composition for RW | TBD | Internal R&D; Array demo
IMEC/ CEA-LETI | 1S1R 3DXP | OTS+PCM | 3D stackable; Binary alloys based OTS Selectors | Limited operating window (Variability?) | Internal R&D; device level
Multiple Univ | 3DXP | OTS + PCM | Materials engineering for Scalability, Reliability, Extendability | No array data | Device Level
RRAM
OTS + PCM
INTEL CONFIDENTIAL

## Slide 18: HP-Hynix-Sandisk/WD Memristor/RRAM Timeline
2012
2014
2016
HP JDP with Hynix .. For 2013 product!
Academic collaborations on 1T1R /1R1r on TiOx, AlOx
HP Hynix IEDM 2015 on Cross-Point 1S1R with NbO2 selector [2x nm]
HP Hynix VLSI 2014 on NbO2 selector for cross-point [5x nm]
HP signs JDP with Sandisk for RRAM based SCM
Sandisk  Western Digital;
HP continues JDP with WD;
WD has JDP with 4DS (2014+) and signs on Rambus (March 17) .. Interfacial RRAM approach?
2018
WD indicated, no future for NbO2 selector (Stanford RRAM workshop)
Hynix SiOx (As doped) Selector with RRAM for 4F2 (IEDM/VLSI)
Unity => Rambus CMOx
INTEL CONFIDENTIAL

## Slide 19: Hynix/HP on Cross Point 4F2 with 1S1R
IEDM 2015
IEDM 2017

## Slide 20: CrossBar: 1T1R and 1T nR [1S1R]
FMS, 2017

## Slide 21: Sony Micron on CBRAM
IEDM 2017, IMW 2018’2019
Sony Cross-Point 1S1R (OTS + CBRAM)
Sony Micron 1T1R (CBRAM)
VLSI, IEDM, ISSCC (’14-’17)

## Slide 22: Nantero: Nanotube Based RRAM
2012
2014
2016
2018
Nantero-IMEC JDP
(demonstrate on scaled structures)
Nantero claims several engagements (license agreements?) with foundries
Nanotechnology 2018

## Slide 23: IBM Macronix JDP on PCM Based NVM
Started with PCM for Auto
Moved to 3D XP for Storage Class Memory
2012-2015
2016 +
IEDM 2018; VLSI 2019

## Slide 24: SK-Hynix @ IEDM 2018  128Gb 3D XP (OTS + PCM)
IEDM 2018

## Slide 25: IMEC and CEA LETI: OTS for 3D XP
IMW 2019
VLSI 2017
VLSI 2017
IMEC
CEA-LETI

## Slide 26: IMEC R&D on 3D XP with OTS + PCM

## Slide 27: Academic R&D on 3D XP Based on OTS
ASU, 2019
Academic consortium,
Chinese Academy of Sciences
Univ of Grenoble,
MINATECH, France
POSTECH, SK Hynix, Korea
2019 Electron Devices Technology and Manufacturing Conference (EDTM)
HU, NTU 2019

## Slide 28: Many Industry Players Pursuing 3D XP Options (Examples of Non-RRAM Memories)
Company | Memory Type | Memory Mechanism | Pros | Cons?* | R&D Effort
Avalanche | 1S-1MRAM | MRAM with Threshold Selector | Stackable 4f2 ; High NL; Lo Ioff; | Disturb; Operating Window (Variability); | Internal R&D; limited array demo
Namlab/Global Foundries | FeFET | HfO2 based FerroFET | High Speed + Low voltage; CMOS compatible | Variability; Endurance; | Univ and Internal R&D; device level
IMEC 3D FeFET | 3D FeFET | HfO2 based FerroFET | High Density 3D NAND like; BE ALD process; | Variability; High Op Voltage; Endurance | Internal R&D; device level
Toshiba | 1FTJ | HfO2 based Ferro tunnel junction | Selector-less; 3D Stackable | Low NL; Variability | Internal R&D; device level
Kilopass / TC Labs | Thyristor (3D) | Vertical thyristor | 3D stackable; high speed; | Epi for abrupt junctions; | Internal R&D; mostly simulations
Sunrise | 3D NOR | NOR | --- | --- | 
Micron/Intel | 1X | Self Select Memory | --- | --- | Internal R&D
MRAM Based
Ferroelectric Based
T-RAM
* Perception based on understanding of memory switching mechanism and published data
INTEL CONFIDENTIAL
NOR

## Slide 29: Avalanche [1S(oxide)-1MRAM]
IEDM 2017

## Slide 30: Namlab /CNT/ Globalfoundries on HfO2 FeFET
CNT, IMW 2019
The Promise of Scalability
Demonstration at Scaled Node (28nm)
Multi-Domains?
GF, IEDM VLSI (2013-2017)

## Slide 31: Ferroelectric Memory Company: HfO2 FeFET

## Slide 32: Variability: Significant Challenge for Scaled FeFETs
Prof. S. Datta group (ND), VLSI 2019
Sayan, NIST, 2005
(Ferro)

## Slide 33
IMEC Positioning 3D FeFET for High Density NVM
ITF 2018 and IEDM 2018

## Slide 34: Toshiba Ferro-Tunnel-Junction (FTJ)
Improved FTJ from prior work (VLSI’16) by using template layer
NL is still somewhat limited
Claim good variability and scalability, but no data, especially on arrays
Toshiba (VLSI 2016): FTJ for High Density 3D Compatible NVM
Toshiba (SSDM’18): Performance Enhancement by
Template Induced Crystallization FTJ for 4F2

## Slide 35: TC Labs : Vertical (Stackable) Thyristor
TC Labs Confidential, shared with Intel under CNDA

## Slide 36: Exec Summary
Emerging memories positioned as scaling option for SRAM, DRAM, SCM and NAND
  Critical challenges (such as variability/instability) in filamentary RRAM/CBRAM limiting its potential for high density NVM
  Significant R&D on cross-point based alternative memories for Storage Class Memory
  Need focused effort on critical challenges for emerging memory to transition from R&D to HVM
INTEL CONFIDENTIAL

## Slide 37: Other Opportunities for Emerging Memory : eNVM, Machine Learning/AI/Neuromorphic Computing
Ann Steegen, ITF 2018
e-NVM
(e-FLASH)
Stanford/MIT: ERI 2018
3D SoC for Machine Learning
Feb 2019, ~ $2B investment

## Slide 38: Emerging e-NVM: Industry Landscape -Slow/Steady Progress towards HVM, but primarily for low density e-FLASH replacement
HVM
Development
Research
STTRAM
PCM
FeRAM
RRAM
CBRAM
TFT based
eFLASH
180
130
90
60
40
28
16
Technology Node (nm)
(Fujitsu 4Mb)
Renesas, 2016
Renesas, TSMC,
Samsung
Renesas, IEDM’16
Everspin, 2015-16
Samsung, TSMC, GF [2019?]
Panasonic, 2013
Panasonic, 2019?
Adesto, 2013-16
Adesto, 2019?
Adesto, Sony
Micron, Samsung, 2014
IBM, Macronix, STMicro
Panasonic, TI, Ramtron, Cypress
GF, Namlab
SEL-UMC
SEL-xyz?
Panasonic;TSMC [2019?]
Everspin, 2019
Sources: Various Publications and Press Releases
INTEL CONFIDENTIAL

## Slide 39: Dynamic Supply Chain for Memory R&D

## Slide 40: Emerging Memory on Gartner Hype Cycle
HfO2 based Ferroelectrics
RRAM/CBRAM for high density NVM
Emerging memory for AI/Neuromorphic
OTS + PCM for 3D XP SCM
STTRAM / RRAM for e-NVM
STTRAM/RRAM for DRAM/SRAM
Closely Monitoring Innovation/Breakthrough’s in Eco-System to Separate Myth/Hype from Reality
* Perception based on published data
INTEL CONFIDENTIAL

## Slide 41: Exec Summary
Emerging memories positioned as scaling option for SRAM, DRAM, SCM and NAND
  Critical challenges (such as variability/instability) in filamentary RRAM/CBRAM limiting its potential for high density NVM
  Significant R&D on cross-point based alternative memories for Storage Class Memory
  Need focused effort on critical challenges for emerging memory to transition from R&D to HVM
Emerging memory gaining traction for embedded NVM and ML/AI applications
INTEL CONFIDENTIAL