## Slide 1: Threshold Switching Phenomenology & Mechanisms
Mechanism | Thermionic | Filamentation | Tunneling | MIEC | MIT | OTS
Construct. | P-N or M-S Jx | Ion (Ag+) in Ox | MIM | Cu+ in SE | NbO2 | Chalcogenide
Switching | Electronic | Atomistic | Electronic | Atomistic | Atomic | Electronic
Polarity | Unidirectional | Bidirectional | Bidirectional | Bidirectional | Bidirectional | Bidirectional
tswitch | sub nsec | ns ~ 100s ns | ps or faster | ns ~ 100s ns | ns to 10s ns | sub ns
JON | < 10MA/cm2 | 1-10MA/cm2 | < 1MA/cm2 | >10MA/cm2 | > 10MA/cm2 | > 10MA/cm2
JOFF | <1A/cm2 | <1KA/cm2 | <1KA/cm2 | <1KA/cm2 | <1KA/cm2 | <1KA/cm2
Vpeak | < 3V | < 1V | <3V | < 1V | < 3V | < 3V
I-V |  |  |  |  |  | 
Reference | Y. Sasago, et. al., VLSI ’09 | J. Yang, et.al., Adv Func Mtls (2018) | B. ﻿Govoreanu, et.al., IEDM’13. P10.2 | K. Gopalakrishnan, et.al., VLSI Symposium ’10. | X. Liu et.al., EDL Oct.’14 | S. Yasuda, et.al., VLSI symposium, ‘17,