## Slide 1: The Pursuit of Atomistic Switching and Cross Point Memory
DerChang Kau
Intel Corporation
2021 International Symposium on VLSI Technology, System and Application
April 19-22, 2021, Hsinchu, Taiwan

## Slide 2: Outline
Introduction
Problem Statement and Solution Space
Cross Point Memory Array and Choices of Selector
3D XPoint Memory Technology
Conclusion

## Slide 3: Outline
Introduction
Problem Statement and Solution Space
Cross Point Memory Array and Choices of Selector
3D XPoint Memory Technology
Conclusion

## Slide 4: Computer Architecture 101: Hierarchy of Memory each has greater capacity than the preceding but less quickly accessible
Introduction
“The Memory Organ – Ideally one would desire an indefinitely large memory capacity such that any particular … word would be immediately … available. … It does not seem possible physically to achieve such a capacity. …We are therefore forced to recognize the possibility of constructing a hierarchy of memories, each of which has greater capacity than the preceding but which is less quickly accessible.”
Preliminary Discussion of the Logical Design of an Electronic Computing Instrument
Arthur Burks, Herman Goldstine and John von Neumann, June/28/1946
Cache
Primary Storage
Secondary Storage and Archive
Main Memory
Bandwidth, Cost
Capacity, Latency

## Slide 5: Cache and Main Memory Scaling SRAM and DRAM scaling have significantly slowed
Introduction
A. Fazio, “Advanced Technology and Systems of Cross Point Memory”, IEDM 2020, S24.1

## Slide 6: Storage Scaling – Flash based Solid State Drive displaces Hard Disk Drive* 3D NAND warrants Cost scaling superiority for path ahead
Introduction
*: Intel Ships Enterprise-Class Solid-State Drives https://www.intel.com/pressroom/archive/releases/2008/20081015comp.htm

## Slide 7: Outline
Introduction
Problem Statement and Solution Space
Cross Point Memory Array and Choices of Selector
3D XPoint Memory Technology
Conclusion

## Slide 8: Storage hardly improves bandwidth without adding capacity
Problem Statement
While capacity has grown for NAND, performance – write performance and in particular as more bits per cell are added – has not kept up with capacity growth.
BW/Capacity scaling critical, as BW goals often solved by brute force (parallel die)  cost barriers to adoption, amplifies scaling challenges.
Source: various IEEE, ISSCC, IEDM, and IMW papers.
Notes: Use Al’s paper reference

## Slide 9: The anticipated solution to bridge the gap
Solution Proposal
von Neumann architecture gave away the answer long ago –
    large memory capacity
    word
    immediately available
      Cross Point Memory is a promising scalable solution
Simple scalable structure + 3D technology  Large Memory Capacity
Individual Cell Access  Word (small granularity accessible)
Fast switching materials + local low resistance metal interconnect  Immediately Available
Challenge: Mating a selector device with non-linear I-V & a memory element with tight distribution

## Slide 10: Outline
Introduction
Problem Statement and Solution Space
Cross Point Memory Array and Choices of Selector
3D XPoint Memory Technology
Conclusion

## Slide 11: Cross Point Memory Array – ½ voltage biased scheme
The selected bit (•) is at the cross point of the selected bitline (BL) and wordline (WL)
Functionality –
A fully networked x-y resistive array  Sneak paths thru all de-selected cells (•) connect the selected BL/WL
Reliability –
All bits on selected BL (•) and selected WL (•) are biased  Read/Write disturbance and retention
A selector isolates memory cells in an array, improves access accuracy and strengthens reliability.
Cross Point Memory Array

## Slide 12: Selector of a cross-point memory cell is a diode
Diode: two terminals and exhibiting a nonlinear I-V, IEEE Standard Dictionary of Electrical and Electronics Terms, 1980
§ : Kowk K. Ng, Complete guide to semiconductor devices, 2nd ed., 2002 ¶ :https://www.digikey.com/en/articles/design-in-tvs-diode-protection-enhance-can-bus-reliability
Unidirectional
Asymmetric
Unipolar
Bidirectional
Symmetric Ambipolar

## Slide 13: Random Access of a Memory in Cross Point Array
Unidirectional L-Shape Selector
Bidirectional S-Shape Selector
A rectifying selector turns on one bit with forward bias and isolates others with reverse bias.
Selected BL/WL are toggled between 0V and V
All bits but selected WL/BL are reversed biased
Subject to Vdrop at each cross points, the selected bit is triggered, and the unselected bits are blocked.
Selected BL/WL are toggled between 0V and ±V
All bits but selected WL/BL are 0 biased
Cross Point Memory Array

## Slide 14: Thin Film Diode Candidates for Cross Point Memory
Selector Devices
Y. Sasago, et. al.,
VLSI ’09. T2B-1
D. Kau, et. al.,
IEDM ’09. S27.1
K. Gopalakrishnan, et. al.,
VLSI ’10. TS19.41
B. ﻿Govoreanu, et.al.,
IEDM’13. S10.2
S. Yasuda, et.al.,
VLSI, 2017. T2-4
S.G. Kim, et. al.,
IEDM ’15. S10.3

## Slide 15: Threshold Switching Phenomenology & Mechanisms
Selector Devices
Mechanism | Thermionic | Filamentation | Tunneling | MIEC | MIT | OTS
Construct. | P-N or M-S Jx | Ion (Ag+) in Ox | MIM | Cu+ in SE | NbO2 | Chalcogenide
Switching | Electronic | Atomistic | Electronic | Atomistic | Atomistic | Electronic
Polarity | Unidirectional | Bidirectional | Bidirectional | Bidirectional | Bidirectional | Bidirectional
tswitch | sub nsec | ns ~ 100s ns | ps or faster | ns ~ 100s ns | ns to 10s ns | sub ns
JMAX | < 10MA/cm2 | 1-10MA/cm2 | < 1MA/cm2 | ~10MA/cm2 | > 10MA/cm2 | > 10MA/cm2
JInhibit | <1A/cm2 | <1KA/cm2 | <1KA/cm2 | <1KA/cm2 | <1KA/cm2 | <1KA/cm2
VInhibit | < 3V | < 1V | <3V | < 1V | < 3V | < 3V
I-V |  |  |  |  |  | 
Reference | Y. Sasago, et. al., VLSI ’09 | Z. Wang, et.al., Adv Func Mtls (2018) | B. ﻿Govoreanu, et.al., IEDM’13. P10.2 | K. Gopalakrishnan, et.al., VLSI Symposium ’10. | X. Liu et.al., EDL Oct.’14 | S. Yasuda, et.al., VLSI symposium, ‘17,

## Slide 16: Outline
Introduction
Problem Statement and Solution Space
Cross Point Memory Array and Choices of Selector
3D XPoint Memory Technology
Conclusion

## Slide 17: Memory Cell
Sandwiched at the cross point of wordline and bitline metals
Selector device is based on Ovonic threshold switches
Storage element is based on chalcogenide alloy with power efficient memory switching without sub-lithography feature
Carbon electrode has two jobs: electrical connector and chemical barrier
3D XPoint Memory Technology

## Slide 18: Memory Switching
Tight statistical control: The entire volume of memory material undergoes bonding transformations between high (fully crystalline) and low (fully amorphous) conductivity with no partial switching.
Deterministic write algorithms: While it shares a chalcogenide-based genealogy with PCM, it does not rely on stochastic crystallization growth processes initiated at the amorphous-crystalline interface no program verification is required.
These fundamental architectural advantages enable low latency, high bandwidth, AND high endurance NVM subsystems.
3D XPoint Memory Technology

## Slide 19: High-Volume Manufacturing Proven
First generation 128Gb 3D XPoint Memory featuring 5-level metal CMOS Under Array technology delivers high density, low latency nonvolatile memory.
3D XPoint Memory Technology
1st Generation 3D XPoint Media Attributes | 
Attribute | Value
Cell Feature Size (half pitch) | 20nm
# Decks | 2
Die Capacity | 128 Gbits
Bank Access Size | 16 Bytes
# Independent Banks | 16
Read Latency per Bank | 100nSec
Write Latency per Bank | 500nSec
Write Bandwidth (MB/s) per TB | >35,000MByte/sec/TB

## Slide 20: Scaling Direction
Physical Scaling (Density)
  Increase deck count  Vertical scaling
  Pitch reduction  Lateral scaling
Energy scaling
  Variation tightening for supply reduction
  Circuit efficiency improvement to reduce AC and DC dissipation
BW scaling
  Protocol and circuit optimization to reduce access latency
  Increase bank count for concurrency
  Material tuning for performance improvement
Flash inspired (NOR and NAND)
  Multi-Level Cell
  Architecture augmentation
3D XPoint Memory Technology

## Slide 21: Outline
Introduction
Problem Statement and Solution Space
Cross Point Memory Array and Choices of Selector
3D XPoint Memory Technology
Conclusion

## Slide 22: In Pursuit of a Dream …
Conclusion
September 28
1970
December 8
2009
August 13
2020
A Half Century Endeavor

## Slide 23: 3D XPoint Technology Bridges Memory-Storage Gap
Conclusion
MEMORY
Storage
Technology claims are based on comparisons of latency, density and write cycling metrics amongst memory technologies recorded on published specifications of in-market memory products against internal Intel specifications.
+
3D XPoint
Latency: ~100X
Capacity: ~1,000X
Latency: 1X
Capacity: 1X
SRAM
Latency: ~10X
Capacity: ~100X
DRAM
Latency: ~10 Million X
Capacity: ~10,000X
HDD
Latency: ~100,000X
Capacity: ~4,000X-8,000X
NAND SSD

## Slide 24: Optane™ based on 3D XPoint
Conclusion
SRAM
DRAM
NAND SSD
Hard Disk Drives
Optane™ SSD
Latency*
Bandwidth
~>mS
~10-100’s mS
~1’s mS
~100’s nS
~10’s nS
~pS
Higher Capacity* / Lower Cost
~10’s TB
~8TB
~1.5TB
~512GB
~128GB
Optane™ DC Persistent Memory
Intel® Optane™ Data Center Persistent Memory
Intel® Optane™ SSD’s