## Slide 1: VLSI-23 debriefing on Memory Technologies
Dany Ly-Gagnon, Hank Wang and DerChang Kau, July/17/23
Mainstream Memory Technologies
  Flash (DerChang)
  DRAM (Dany)
  SRAM (Dany)
Niche Memory Technologies
  MRAM (DerChang)
Disruptive Memory Technologies
  Gate: Ferroelectric Cap/FET (DerChang)
  Channel: Oxide for 3D memory (Hank)
  RRAM, PCM and TF Diode for SCM (Dany)
  U-MRAM (DerChang)
Bandwidth, Cost
Capacity, Latency
It’s the Memory, Stupid!
…Processor Speed Has Outstripped Memory … today’s chips are largely able to execute code faster than we can feed them with instructions and data. There are no longer performance bottlenecks in the floating- point. ...The real design action is in memory subsystems, caches,buses, bandwidth, and latency…I expect that over the coming decade memory subsystem design will be the only important design issue for microprocessors.
Architects Look to Processors of Future,
Microprocessor Report, V10, N10, Aug/5/1996
Dick Sites, Digital Equipment Corp

## Slide 2: Mainstream Memory Technologies
3D-NAND
DRAM
SRAM

## Slide 3: 3D NAND Leadership
2020 Micron QLC 3D-NAND 176-layer 19nm 512Gb 10.27Gb/mm2, cell size: 56vx152x130nm3
2022
https://www.micron.com/products/nand-flash/232-layer-nand

## Slide 4: 3D NAND Product
T3-4 Samsung 7thGen 1Tb 3D NAND QLC
T3-1 Samsung 8thGen 1Tb 3D NAND QLC

## Slide 5: 3D NAND Scaling direction
T3-3 Kioxia’s Recovery Anneal on 7b/cell Cryo Flash
T3-2 TEL’s HAR (>100) etch for > 10µm/400 ONON layers
T7-1 Kioxia’s MILC for 14µm/300 layers 3D NAND

## Slide 6: DRAM – Recent generations
EUV deployment
DRAM Leadership
12nm ½Pitch
Estimated
(1.35x density improvement)
14nm ½Pitch

## Slide 7: DRAM
T18-1 Samsung 14nm w/ 5 layer EUV
1z
1a
DRAM generation

## Slide 8: 3D-DRAM directions
TFS-1 Vertically scaled DRAM (Samsung)
T18-2 HBI + mini-TSV for DRAM (UniIC + Wuhan Xinxin)
Wafer-to-wafer HBI
(invited talk)
135GBps / 1Gb mem ; 0.66pJ/bit

## Slide 9: SRAM design
C9-2 / 576kb SRAM with 1.9GHz (1.1V) / 0.57V Vmin in 5nm (IBM)
C9-1 / 3nm 256Mb SRAM with interleaved triple WL (TSMC)
M1//M3 or M1//M5 strapping
Rebalance array for FBL

## Slide 10: SRAM design
C9-4 / 4.24GHz 2-port 6T SRAM in 5nm (TSMC)
C9-3 / 4.0GHz 2-port 6T SRAM in 4nm (Samsung)
Clamped Bit-Line Discharge
Bit-Line Charge Time Reduction
Flying word-line

## Slide 11: Niche Memory Technologies
MRAM

## Slide 12
SoA MRAM and Application
iedm’21 Samsung on 28nm MRAM
for Frame Buffer Memory in CIS
May’23 Everspin
NXP, TSMC bring embedded MRAM to
automotive MCUs, May 16, 2023
Isscc-19
13.3 Intel on 22nm eMRAM
Iedm-20
11.4 TSMC on 16nm eMRAM
15.2~18.1 Mb/mm2
vlsi-23 T18-4 Samsung on 14nm eMRAM and beyond (10nm)
vlsi-23 C2-2 Samsung’s 14nm 128Mb@0.64V/12.5ns/18.1Mb/mm2

## Slide 13: Disruptive Memory Technologies
Scalable Ferroelectric Devices
Oxide TFT for 3D memory
PCM/RRAM/Threshold Switching Devices
Unipolar STT-MRAM

## Slide 14: FE-Cap
T12-4 N Taiwan U’s experimental validation 2Pr,max : Ti/EpiHZO/n+Si 84µC/cm2 or Ti/EpiHZO/n+Ge 73µC/cm2
T7-3 Stanford’s record remanent polarization @ 108 μC/cm2 Mo/HZO/Mo
Background –
Theoretical limit of 2Pr (remanent polarization) of piezoelectric material is in the range of 1000s µC/cm2
PZT (Lead Zirconate Titanate) and BaTiO3 (Barium Titanate) reported 2Pr from 100s to 1000s µC/cm²

## Slide 15: FE-FET
T5-1 KAIST/KIST on 3D FE-FET orientation charx
T5-2 U.Tokyo on THZO Characterization and Cycling Endurance
T5-3 N. Taiwan U on NS FE-FET, MW=1.8V, Vp=±2V
T7-2 Hynix’s QLC 3D Fe NAND

## Slide 16: Alternative capacitive FE devices
T10-1 Chinese AoS. 128Kb 1T1C FeRAM
T5-4 NUo Singapore on M-IFE-M-FinFET @50nm LG
T12-2 NUo Singapore on M-IFE-M-FET @41nm LG
T10-4 NUo Singapore on BG FE-FET+ Diode Source

## Slide 17: FTJ
T10-2 GSAT, N Taiwan U on 3D M-i-FE-M FTJ
T10-3 KAIST on Bilayer M-i-FE-S FTJ

## Slide 18: VLSI’23 Oxide TFT – BEOL compatible 3D Memory (1/2)
T17-2 Purdue on scaled ALD a-IGZO TFT
Background: Oxide semiconductor (In2O3, ITO, IGZO, IZO, ...)
Material Basics
  BEOL compatible T < 400 °C
  Relatively high µe : 40~100 cm2 / V*s (Si: ~1400)
  Wide Eg 2.5~3.5 eV => low Ioff
  Drawback: lack of reliable dopant, especially for P
Application: Display(mature), DRAM, 3DNAND
Research Trend: (1). Device scaling w/ advances in dep method. (2). Device optimization for gain cell.
T11-2 NUoSingapore on thickness eng. of a-ITO TFT
T14-1
Notes: T11-2: ITO vt tuning w/ thinner film, together with mobility degradation. SCE still dominates T17-2: how is Ion in Ion-off ratio defined?

## Slide 19: VLSI’23 Oxide TFT – BEOL compatible 3D Memory (2/2)
T17-4 Hynix PVD c-IGZO TFT w/ high thermal budget
T14-2 NYCU/TSMC demo’ed LCH = 8 nm ALD a-IZO TFT w/ controlled SCE & Gm ~ 802 µS/µm
T11-4 Stanford/UoTokyo on gain cell optimization through ITO TFT device engineering
T17-5 imec on IGZO patterning for 2T0C DRAM
PBTI
Notes: T17-4: high thermal budget for memory application
Is GAA IGZO worth reporting?

## Slide 20: Long gestation of Disruptive Memory Technologies
4Kb
200nm feature,
4-mask
Sublitho Heater
Damascene “M “
Subtractive “S”
1970
64Mb
180nm ½ Pitch
6-Mask
Sublitho Heater
Damascene “M”,
Subtractive “S”
64Mb
100nm feature
2-Mask
Self-Aligned,
Subtractive Cell
64Mb
50nm ½ Pitch,
2-Mask
One Deck,
Self Aligned
Subtractive Cell
128Gb
41nm Pitch
Dual Deck
Self Aligned Subtractive Cell
Scaled
Line/Space
2003
2007
2010
2012
2013
2015
2019
1st Production Generation
2nd Production Generation
3rd Production Generation
Ideation
PoC: Electron Devices
PoC: Cell and Array
PoC: Process Architecture
Research Graduation
Contains or derived from supplier Confidential Information
256Gb
41nm Pitch
Quad Deck
Self Aligned
Subtractive Cell

## Slide 21: PCM / chalcogenides
T9-1 Selector-only memory for XPA (Hynix)
T9-2 In-Te OTS for 3D-XPA (Hynix)
Issues with OTS+PCM:
Program window
Endurance
Thermal disturb
Aspect ratio

## Slide 22: 3D RRAM
T9-3 3D RRAM (Ch. Acad of Sci.)

## Slide 23: T18-5 Unipolar MRAM
Bipolar MRAM