## Slide 1: Problem Statement: Can HBM like multi stack be 3D stacked on XPU?
Typical HBM Stack
HBM* stack scaling w/ bumpless Hybrid Bonding
Potential flow to stack HBM* on XPU in 3D
Collateral info
  TSMC SOIC (F2B) for AMD-V Cache
  TSMC SOIC F2F in TD
prashant majhi, FTE

## Slide 2: Typical HBM (POR)
AMD Vega Product
prashant majhi, FTE

## Slide 3: HB for DRAM Stacking [Cube]…… (1/2)
HBM roadmap includes bumpless stacking with Hybrid Bonding
SK Hynix, Samsung
SK Hynix, VLSI 2021
prashant majhi, FTE

## Slide 4: HB for DRAM Stacking [on Logic]…… (2/2)
Xian, Powerchip, IEDM 2020
WoW Alliance + Micron
Scaling Si thickness and increasing 3DID
HB of 3D stacked DRAM (customized with high I/O) on Logic for optimal bandwidth & power
prashant majhi, FTE
Mediatek @SRC’2021

## Slide 5: Potential flow to stack HBM* on XPU in 3D
Si (Top):
Transistors
Interconnects
Si (Bottom):
Transistors
Interconnects
Substrate
TSMC Symposium 2020
Modification of TSMC Symposium 2020
INTEL XPU
Stacked DRAM
TSCM ECTC 2020
Chip-2 as Intel CPU and Chip-1 DRAM stack?
prashant majhi, FTE
F2F HB CoW with ODI like connections for Chip-2

## Slide 6: Problem Statement: Can HBM like multi stack be 3D stacked on XPU?
Typical HBM Stack
HBM* stack scaling w/ bumpless Hybrid Bonding
Potential flow to stack HBM* on XPU in 3D
Collateral info
  TSMC SOIC (F2B) for AMD-V Cache
  TSMC SOIC F2F in TD
prashant majhi, FTE

## Slide 7: AMD CPU Strategy: Multi Chip  Chiplets  X3D?
prashant majhi, FTE
7nm  5nm ?
GF12 nm  N6 nm ?
Std  Info?

## Slide 8
HB for SRAM/Cache on Logic: AMD/TSMC 1/3
prashant majhi
Speculative CoW Flow

## Slide 9
prashant majhi, FTE
SRAM [V-Cache]
CCD [Face Down]
Top: SRAM
Bottom: CCD XPU
HB for SRAM/Cache on Logic: AMD/TSMC 2/3
AMD @ HotChips ‘21
~9um
~6um
SiO2
Bonding Oxide Stack
Speculative CoW Flow

## Slide 10
Tom DeBonis

## Slide 11: V-Cache + Fusion Bond results in “Monolithic-like” Blocks
AMD/TSMC V-Cache
Top Memory Die
Str. Silicon
Str. Silicon
Logic Die
10um
Micro TSVs
5um
15um
~750um
BSM
Oxide Fill
Oxide Fusion Bond
Structural Silicon 2
Cu:Cu /Ox:Ox Hybrid Bond
  CCD Base Wafer
  Top Cache Die
  & Structural Si
C2W Bond (20um die)
PECVD SiOx Gap Fill, Backgrind
Std Process + TSV & Sort
Passiv/Bond /TSVReveal/ HB pads, CMP
Finish Std Process: Bumps, etc.
Fusion Bond Structural Silicon 2
HB Pad Surface Prep
Std Process
Plasma Singulation on frame
Expected TSMC SoIC Process for AMD Zen 3 V-cache
Tom DeBonis

## Slide 12
Grind/Expose TSV
Cu Hybrid Bond Pads
prashant majhi
Flow for V-cache [speculation]
Stack Si structural support wafer on back to expose base die Al-pad and C4 bump;
Std A&T after that
Multiple CoW to fill Wafer
prashant majhi, FTE

## Slide 13
Flow for V-cache [speculation]
Grind/Expose TSV
Cu Hybrid Bond Pads
prashant majhi
Multiple CoW to fill Wafer
prashant majhi, FTE

## Slide 14
CoW Hybrid Bonding
Si
Transistors
Interconnects
Cu
Si
Interconnects
SRAM Chiplet
Si
SRAM Chiplet
1x SRAM Stack
[CoW]
Si
SRAM Chiplet (Cube)
4x SRAM Stack
[WoW + CoW]
prashant majhi

## Slide 15: AMD V-Cache: Future?
prashant majhi, FTE
HB for SRAM/Cache on Logic: AMD/TSMC 2/3
Epyc BIOS with #N Stack
TSMC IEDM ‘20
Speculative CoW Flow

## Slide 16: IMEC Process Dev/Learnings with WoW (N=4)

## Slide 17: 3D Chip Stacking + Adv Packaging
https://min.news/en/economy/64f15e0861b4f16760f4ef7b43873b92.html
prashant majhi, FTE

## Slide 18: TSMC OIP 2021: eTV with Logic on Top
https://semiwiki.com/semiconductor-manufacturers/tsmc/304612-update-on-tsmcs-3d-fabric-technology/
prashant majhi, FTE

## Slide 19: TSMC OIP 2021: eTV and eco-system for 3DIC
https://semiwiki.com/semiconductor-manufacturers/tsmc/304612-update-on-tsmcs-3d-fabric-technology/
prashant majhi, FTE

## Slide 20
prashant majhi, FTE
TSMC SoIC @ IEDM 2020 “Abstract”
Wrote About 2 Prototypes TV but only presented one (PTV1)!
Test Chip #1
Test Chip #2

## Slide 21: AMD Future 3DIC With Hybrid/Fusion Bonding?
SOIC Multistack SRAM [CCD  SRAM x N]
WoW Deep Trench Cap for high Cap Density [PI for I/O , CCD ?]
ISMC for Thermals
SOIC [V-Cache] + HBI interposer [CCDCCD… Graphics?]
Logic/DRAM Stack?
Structural Si Also as LSI Interposer
WoW Logic + DeepTrenchCap
High MIM Cap Density for Droop and Structural Si support?
prashant majhi, FTE

## Slide 22: F2F(Std)
Si (Bottom):
Transistors
Interconnects
Si (Top):
Transistors
Interconnects
Substrate
Si (Top):
Transistors
Interconnects
Si (Bottom):
Transistors
Interconnects
Substrate
Si (Top):
Transistors
Interconnects
Transistors
Interconnects
Substrate
F2B(std)
F2F (BS-PDN)
Feature | F2F (std) | F2B (std) | F2F (ODI) | F2B (ODI) | F2F (BS-PDN)
Socket T | Bump/Pad [R,L,C] | Bump/Pad [R,L,C] | Bump/Pad [R,L,C] | Bump/Pad [R,L,C] | Bump/Pad [R,L,C]
Adaptor T-B | --NA-- | TSV (B): micro-TSV | --NA-- | TSV (B): micro-TSV | --NA--
Socket B | Bump/Pad [R,L,C] | Bump/Pad [R,L,C] | Bump/Pad [R,L,C] | Bump/Pad [R,L,C] | Bump/Pad [R,L,C]
Additional routing T-S | TSV (B) | TSV (B) | TMV | TMV | nano-TSV(B) + IC(B)
Adaptor B-S | TSV (B) | --NA-- | TSV (B) | --NA-- | nano-TSV (B)
Socket B-S | C4 bump | C4 bump | C4 bump | C4 bump | C4 bump
F2F (ODI)
Si (Top):
Transistors
Interconnects
Si (Bottom):
Transistors
Interconnects
Substrate
Si (Top):
Transistors
Interconnects
Substrate
Si (Bottom):
Transistors
Interconnects
F2B (ODI)
Socket T
Socket B
Socket B-S
RDL like Routing to HB pads
prashant majhi, FTE

## Slide 23
Samsung @ SAFE 2021
prashant majhi, FTE

## Slide 24
Samsung @ SAFE 2021… HB Stacking DRAM?!!
prashant majhi, FTE