## Slide 1: CHIPKA: Process Options and Risk Assessment
prashant m .. .for internal discussion with CHIPKOOS …. 12/18/2018

## Slide 2: Preferred Approach for Shared CMOS (option d’)
Architecture Overview
Array Operation: CMOS from top wafer drives blocks from both top and bottom wafer (saves CMOS processing steps)  connected BLs, separate string drivers for top and bottom wafers.
New Process: via through the bottom of the CMOS (~5um deep, similar to CON3 dimensions: 600nm pitch, 400nm diameter) is required to connect the bottom array.
Top Wafer (no change): Array + CMOS + top metals
Bottom Wafer: Array + BL metal layer + W0 + Cu1
Performance Impact: 2x reduction in RR IOPS and Seq Write BW
Chip Layout: appears feasible to fit all CMOS in bottom wafer (N39A density)
Total cost savings: 8.1%
INTEL CONFIDENTIAL

## Slide 3: 2+ Process Options (D), (E), (G) ….
INTEL CONFIDENTIAL
Preferred Structure for Shared CMOS

## Slide 4
CMOS+Array (Wafer 1)
Array (wafer 2)
Si
Si
SiO2
Process Option D: Hybrid Bonding
INTEL CONFIDENTIAL
Si
Support Wafer
Temp bond support wafer
Support Wafer
Thin Si
Support Wafer
Via through Thin Si + Metal
Si
SiO2
Support Wafer
Hybrid Bonding
+ De-bond Support wafer and expose pads
(1)
(2)
(3)
(4)

## Slide 5
INTEL CONFIDENTIAL
Array
Si
Si
SiO2
Si
Perm bond Si wafer
Thin Si,
+CMOS
+Shallow TSV +Array
Si
SiO2
Si
SiO2
Process Option E

## Slide 6: Risks with Options (D) and (E)
D
E
Hybrid bonding Alignment Capability Curved wafer Yield | Procure IMEC dedicated HB wafers and work with EVG? Join IMEC-3D program?
Fusion Bonding (Temp/Perm) and de-bond/remove | - EVG/TEL/SUSS demo?
Backside Thinning - Grind / Lap / CMP / Metro | - demo’s (Disco/AMAT) ?
Shallow TSV (Etch / Insulator/ Metallization) | - demo’s (LAM /AMAT)?
?? | 
Hybrid bonding | 
Fusion (perm) Bonding | EVG/TEL/SUSS demo
Backside Thinning - Grind / Lap / CMP / Metro | - demo’s (Disco/AMAT) ?
Shallow TSV (Etch / Insulator/ Metallization) | - demo’s (LAM/AMAT)
Extra Thermal budget on bottom array | internal assessment
Thinned Si for active transistors | Demo +internal assessment
Risk
AR
Risk
AR

## Slide 7
INTEL CONFIDENTIAL
Bottom Array (wfr 1)
Si
Si
SiO2
Bond and transfer CMOS
Bond and Transfer Array + CON3 + top metals + Pad
Si
SiO2
Si
SiO2
Process Option G
Si (only CMOS / No metals)
oxide
Temp Bond Carrier
CMOS (wfr 2)
[Temp Bond and Backside Thinned]
Top Array (wfr 3)
[Temp Bond and Si Removed]
oxide
Temp Bond Carrier
Si (only CMOS / No metals)
oxide
Shallow TSV + Metals

## Slide 8
INTEL CONFIDENTIAL
Bottom Array (wfr 1)
Si
SiO2
Process Option G (Build)
Si (only CMOS / No metals)
oxide
Temp Bond Carrier
CMOS (wfr 2)
[Temp Bond and Backside Thinned]
Top Array (wfr 3)
[Temp Bond and Si Removed]
oxide
Temp Bond Carrier
Bond and transfer CMOS
Si
SiO2
Si (only CMOS / No metals)
oxide
Si
Bond and Transfer Array + CON3 + top metals + Pad
Si
SiO2
Shallow TSV + Metals

## Slide 9: Snapshot of IMEC 3D Hybrid Bonding Test Vehicle

## Slide 10: Evidence of TSV Through Fusion Bonded Interface
Bonded interface
(ISP/DRAM)
Bonded interface
(DRAM/CIS)

## Slide 11
8um

## Slide 12: Expected Flow for CIS/DRAM/ISP Integration
ISP (Si + CMOS)
ISP backend (Metals/landing pad)
DRAM (Si + CMOS)
DRAM backend (Metals/landing pads)
CIS (Si + Metals)
CIS backend (Metals/landing pads)

## Slide 13: Expected FLOW for CIS/DRAM/ISP Integration
ISP (Si + CMOS)
ISP backend (Metals/landing pad)
DRAM (Si + CMOS)
DRAM backend (Metals/landing pads)
CIS (Si + Metals)
CIS backend (Metals/landing pads)
ISP (Si + CMOS)
ISP backend (Metals/landing pad)
DRAM (Si + CMOS)
DRAM backend (Metals/landing pads)

## Slide 14: Expected FLOW for CIS/DRAM/ISP Integration
ISP (Si + CMOS)
ISP backend (Metals/landing pad)
DRAM (Si + CMOS)
DRAM backend (Metals/landing pads)
ISP (Si + CMOS)
ISP backend (Metals/landing pad)
DRAM (Si + CMOS)
DRAM backend (Metals/landing pads)
ISP (Si + CMOS)
ISP backend (Metals/landing pad)
DRAM (Si + CMOS)
DRAM backend (Metals/landing pads)

## Slide 15
ISP (Si + CMOS)
ISP backend (Metals/landing pad)
DRAM (Si + CMOS)
DRAM backend (Metals/landing pads)
CIS (Si + Metals)
CIS backend (Metals/landing pads)

## Slide 16
ISP (Si + CMOS)
ISP backend (Metals/landing pad)
DRAM (Si + CMOS)
DRAM backend (Metals/landing pads)
CIS (Si + Metals)
CIS backend (Metals/landing pads)
ISP (Si + CMOS)
ISP backend (Metals/landing pad)
DRAM (Si + CMOS)
DRAM backend (Metals/landing pads)
CIS (Si + Metals)
CIS backend (Metals/landing pads)

## Slide 17
ISP (Si + CMOS)
ISP backend (Metals/landing pad)
DRAM (Si + CMOS)
DRAM backend (Metals/landing pads)
CIS (Si + CMOS)
CIS backend (Metals/landing pads)
ISP (Si + CMOS)
ISP backend (Metals/landing pad)
DRAM (Si + CMOS)
DRAM backend (Metals/landing pads)
CIS
CIS backend (Metals/landing pads)
ISP (Si + CMOS)
ISP backend (Metals/landing pad)
DRAM (Si + CMOS)
DRAM backend (Metals/landing pads)
CIS
CIS backend (Metals/landing pads)

## Slide 18: Re-Cap: Hybrid Bonding (Classification and Implementation)
Tezzaron’s 8 wafer stack w/ Hybrid Bonding
Sony Camera in Samsung S7
Intel Confidential
In R&D
YMTC XStacking
In HVM
3D NAND
CMOS image sensors with DRAM (3 wafer stacking)
Novel 3D integration (monolithic <===> TSV)
Split n Bond (reduce cycle time)
…