## Slide 2: Via in one Stephen Morien

## Slide 3: Via in one
Recently there has been confusion in several conversations as to what via in one is, what qualifies as via in one, how we are using it in AMT and AMT RA

## Slide 4: Via in one vs TSV
TSV
  Etch a hole in silicon
  Apply dielectric layer to isolate from silicon
    If via last process, remove dielectric layer from bottom contact
  Fill with metal
    If via mid/first grind to to TSV expose
Via in one
  Etch a trench in silicon before transistors/metalization
  Bond wafer
  Grind to thickness less than depth of oxide trench
  Etch via hole
  Fill with metal, contacting multiple levels if needed

## Slide 5: Via in one vs. TSV
Application in AMT is multi-high multi-connection stacking
But lets focus on via in one baseline first
  Trench is through silicon only
  A “large” structure, with low aspect ratio
    Ex for DRAM application
      8u total thickness – 2u silicon, 6u capacitor, metal, pass
      For 15u via in one 12.5u trench : not 5:1 aspect ratio, but 1:6.25
      For <15u via in one pitch, multiple via in same trench
    For 5u via in one; 15u trench with 3 via in one; 2:15 AR
  Increased spacing vs. dielectic liner also reduces capacitance
Also : trench fully penetrates silicon:
  Replaces DNW impact for substrate isolation
  In many processes mask count neutral to add via in one trench

## Slide 6: Multistacking
Single pass would be ideal….
  for 15u AMT Stack:
    64u (8xdram) + ~2u (to base die metal)
    66u x 7.5u - 8.8:1 aspect ratio
  For 5u AMT stack
    66u x 2u 33:1 aspect ratio
These numbers are possible…
  But not necessarily with tools in this fab

## Slide 7: MultiPass
Can do via in one in several passes
  First layer : 16u+2u, contact 3 layers
    2.4:1 aspect ratio
  Surface planarized to oxide bond next wafer
    Can do oxide over via in one to have homogenous layer

## Slide 8: Multiple pass
Second layer : 2 or 3 wafers
  16u or 24u – 2.1:1 or 3.2:1 aspect ratio
And repeat to get 8+1 stack
These shallow AR’s are easily in range for cu metal
Note: each via in one contacts previous via in one
  Not HBI.
Penalty is series construction

## Slide 9: Multipass 5u via in one
2u via in one CD:
  9:1 AR for base + 2
  8:1 for adding 2 wafers
  12:1 for adding 3:1 wafers
Still in range for cu metaliztion – but pushing it
But getting small enough to use tungsten

## Slide 10: Via in one data line vs. dram planar data line
Via in one resistance Cu vs. W would seem to be significant (5x)
However, even at 2u CD (5u via in one pitch)
  Cu resistance <2 ohm
  W resistance < 10 ohm
And are not significant vs. in plane local data line (>50ohm)