## Slide 1: Transistor Pathfinding for 3DXP Decoder
Team CMOS, WW03.3
3DXP scaling path – ~30% cost reduction every generation (5Q).
Transistor evolution ideas – Starting from planar bulk CMOS
  Bulk CMOS geometry augmentation such as Recess Channel and/or Saddle Fin Channel
  NSG TCAD assessment on R-FET and SF-FET scaling path
  Wideband gap channel enable aggressive channel length scaling
3DIC for die size reduction and parallelism improvement (tile size)
  Technologies include Layer Transfer-Si, Poly Si TFT and Adamantine
  CR collaboration on LT-Si, Poly-Si TFT and ADM for gap assessment and closure.
  Array architect and technologist to complete die size, cost and performance assessment of 3DIC for strategy development
First round of transistor technology benchmark by mid Q1

## Slide 2: Si CMOS Geometric Augmentation

## Slide 3: Transistor Active Area Augmentation
Planar Channel FET
ZDrawn= 0.41mm
LDrawn = 0.35mm
In 0.5X0.9mm2 footprint
Recess Channel FET
ZDrawn= 2X 0.41mm
LEff = 0.35mm
in ~0.5X0.5um2 footprint
Saddle-Fin Channel FET
ZEff= 2X 0.41mm + 2*n*HeightFIN
LEff = 0.35mm
in ~0.5X0.5um2 footprint
P-FET
R-FET
SF-FET

## Slide 4
P-FET
R-FET
P-FET
R-FET
SF-FET
SF-FET

## Slide 5: Simplified Lumped Model
Also what was done with Adamantine SF-CAT as an example
Half Channel
SF CAT

## Slide 6: Z, L Design Strategy
Fin height for on-state resistance to optimize tsense
Recess Fin to increase Chanel length to reduce leakage for retention time
L1
Z1,H
Z1,W
RCh1 = (qµCoxVon)-1 · L/W
RCh1-1 = qµCoxVon· (2·Z1,H+ Z1,W)/LG1
RCh2 = (qµCoxVon)-1 · L2/[ ½ ·(Z1+Z2)]
RCh2-1 = qµCoxVon· [Z1,H+ Z2,H+ ½(Z1,w+Z2,w)]/L2
L1 + 2 · L2 ≈ Lmin ;
Z2,H = Z1,H + L2 ;
Z2,W = Z1,W + 2 · L2 ;
RCh1-1 = qµCoxVon · (2 · Z2,H + Z2,W – 4 · L2) / L1 ;
RCh2-1 = qµCoxVon · (2 · Z2,H + Z2,w – 2 · L2) / L2 ;
where
Von = VP – VT ;
RCh = RCh1 + 2· RCh2 ;
Active Design Rule (2 Cells)
Cell Active Pitch = Z2W+ SZ ;
Cell Active Pitch = 3 · LSD + 2 · L1 + SL
L2
Z2,H
Z2,W
LSD
SL
SZ

## Slide 7: Channel Morphology
Sharp inner corners impede field effectiveness; it degrades Ioff and Ron

## Slide 8: Recess vs. Saddle Fin Channel
L1
L2
L2
L1
Z
Z
2·L1+L2
Z
x·Z
x·Z
L1
L2
L2
L1
Z
Z
x·Z
L1
Z
L2
L2
Z
H
x·Z
L1
H
x·Z
L1
Z+2·H
L2
R1=K·L1/Z
R2=K·L2/Z
RH=K·L2/(2·H)
RA = 2·R1 + R2
= K·(2·L1+L2)/Z
RB > 2·R1/x + R2
= K·2·(L1/x+L2)/Z
= RA + 2·R1·(1-x)/x
Where 0 < x < 1
RA
RB
RC
RC > 2·R1/x+(R2//RH)
= 2·R1/x+R2·[1–H/(Z+2·H)]
= RB–R2·[2·H/(Z+2·H)]
= RA + 2·R1·(1-x)/x
– R2·[2·H/(Z+2·H)]

## Slide 9
Active Area, Deep Trench
Saddle Gate, Med Trench
Recess Channel, Shallow Trench