## Slide 1: FERROelectrics review FEB. 2020
Jan Van Houdt on behalf of the ferro team

## Slide 2: outline
Introduction: program targets and research vehicles
2019 Plan
Progress made in 2019
  Materials and basic understanding
  2D FeFET
  3D FeFET
What’s new in 2020?
Conclusion

## Slide 3: Ferroelectric memory Program targets - 2019
Identify the best materials stack for nonvolatile ferroelectric FETs (currently Hf-based)
Build basic understanding on ferroelectric switching behavior in Hf-based materials and related reliability issues
Demonstrate the best stack in vertical FeFET vehicle and planar FET vehicle

## Slide 4: TEST VEHICLES
Blanket test material
CAPATWO 1maskflow (SIS)
CAPATWO 1maskflow (MIS)
SAKKARA 3DFET Trench device
SAKKARA Macaroni (Memhole) device
SALSA3-PLANAR 2DFeFET device

## Slide 5: FERRO HLP 2019
Code | Topic Group | Deliverable | Success criteria | Timeline | Status
FF01 | Basic understanding | Ferroelectric modeling | Fundamental study of the wake up effect Analysis of dopant confinement effects Theoretical assessment of nucleation and propagation dynamics | Dec. 2018 April 2019 Oct. 2019 | Nucleation and propagation study showing very fast propagation (nucleation limited switching)
 |  | Material characterization | Continuous material analysis through XRD (phase optimization) | Dec.2019 | XRD phase ratio vs. cycling confirmed on Si-doped films Nanograin ongoing
FF02 | Material study | SIS further exploration and optimization | SIS Material exploration (dopants/dep. conditions) SIS Best known stack delivering 10 years of retention @85C, 100k cycles, <4V operating conditions, in cap flow | April 2019 Oct. 2019 | La: HfO2 film developed and first 2 lots evaluated. La layer ready for integration
 |  | MIS exploration and characterization | MIS Si-doped HfO2 stack available in MIS (>1000C TB, 1yr retention @RT, 100k cycles @<4V) MIS Imprint analysis finalized on Si-doped HfO2 stack | June 2019 Oct. 2019 | MIS imprint ready. New model available.
FF03 | 2DFeFET MIS | Planar FerroelectricFET demonstration | Functional single cell (0.5V MW) Single cell with 1E5 cycles endurance and 1yr retention @RT | April 2019 Oct. 2019 | 2DFeFET pipecleaner ready and working, endurance reached, retention not
FF04 | 3DFeFET SIS | Vertical FerroelectricFET optimization in Memholes and Trench approaches | Plug cell with 1V MW @1k cycles and 10 yrs of retention @RT Trench FeFET 1st electrical results (read current density similar to plug version and 0.5V MW) Trench FeFET Endurance (1k) and 10 yrs retention @ RT | Dec. 2018 April 2019 Oct. 2019 | Trench etch development completed for pipecleaner. First 3D Trench FeFET cells found working. 2nd lot showing good yield and large memory windows (~3V)

## Slide 6: Progress (highlights)

## Slide 7: FF01 basic understanding: summary
Ab-initio work shows good progress:
  Dopant impact
  Nucleation/propagation dynamics
  Link to XRD to explain wake-up (phase transformation)
XRD analysis has been helpful to understand phase (ratio) changes
o-content decreases
m-content increase

## Slide 8: FE HfO2 – ab initio analysis
Linear impact of dopant concentration on energetic stability of the ferro phase
Chart: Dopant concentration [atomic%]
| 0.14000000000000001 | 1.4 | 4.2
Al | -0.0091431 | 0.0082514 | 0.090976
La | -0.0091467 | 0.0016575 | 0.066969
Si | -0.0061479 | 0.039441 | 0.13852
Chart: 
Energy (eV/atom) | 0 | 0.01 | 0.024 | 0.025 | 0.028 | 0.029 | 0.055 | 0.089 | 0.139
Experimental % for FE
5%Al-doping/3.6%Si-doping make ortho-IV, tetra-II and cubic phases accessible
Relative energy [eV/atom]
G1

## Slide 9: Ab initio study of ferroelectric switching dynamics in HfO2
Polarization reversal barrier
1st Nucleation
2nd Nucleation
Domain switching dynamics
m
Final
m
Final
Crystal clamping
FE Switching = stochastic process of jumping across a barrier. Barrier is modulated by T, strain, Efield, defects, etc.
Un-clamped system  freedom to relax/phase-transform towards lower energy configuration (monoclinic grains)

## Slide 10: GIXRD for phase ratio analysis
Polycrystalline
Poly-phase
Several “doping” atoms
  Different phase ratio
HfO2 films
Material optimization for different dopants/doping levels done (Si, Al), La underway

## Slide 11: Basic understanding and materials
o-content decreases
m-content increase
90º domain flip to accommodate strain
Grains re-orient to put polarization direction of o-phase parallel to E-field Pr increase
Measured o-content decreases due to limitation of GIXRD
m-phase is generated to accommodate strain => wake-up mechanism
Grain re-orientation identified as main mechanism for wake up

## Slide 12: Imprint explained from interaction with traps
defect density corresponding to same effect as polarization charge (8μC/cm2)
+
At high defect density,
charge trapping balanced
by polarization charge
Imprint can be drastically suppressed when impact of defect density becomes lower than that of polarization charge

## Slide 13: Charge trap characterization
Similar defect density for both layers present
Et ~ 2eV below HfO2 conduction band minimum
Comparison ferro vs. non-ferro
9.5 nm Si: HfO2
9.5 nm HfO2
1.85 eV below Ec min
Sigma 0.124
Nt = 2.3E19
1.7 eV from Ec min
Sigma 0.087 eV
Nt = 2E19

## Slide 14: Ff02 materials study (caps): summary
Si- and Al-doped stacks delivered with 1E5 cycles and 10 years retention at 85C
La-doped stack almost ready (retention @RT)
MO precursor route explored (not beating Cl-based)
2.5% Si

## Slide 15: MIM vs SIS
TiN
TiN
HfOx
Si
Si
MIM with Si interfaces
p-type
TiN
TiN
HfOx
SIS with TiN interfaces
p-type
n-type
Pristine
1000 cycles
MIM behavior without opening –
Strong pinning of domains at interface
SIS behavior –
2nm Si interfaces: no need to wake-up
Pristine
1000 cycles
Key role of interfaces!
Our focus sofar

## Slide 16: Endurance and Retention on Si:HfO2 SIS caps
4.5MV/cm
2.5% Si
SIS stack specifications are reached
1E5 cycles

## Slide 17: Endurance and retention on Si:HfO2 MIS caps
Good endurance for both 3.6% and 2.5% Si content wafers
105 cycles - 4V
3.6% Si
2.5% Si
norm. variation
Similar to the SIS case, low Si dopant concentration in MIS gives better retention
2.5% Si

## Slide 18: La:HfO2
flow
18
Metal Precursors:
  HfCl4
  LOLA’
Oxidant: H2O
Reactor Temperature: 300oC
As grown La:HfO2 films: Amorphous
Hf:La = 14:1 - 48:1
La% = 5.6 – 1.9%
N2
N2
N2
N2
N2
TMA
TMA
H
2
O
H
2
O
O3
H
2
O
H
2
O
O3
N2
N2
N2
N2
LOLA’
HfCl4
Hf cycle
La cycle
Pulse ratios: 14:1-48:1
14-48 pulses
1 pulse
Anneal: 700ºC/60s
900ºC/60s
1000ºC/30s
 Poly Si did not crystallise

## Slide 19: Endurance on La:HfO2 SIS caps
best hysteresis loop (higher 2Pr) for 14:1 ratio
Better endurance (10k) for intermediate PDA temperature (900C 1min)
1000C 30s
900C 1min
104 cycles, 4V bias
Retention not met at 85C

## Slide 20: Endurance on La:HfO2 MIS caps
PDA: 1000C 30s, 1nm SiO2 (ISSG)
Good endurance at 4V up to 105 cycles
14:1 20:1 34:1 40:1 48:1
Good RT retention results extrapolated to 1 yr
Good endurance and RT retention obtained on La-doped MIS stacks

## Slide 21: Ff03 planar fet: summary
Working MFIS FET established in Salsa-3 (Si-doped HfO2)
Si buffer layer between HfO2 and TiN yields 1E5 cycles
La-doped FET underway (later also Gd and Y)
~0.8V MW @ 1e5cycles

## Slide 22: Metal/Insulator/Semiconductor (MIS) FeFET
Top Electrode Stack:
50 nm CVD Si (Poly-crystalline Gate)
5 nm ALD TiN / 2nm PVD Si (Metal Gate)
Ferroelectric layer:
9.5 nm Si-doped HfO2
3.6% Si doping
PDA: 1000C, 30s, N2/O2
Interfacial Layer:
1 nm SiO2 (chemical)
Substrate:
p-Si
Reference
DOE: MW as function of Si doping, HfO2 thickness and interfacial layer composition
GATE
SOURCE
DRAIN
FERRO
Aluminum
MG
PG
p-Si substrate
Pwell
IL
SALSA3-PLANAR 2DFeFET device

## Slide 23: Working 2D FeFET (MFIS)
IL: 1nm SiO2
Ferro: 9.5nm/3.6% Si
MG: 5ALD-TiN/2PVD-Si
PG: 50CVD-Si
PDA: 1000C,30s,N2/O
MW @ 100cycles = 0.5V
init
Vth
April PTW

## Slide 24: High endurance 2D FeFET
IL: 1nm SiO2
Ferro: 9.5nm/3.6% Si
MG: 2PVD-Si/5ALD-TiN/2PVD-Si
PG: 50CVD-Si
PDA: 1000C,30s,N2/O
FE MW
Asymmetric pulse +4V / -5V
~0.8V MW @ 1e5cycles
1E5 endurance and RT retention after 1kcycles obtained on Si-doped 2D Fefets
Low Vt level
High Vt level

## Slide 25: Ff04 3d Fefet: summary
3V window!
Trench cell shows large window with good uniformity but limited endurance (1E3)
Plug cell shows 1E5 cycles with good uniformity but limited window (~1V)
TSEL
CG
BSEL
MW

## Slide 26: Where could it fit in?
MRAM
Legend
Emerging/MIM
Ferro
Flash
Separate offering
Archival
Slow cache L3/eDRAM
On-chip (embedded)
Off-chip
(stand-alone)
SOT MRAM
STT-MRAM
MIMCAP
3D DRAM / IGZO select transistor
3D SCM (PCM +selector)
3D NAND
DNA-inspired
STT-MRAM + selector
3D FeFET
NOR
eFlash
STT-MRAM
OXRAM/CBRAM
SCM
Memory insite
Device for Machine Learning
Disruptive

## Slide 27: vertical ferroelectric FET
Poly
Oxide
Poly
Oxide
oxide
Gate
ferroelectric
Channel liner
Dielectric filler
Cell 1
Cell 2
3D NAND scaling limitations :
    Vertical pitch: high voltages (O), channel length (P)
    Lateral pitch: plug diameter and slits (RMG)
FeFET = 1T
    Similar to existing 3D architectures
    Higher density possible
      Vertical: lower voltages, no lateral charge migration, no interference, shorter channel (thinner EOT)
      Lateral: thinner gate stack, relaxed etch, POPO flow allows for fewer (or no) slits
    Bonus: low EOT yields higher read current (for same channel quality)
Challenges/solutions
    Reduce depolarization/disturbs : POFET concept
    Stable ferroelectricity on vertical sidewall : ALD
    Statistics of grains and domains: nanograin
gate
gate
gate
HfO ferro layer
Poly channel
Oxide filler
source
drain

## Slide 28: 3D Trench fefet: the rationalE
2bpc trench FeFET can be denser than 4bpc NAND because of better lateral and vertical scaling
Main parameters [nm] | Memory option |  |  | 
 | Scaled 3D NAND | Plug FeFET | V-RRAM | Trench-FeFET
Plug diameter /trench width | 60 | 60 | 60 | 60
Dielectric stack | 15 | 8 | 16 | 8
Cell width | 100 | 100 | 50 | 50
Cell length | 20 | 10 | 10 | 10
Intergate spacing | 15 | 8 | 14 | 8
J. Van Houdt, invited papers at 2017 IMW and VLSI

## Slide 29: 3D FeFET
Improved MW uniformity between gates with thinner channel
Asymmetric pulses allowed better endurance up to 1E5 cycles
POR (20nm channel)
11nm channel
Endurance
Thin channel (11nm)
MW
MW
MW
# cy
# cy
# cy
MW
D18 11nm Undoped channel
TSEL
CG
BSEL

## Slide 30: Endurance
Some cells have large MW after 1E5 cycles
TSEL P7N8
0.8

## Slide 31: 3D trench Fefets
Vertical trench cells obtained with good Id-Vg characteristic and ferroelectric memory window... But low yield....
Vt after -8V pulse
Vt after +8V pulse
+/-8V 100ns pulses
0.6V
143
Good Id-Vg characteristic

## Slide 32: Yield improvement for 3D trench fefets
Leakage (gate)
68.6%
Leakage (other)
27.4%
Working 3%
Leakage (gate)
17.6%
Leakage (other)
12.4%
Open 5%
Working 75%
April 2019: pipecleaner lot
October 2019: LC1
Significant yield improvement with modified trench etch strategy
APF based trench etch
Surface full of pits
242nm
333nm
99.5o
SoC based trench etch
Clean surface
280nm
350nm
96.5o

## Slide 33: LARGE Memory window OBTAINED in 3D trench!
MW larger (up to 3V window)
1k endurance and RT retention
Good uniformity between gates
Vertical uniformity
Bias impact
3V window!
10yrs
Pos pulse
Neg pulse
Retention
MLC capability to be checked

## Slide 34: longer pulse yields same window for lower Vpp
Longer pulse duration of 1us (i.o. 100ns) allows high MW also at 10V bias amplitude.
   RC delay problem at 100ns
Increasing to 10us does not improve further
   Max achievable MW for this stack = 3V
Case 12nm Si:HfO2 ; P-type gate (D11)

## Slide 35: Reason for high Vprog
Bias amplitude can be lowered by longer duration pulse (RC delay problem with short pulses)
Root cause is low channel conductivity rather than WL issue:
  Strong dependence of MW on channel width
  Interfacial layer at drain / channel and source / channel observed in TEM (worse on drain side since Ion @Vd=1V > Ion @Vs=1V)
  No difference between n-type and p-type gate
  Gates are similar in memhole and trench versions, yet memhole device does not need high Vprog

## Slide 36: Cycling with verify
Verify reduces the memory window variability
More stable window up to 1E3 cycles
MW
+14V 100ns
-14V 100ns
Single pulse P/E
P/E to target [ -1.5 | +1.5V ]

## Slide 37: Channel width dependence
Sharp Ion decrease, STS variability below 100nm

## Slide 38: 3D trench : summary

## Slide 39: 3D FerroFET patents

## Slide 40: Highlights - summary
Good understanding of nucleation/propagation effects and their interplay
Explanation for wake-up and cycling-induced phase ratio change in Si:HfO2
Improved model for imprint in ferrocaps and –fets
Working La-doped HfO2 layer developed (cap level)
Improved endurance on 2D and 3D GAA FerroFET (1E5 cycles)
Good yield and large memory window (~3V) obtained on 2nd 3D trench FerroFET lot

## Slide 41: What’s next?

## Slide 42: Ab initio study of ferroelectric switching dynamics in HfO2
Polarization reversal barrier
1st Nucleation
2nd Nucleation
Domain switching dynamics
m
Final
m
Final
Crystal clamping
FE Switching = stochastic process of jumping across a barrier. Barrier is modulated by T, strain, Efield, defects, etc.
2020: trapping-switching interaction study

## Slide 43: Basic understanding and materials
o-content decreases
m-content increase
90º domain flip to accommodate strain
2020:
- nanograin exploration for more uniform response
- new dopants Gd/Y in HfO2
- HfZrO4 will be revisited in MiM caps (+ doping) as well as alternative ferroelectrics
Grain re-orientation identified as main mechanism for wake up

## Slide 44: Nanograin for ferro
Variability and coercive field control through grain size engineering
Nanograin could provide better control
Yoo et al., IEDM 2017, p481
Requires accurate annealing control
Requires also adequate metrology
Benefit to be proven
Large WiW variation in (single shot) ferro characteristics

## Slide 45: High endurance 2D FeFET
IL: 1nm SiO2
Ferro: 9.5nm/3.6% Si
MG: 2PVD-Si/5ALD-TiN/2PVD-Si
PG: 50CVD-Si
PDA: 1000C,30s,N2/O
FE MW
Asymmetric pulse +4V / -5V
~0.8V MW @ 1e5cycles
2020: need to improve retention
Iaft_pos
Iaft_neg

## Slide 46: Further improvements on 3D FeFET planned for 2020
MW
CG
MW
TSEL
MW
BSEL
-14V
+14V
higher endurance & lower P/E voltage
MW=2V
Current MW=1E4
larger window and Ion/Ioff ratio
retention
improved retention
MW
Start MLC study & scale z-pitch

## Slide 47: FERROelectrics 2020 HLP and deliverables
Code | Topic Group | Deliverable | Success criteria | Timeline | Status
FF01 | Basic understanding | Ferroelectric modeling | Understanding of the interaction between defects and ferroelectric switching Impact of this interaction on wake-up, imprint and fatigue | Oct. Dec. | 
 |  | Material characterization | La-doped ferroelectrics benchmarked wrt Si doped Alternative dielectrics screening (literature, simulations) | April April | 
FF02 | Material study | MIS further exploration and optimization | Optimized La-doped MFIS stack (better than Si-doped case) | Oct. | 
 |  | MIM exploration of alternative dielectrics (HZO/perovskites...) | Doped and undoped HZO MIMcaps with high endurance (1E9) Choice of alternative (non-Hf) ferroelectric with implementation plan Final benchmarking of dopants in HZO for high endurance | June Oct. April 2021 | 
FF03 | 2DFeFET MIS | Planar Ferroelectric FET demonstration | Optimized 2D MFIS FET with 1E5 cycles and 10yrs retention at 85C | Oct. | 
FF04 | 3DFeFET SIS | Vertical Ferroelectric FET optimization in Memhole and Trench approaches | Memhole cell with >1.5V MW, 1E5 cycles and 10 yrs retention @85C, incl. first MultiLevel assessment Trench FeFET with sufficient reliability (>1E4 Endurance and 10 yrs retention @ 85C) 2 bpc demonstrated on trench | April Oct. Dec. | 

## Slide 48: ferroelectric Activity ROADMAP
Basic understanding
Hf-based stacks
Zr-based stacks
Materials research
Vertical plug device
3D FeFET
Other applications
2019 | 2020 | 2021 | 2022 | >2022
MLC assessment
In-memory computing
Steep slope FeFET
In logic program
Reliable trench cell
Reliable plug cell
In Machine Learning program
1st MLC assessment ready
Nucleation dynamics
Hf-based FET
2D FeFET
Optimized FET
Trapping-switching interaction
Alternative ferroelectric
High endurance stack
Vertical trench device
Ultimately scaled cell
Final report
Notes: Materials optimization continued (nanograin); 2D FeFETwork ramped up, 3D plug cell continued but trench is final goal (also MLC analysis)

## Slide 49: Key messages
Continued effort on fundamental understanding : variability & reliability
New materials under way (dopants, non-Hf)
MIM capacitor work added
3D FeFET work continued on trench (large window/MLC/vertical scaling)

## Slide 51: NAND replacement
?
Benefits
Vertical device: larger FE area => many domains => MLC?
Lower voltages and power
Faster W/E => throughput
Cost (MV, no separate selectors, potentially larger density for trench, no curvature)
Challenges:
Vertical uniformity of FE layer ?
Endurance (memory type) / MLC (storage type) not obvious
Huge market potential, high density entry level...

## Slide 52: NOR/AND
?
Benefits
Vertical device: larger FE area => many domains => stability
Lower voltages, power
Faster W/E => throughput
Challenges
Maturity
Enough differentiator wrt floating gate/NROM?
Few NOR players (Cypress, Macronix, Micron)
Smaller market potential, lower density entry level but still (relatively) high entry cost

## Slide 53: embedded NVM
?
Benefit
Finfet contains sufficient domains
Lower voltages, power
Faster W/E => throughput
Cheaper than STT
Challenges
High temperature/robustness (automotive)
New market needed (IoT?)
Strong IP confinement (FMC/GF)
Small-medium market potential, lower density entry level but still high entry cost
9 patent apps

## Slide 54: machine learning
?
Benefit
Finfet contains sufficient domains
Low power
Strong non-linearity (Ion/Ioff)
Challenges
Accurate analog programming? (not always needed)
Other device options get more traction
Large market potential, lower density entry level but still high entry cost
Purdue, IEDM18 (see also Notre Dame)

## Slide 55: FPGA
Memory
Memory
M
FeFET or FeCAP possible
Regular NMOS
FeFET
2T version (PSU patent)
2T1C version (imec patent appl.)
1
2
3
4
2
1
3
4
5
IGZO
Medium market potential, low density entry level but still high entry cost
2 patent apps
Notes: Defense, military systems, telecom = signal integrity/decoding towers and cablebox at home, finance, medical devices.. FAST and reprogrammable on the fly
Ghz range for processor, but 1 operation at a time (sequential)  FPGA can work in parallel so you can send a lot of data in real time (ex. HDMI)

## Slide 56: summary
application | market size | entry cost | main benefit | main issue
NAND | ++ | ++ | NAND-like | density (MLC)
NOR | - | + | more scalable | entry cost
DRAM/SCM | ++ | ++ | lower cost | endurance
Embedded NVM | - | + | lower voltage | high T behavior
Machine learning | + | + | low power | integration
Steep slope logic | +++ | ++ | still a MOSFET | hysteresis
FPGA | - | + | direct boot | cost