## Slide 1: 3D XPoint™ Technology
DerChang Kau, Max Hineman, Davide Fugazza, Kumar Virwani, Prashant Majhi & Al Fazio
WW50.4/2018
3DXP @ Intel
Architecture
Read / Write
SD, PM and Electrodes
Roadmap & Scaling
BiSM

## Slide 2: 3D XPoint™ Technology Development Evolution
4Kb 200nm feature, 2-Mask Sublitho Heater
Damascene PM Subtractive SD
2003~2006 Santa Clara, CA
SD only
PM
SD
TiSiN
TiAlN
TiAlN
SXP cell
64Mb 180nm ½ Pitch 6-Mask Sublitho Heater Damascene PM, Subtractive SD
2007~2009 Santa Clara, CA
PM
SD
TiSiN
C
C
X-section along ROW
W
C
SD
PM
Mid Electrodes
64Mb 100nm feature, 2-Mask
Self-Aligned, Subtractive Cell
2010~2011 Agrate, Italy
64Mb 50nm ½ Pitch, 2-Mask
Dual Deck, Self Aligned Subtractive Cell
2012~2013 Agrate, Italy
128Gb 20nm ½ Pitch 7-Mask
Dual Deck Self Aligned Subtractive Cell
2013~2018 Boise, ID
256Gb 20nm ½ Pitch 13-Mask
Quad Deck Self Aligned Subtractive Cell
2015~2019 Lehi, UT & Rio Rancho, NM
512Gb 14nm ½ Pitch 13-Mask
Quad Deck Self Aligned Subtractive Cell
2019~2020 Rio Rancho, NM

## Slide 3: 3DXP Process Architecture Overview
3DXP is a back end memory technology. CMOS enabling array access and control logic plus I/O are completed prior to array processing.
Due to properties of the memory materials array processing is done at temperatures consistent with Cu interconnect requirements.
The cross point structures are stacked to achieve higher memory density at a given die size.
The top metal is a final interconnect layer (primarily bussing) and enables cost effective wirebonding.

## Slide 4: Memory Cell Architecture – High Level
The cross point is created by cutting wordlines in a line/space pattern without the bitline conductor.
Then after gapfill and planarization to expose the top electrode, depositing the bitline conductor and cutting bitlines in a perpendicular line/space pattern stopping above the wordline conductor to leave a square memory cell stack at the intersection and a true 4F2 cell size.
Pattern scaling due to a simple line/space pattern moves from spacer based pitch doubling to spacer based pitch quad. No multiple patterning required.

## Slide 5: Patterning
The wordline (and bitline) etch process is split in two to avoid cross contaminating the PM and SD as the cross contamination degrades the response of each film. A liner is used to protect the PM during the SD etch and in the case of the wordline – the W etch.
The liner between the first and second “partial” etch processes is a bilayer, nitride is required for adhesion of the oxide liner to the carbon electrodes and the oxide is required for durability through the W etch. A seal film is then applied prior to gap fill to protect both PM and SD.
Gap fill between the array pitch lines requires > 10:1 AR and retrograde capability. Using spin on, need to control thermal energy transfer from a bit being written to the neighboring bits.
Ambient control is used (N2 purge of FOUPs, EFEM) is used to avoid air exposure of PM/SD. The film composition is modified through the etch/clean sequence (undesirable) and this modification is exacerbated by ambient exposure.

## Slide 6: How SXP cell works
Demarcation Read on Quasi-static I-V curves
STEM-ADF: High throughput for c/a fraction
Fully crystalline (c1)
a corners
(c  0.85)
Fully a
(c  0)
Reset Operations : Melt-quench vitrification to produce glassy PM / high threshold switching state
Key attributes: IRESET, Vt,RESET
Set Operations: Solid-state recrystallization to produce crystalline PM / low threshold switching state
Key attributes: ISET, Vt,SET, 𝜏SET
Amorphous (a)
Amorphous
SET
State
RST
State
On-bias
a.k.a.
Snapback NDR
Off-bias
a.k.a.
SubVt
VDM

## Slide 7: Components in a 3DXP cell
SD: Selector
PM: Storage
Electrodes: Physical Barrier and Electrical conductor

## Slide 8
(120nm)2
(45nm)2
J [A/nm2]
V [Volts]
Full-STACK
Electrode only
V [Volts]
J [MA/cm2]
48
32
16
64
Bottom
Electrode
Top
Electrode
BE
TE
Near Threshold
BE
TE
Threshold,
(positive feedback)
Snapback Regime
TE
BE
Ambipolar
On-state
1.7
BE
TE
3.0eV
4.4eV
φB=.85eV
EF
1.7eV
TE
BE
SubThreshold
PF conduction
Best Know SD Model
Selector
Bi-directional I-V

## Slide 9: SD Material Exploration
SD L0 physical and L1E Electrical success criteria corresponding to DTS (with examples from SDd experiments)
SD Material system explored include: SD0 (GeAsTe, aka TAG), SD1(GeAsSe, aka SAG), SD2 (POR, SiGeAsSe, aka SiSAG), SD3 (PF including InSAG, GaSAG, doped GexSe binary and doped oxide)
VT@L1E Vs. EGap@L0
Alloy [25 nm] | L0 |  |  | L1E |  |  |  | 
 | Thermal Stability |  | BG | VT,FF [V] | VT@1E3 cyc [V] | Ileak @85%VT [nA] | VT drift (mV/dec) | Bounce [mV/s]
 | 320C | 375C | Egap [eV] | < 7.9 | > 3.6 | < 30 | < 20 | < 50
goal | no rough. | info |  |  |  |  |  | 
SDdelta.A001 |  |  | 1.95 | 7.15 | 4.6 | 61 | -4.4 | 54.5
SDdelta.B001 |  |  | 1.97 | 6.37 | 4.23 | 14 | -1.9 | 59.7
SDdelta.B002 |  |  | 1.97 | 6.36 | 4.21 | 17 | -5.9 | 69
SDdelta.B003 |  |  | 1.97 | 6.12 | 4.33 | 6 | -5.1 | 67
SDdelta.B004 |  |  | 1.96 | 6.17 | 4.35 | 5 | 4.2 | 70
SDdelta.B005 |  |  | 1.95 | 7.41 | 4.27 | 6 | -8.6 | 68
SDdelta.B006 |  |  | 1.9 | 8.23 | 3.84 | 11 | 8.9 | 102
I ~ e - Eg/kT
As2Te3  As2Se3
Si  In2Se3
Ge

## Slide 10: PM: Atomistic Switching Model (Ge2Sb2Te5 example)
PM
SD
TE
ME
BE
FCC
Amorphous
Crystalline
10% structural vacancies result in localized states near LP band, exhibiting p-type semiconducting characteristics
Over- and under-coordinated Tellurium lead to defects/traps
Glassy PM exhibits threshold switch characteristics
Ec
Ev
Ef
E
CB
VB
Te
V
Ec
Ev
Ef
E
CB
VB
Te
HCP

## Slide 11: PM Material Exploration
PM L0 physical and L1E Electrical success criteria corresponding to DTS
PM Material system explored PM0(GeSbTe a.k.a. GST), PM1(InSbTe a.k.a. IST), PM2(In doped GST or I-GST) and PM3 (PF including Y-GST, Ga-GST, Sc-GST and doped GeSb at IMI)
Alloy | L0 |  |  | L1E |  |  |  | 
 | Phase Segr. (XRD) |  | BG | RVIR [KW] | RSET [KW] | VT [V] | VT@3uA [V] | Set 'speed' [ns]
 | 320C | 375C | Egap [eV] |  |  |  |  | 
goal | single | single |  | < 10 | < 4 | info | > 1.2 | < 500ns
PMd.A001 |  |  |  | 12 | 1.9 | 1.36 | 1.20 | 200
PMd.A002 |  |  |  | 9.6 | 2 | 1.39 | 1.21 | 200
PMd.A003 |  |  |  | 10.7 | 2.2 | 1.50 | 1.40 | 200
PMd.A004 |  |  |  | 13 | 2.2 | 1.45 | 1.50 | 200
PMd.A005 |  |  | 0.77 | 15.8 | 2.1 | 1.56 | 1.56 | 200
speed [ns]
VT [V]
Eg [eV]
Segregation
(XRD, 375C)

## Slide 12: Role of Electrode
Graphitic carbon servers two roles
  Physical barriers to eliminate cross contamination between PM, SD and WL/BL metals during manufacturing and product operations
  Heating elements for phase change
Irreversible resistance change subject to thermal budget
Electrode Success Criteria
Interfacial liner, W, is needed to improve contact specific resistance to PM.
Component | L0 Spec (mW∙cm) | 
Electrode (El.) Bulk resistivity | As dep | 1~200
 | 300C cycled | 1~30
 | 600C cycled | 1~2.5
E/PM Interface | < 10MW∙nm2@1mA | 
E/SD Interface | < 100MW∙nm2@1mA | 
C/PM/C
C/PM/W/C

## Slide 13: Roadmap and Pathfinding

## Slide 14: 3D XPoint™ POR Roadmap
Technology |  | 10s | 20s | P1240 | P1241
½ Pitch [nm] |  | 20.5 | 20.5 | 20.5 | 14
Effective F [nm] |  | 14.5 | 10.25 | 10.25 | 9.8
Immersion layer |  | 7 (4 PD) | 13 (8 PD) | 13 (8 PD) | 13 (8 PQ)
Product |  | S15 | S26 | ALF32 | ATF-64
Platform PRQ |  | Eo’18 | Eo’19 | Eo’20 | Eo’21
Capacity [Gb/die] |  | 128 | 256 | 256 | 512
Read BW [MB/s] |  | 1600 | 1600 | 3200 | 4800
Write BW [MB/s] |  | 550 | 800 | 1100 | 2200
Read E [pJ/b] |  | 71 | 52 | 39 | 28
Write E [pJ/b] |  | 170 | 118 | 92 | 77
Power [W] |  | 0.9 | 0.75 | 1 | 1.15
X8 I/O Interface |  | DDR4 | DDR4 | DDR5/LPDDR5 | LPDDR5+
DDR Rate [MT/s] |  | 1600 | 1600 | 3200 | 4800
Chop | Capacity [Gb/die] |  |  | 128 (2D or 16P) | 256 (2D or 32P)
 | Read BW [MB/s] |  |  | 3200 | 4800
 | Write BW [MB/s] |  |  | 1100 or 550 | 2200 or 1100

## Slide 15: P1241+ Scaling Enablers
PM pathfinding:
Need 30% higher due to vertical scaling
Need 50% 𝜏nuke reduction due to lateral scaling
SD pathfinding:
15% 𝜎VT reduction (Empirical)
Exploit Memory window (Empirical)
Seeking opportunity in Drift Reduction (Empirical, SD3 L1E)
Patterning:
Etch/cleans improvements to minimize modification of the PM/SD compositions.
  Known improvements by wafer ambient control – minimizing exposure to atmospheric O2, H2O with tool modifications
Etch improvements for profile in the multilayer.
  Initial work with modified insitu depositions (newer tool configuration) has shown capability at 14nm.
Liner/Seal/Gap Fill:
Improved step coverage of liner/seal. These are currently bilayers (nitride/oxide) to ensure adhesion to cell and durability/mechanical stability.
  The oxide is good step coverage (ALD) the nitride is a PECVD (pulsed plasma) film with poor step coverage. Directions we need to explore are halide free, low temperature ALD films.
Improved durability and barrier capabilities of the liner films (H & O)
  Replacement of oxide w/ metal oxides (Al, Hf) have shown improved durability, but add significant complexity to etch at 2nd cut.
Lower thermal conductivity gap fill to reduce thermal cross talk
  Work with the supplier on modifications to the c-doped oxide SOD, higher C content, was in progress. Mechanical stability and etch impact at 2nd cut are additional risks.

## Slide 16: P1242 definition and Beyond
Four options being analyzed
  Option-1: 4 Deck Cross Point Array Stack / PQ, F=10.25nm – Feff = 5.125nm
  Option-2: 3D Tier w/o TFT  not scalable ( = dual deck cross point array)
  Option-3: 3D Tier with Pillar Select X’tor, 2 bits per pillar each tier (Doublet)
  Option-4: 3D Tier with Pillar Select X’tor, 1 bit per pillar each tier (Singlet)
3D Tier Doublet example
Pillar Select Transistor
WL Comb:
2 WL Decoders per Tier
Pillar Doublet
2 bits per pillar each tier
WL:
Tier Bias
BL:
Pillar Bias
PS: Pillar Select

## Slide 17: Enabling technology needed for 3D-Tier 3DXP
Pillar Select Transistor
5V, 110uA GAA TFT (H75nm , W270nm , T42nm , S62nm), On-Resistance 3KΩ, off leakage < 10nA
Low thermal budget for BEOL integration
Contact resistance (X2) < 300Ω (to BL & pillar)
Tier Array Process
1st cut is similar to 3D-NAND’s, either replacement vs. subtractive for WL metal
ALD Chal, Carbon & W lamina – maintain composition uniformity at high aspect ratio for chal films
Recess process control: thickness control impacts - sigma in Vt, delta Vt, Iprogram (heaters) ~ endurance/WD
2nd cut etch capable of W lamina removal over entire height of bit (vertical lamina) without chal damage
Replacement Pillar Metals, liner with good good contact to TE carbon and pillar select source/drain and barrier properties for W dep.
Parameter | 3D XP (3D Tier) | Poly-Si | Poly Ge / III-V | Oxide (ZnO; IGZO) | 2D TMD
Ion Lin (uA) @ (Vg-Vt)=4V; Vd = 0.3V | 110 uA |  |  |  | 
Operating Voltage | 5 |  |  |  | 
Ioff (nA) | <10 (Vg=0) |  |  |  | 
Contact Resistivity (MΩ.nm2)# | <2 |  |  |  | 
Transistor Lg (nm); W (nm) (GAA) | 75; 600 |  |  |  | 
Transistor EOT (nm)* | 10 |  | HiK | HiK | HiK
Transistor Mobility (cm2.v.sec) | >35 |  |  |  | 
Reliability (BTI, ??) | TBD |  |  |  | 
Process Compatibility (Max Temp?) | 430 C @ 3mts 300 C @ 1hr |  | High DT ? | H+/O barrier | 
CMOS | Yes for BiSM |  |  | pTFT poor | No process
# Based on Rcontact ~ 10% of R(total) => 2Rc < 300 ohm
* Based on Si with SiO2 gate dielectric; HiK will likely be lower EOT
PST Success Criteria and Preliminary Survey

## Slide 18: BiSM

## Slide 19: Introduction to atomistic memory switch with Built-in Selector a.k.a. Built-in-Select Memory (BiSM)
GeSe2
As2Se3
SD.G09
1.76eV
SD.G05
1.9eV
1.75eV
1.75eV
Conceptually, it is a 3D XPoint™ technology.
  Physical construction of BiSM array is BEOL 3D stackable X-Y cross point array comptatible with mainstream CMOS.
  Read/Write access deploys threshold selecting one cell while inhibiting the rest of cells in an array with subthreshold bias.
The best known ∆VT physics is an electrochemical potential modulation subject to mass transport by polarity.
VT [mV]
VT [mV]
Deck 0
Deck 1
Deck 0
Deck 1
Beginning of Life
After 4M cycles
Sigma of Bit
Set
Sigma of Bit
Reset
Set
Reset
Set
Reset
Set
Reset
  Bipolar memory switching with elemental segregation are observed in wide range of Chalcogenide glasses
A VT window VT) is observed by applying programming pulses with opposite polarity
TE. BE
Se
As
Ge
TE. BE
SD1 alloy

## Slide 20: Switching vs. Disturb: Risk and Mitigation
50%
100%
SET
RST
Disturb curve Vs. Duty cycle @V/VT ~0.65
Memory Switching mechanism is also subject to Read/Write inhibiting disturb
Can BiSM hold off cross point disturb w/o a selector
Disturb time Vs. Norm. Stress
Inverse correction between Time-to-fail and subVt leakage suggests segmentation of underline mechanisms
Seeking BiSM material properties to improve R/W disturb immunity
Constant ratio of TTF : Ileakage-1
suggesting “QBD” mechanism incentivizes for switching physics development

## Slide 21: Supporting Materials

## Slide 22: Value Proposition of Built-in-Select Memory Architecture & Motivation
Value Proposition (ref. tech: 3DXP)
  No cross-contamination between Memory and Selector materials
  Lower cell aspect-ratio (10:1 5:1)
  Lower programming current  relaxes metal (WL/BL) requirements and array capacitance
  No nucleation required, fast write (40ns)  an opportunity for symmetric memory access (read/set/reset)
  Perceived as 3D-Tier integration Friendly
BiSM
3DXP
3D-tier
Motivation
  Bipolar memory switching with elemental segregation are observed in wide range of Chalcogenide glasses
  Threshold switching characteristics are not limited to Chalcogenide glass. It has been sighted also with other binary oxide, such as NbOx, SiOx and etc.

## Slide 23: L0/L1D Physical characterization
1. L0: As-deposited film char: Material intrinsic properties
2. L1D ’movies’: Composition transfer function & bit-2-bit
Category | Technique | Metrics (m, s)
Avg. Composition | XRF, ICP-OES XRD | Element % Match peak ratio x-wafer
Process Int. compatibility | EDS ‘wrikle’ test (200C-340C) | El % std dev (eq. bit-2-bit) ‘bubbling’ onset
Electrical proxy | Rs Vs T scans [30C-650C] UV-vis spectroscopy TDTR [SC9] | R(post-DT)/R(asdep), EA,… Opt. Egap (pre-/post-anneal) Thermal Resistance
Category | Technique | Metrics (m, s)
Cell Health (composition) | XRF, EDS, (XRD) | Element % Stack x-contamination
Cell morphology | STEM | CDx, CDy, thicknesses
As deposited Elemental mapping

## Slide 24: L1E/L3 Physical characterization
3. L1E/L3, including EoL & reliability (FM-TEM): Physical root-causing to intercept (i) PE, (ii) PI, and (iii) TD changes
4. Metrology and methodology main gaps and plan
Category | Technique [multi-bit cut] | Metrics (m, s) [Automated]
Sample preparation | FIB ‘grounding’ method | Output: Reduce beam sensitivity artifacts on element distrib. ^
Physical Structure | STEM | CDx, CDy, thicknesses
Composition/x-contam. | EDS, (EELS) | Element % vertical/lateral elem. gradients
Crystallinity / (amorphous) | STEM-ADF (coarse resol.) NBD (fine) | Crystalline fraction Phase determination
Atomic resolution | HR-TEM | CDx, CDy, thicknesses Phases location
Gap/Challenge | Comments and current plan
Chal. selector fingerprint (elem. profile, bonding, band align.) Vs. e-stimuli | Collaboration w/ OR-CQN started w.r.t. APT and XPS/IPE Raman also being evaluated (TBD)
Mobile species detection | N/A

## Slide 25: Moat isolated Thin Film Device for RRAM/Selector L1E

## Slide 26: Connectivity of “Bottom” Electrode
Connectivity below top electrode
  DUT load-line, such as Ballast Resistors, MOSTs
  Proximity heaters
  And other active components
Options including
  “C-pad” – 10~100K:1 high “R” ratio
  Budding contact to backside
  Poor man’s Anti Fuse
Basic Device Formation

## Slide 27: DUT examples
TE
BE
BE2
BE1
BE3
BE4
TE
Heater
Heater
TE
GND
Control
TE
“P”
Cntl-P
Cntl-N
“N”
TE
GND
Control
Heater
Heater
To exploit Intel’s CMOS power house for thin film device characterization in 10s nm regime without thin film patterning.
The CMOS base technology is used for DUT loadline, electrical/thermal stimuli and sensing metrology.
TE
Kelvin
Probe
GND
Control
Kelvin
Probe