## Slide 2: Strategy
First establish baseline and optimization at L0/L1E site
PM: POR PM2A3
  Ge-Sb optimization
  Replace In with Y, then Ga
  Explored other host matrix such as GeSb
SD: POR SDV12
  Si-SAG optimization
  Remove Si for optimized SAG with In doping
  Replace In with Ga
  Explore other host matrix such as oxide

## Slide 3: PM Milestone and Decision Point
Establish Baseline & fingerprint (PM2A3) & Ge-Sb Optimization
  IMI based L0 and L1E Metric is used
Phase–I: Y-GST
  Deposit a PM2A3-like GST matrix with 1 to 9% Y substituting In
Phase–II: Ga-GST
  Same Strategy to Y-GST.
Phase–III: Ga-GeSb
  GeSb based publication
Phase–IV: Sc-GST
  (this is questionable based on paper published)

## Slide 4: SD Milestone and Decision Point
Establish Baseline & fingerprint (SDV12) & Optimization (V16-like)
  Memory effect optimization (need L1?)
Phase–I: In doped SAG (Si elimination)
  Sigma improvement, drift optimization  RWB improvement
Phase–II: Ga doped SAG
  All Phase–I + leakage improvement
Phase–III: doped oxide
  Aiming at flatten cycling evolutions curves.
  Compostions are yet to be explored.

## Slide 5: JDP Learning

## Slide 6: JDP Campaign priorities & planning
Tentative plan, could change soon and frequently based on results and priorities

## Slide 7: PM exploration in short term: Y-program
Status of learning on Y-GST:
  On the basis of very preliminary and few:
    EG high enough w/ low Y% in the Sb-rich EoL region
    Just only one CLV data available
Strategy:
  Deposit a PM2A3-like GST matrix with ~3% Y substituting In to check the value at L3
  Extend the mapping moving to the 4C
Integration:
  Trials on going to find the path for etching avoiding the pronounced tapering
SD punch thru
Agotti/Pavan
PM2A3
Y-GST

## Slide 8: PM exploration: further options
Standard slope
~ 1sigma/100mV
GST Corners
Sb poor/ Te rich
Limited Degrees of Freedom w/ 3C
Alternatives to paths to Y:
  Optimization of the GST matrix  corner (Ge-Sb ratio) is suggesting some room of improvement w/ Sb-poor GST compared to PM2A3; WLR pending
  Ga-GST  Ga could play, electrically, the role of Indium, but it is expected to be easier for integration (higher Ga content allowed?); sequentially to Y-GST in the 3C, wk#21
  GaSbGe (GSG)  pro: Scalable due to high Tx, low volume expansion, easier to etch (no In); cons/unknown: GaSb phase separation? VT-set speed correlation?; exploration can start the completion of GST corners (tentatively: wk #21)
  Sc-GST  only suggestions from literature and atomistic simulation results, just lighter than Y (easier sputter etch), but not so strong value to support targets purchase now (new assessment after Y data)

## Slide 9: SD campaigns in the short term:
DTS goal
Alloy6
SD.K2
CR5.3
SD.K1
DVt (1 ms)
Focus on In-SAG system actually privileged alloy for some upsides:
  Sigma  down up to 80/90 mV
  SSM window  > 1.3 Volts
  Memory Effect  ~400mV, although degrading w/ cycling
SDK.2 candidate to meet the SSM window:
  SDK.2 w/ 9% will be installed in the MUM500 from week#17 w/ 2 SDK.1 mono-tgs
  K* campaign still under completion exploring As% reduction possibly beneficial for SSM window  Readout wk#21
G* campaign is exploring further As% reduction, in addition to:
  The role of each Ge, As, Se thru extended mapping
  Stair case emulation of the programming induced segregation thru the bi-layered SD
Large In-SAG targets fabrication will focus on SDK2
  2 large tgs of V16 delivered
Link to all presentations

## Slide 10: SD: medium term activity  Ga-SAG (O* campaign)
Ga-SAG value proposition:
  To catch all the benefits of In-SAG (namely: good sigma, good SSM window and controlled drift), w/ plus: facilitate the integration substituting In with Ga (Gallium based SD expected to be easier for dry etch and pattern as compared to Indium based SD)
Ga2Se3 target available, installation after G*
Strategy:
  Replicate the K* camp in a 3C with Ga sub. of In by means of As2Se3, Ga2Se3 & Ge
  Replicate the K*+E* camp in a 3C with Ga sub. of In by means of As2Se3, Ga2Se3 & GeSe4.5%As
News:
  Just signed the purchase of a new 4C: this will allow to merge the two strategy speeding up the exploration!
Ga2Se3
Ga substitutional to As
Ge skew in the ~15-20%
Ga skew in the ~5-15%
Ge skew in the ~15-20% (@ lower As)
Ga skew in the ~5-15%
Keep As/Se lower w/o increased Ga + Ge
Targets config

## Slide 11: SD: medium term activity  Ga-SAG (O* campaign)
Ga-SAG value proposition:
  To catch all the benefits of In-SAG (namely: good sigma, good SSM window and controlled drift), w/ plus: facilitate the integration substituting In with Ga (Gallium based SD expected to be easier for dry etch and pattern as compared to Indium based SD)
Ga2Se3 target available, installation after G*
Strategy:
  Replicate the K* camp in a 3C with Ga sub. of In by means of As2Se3, Ga2Se3 & Ge
  Replicate the K*+E* camp in a 3C with Ga sub. of In by means of As2Se3, Ga2Se3 & GeSe4.5%As
News:
  Just signed the purchase of a new 4C: this will allow to merge the two strategy speeding up the exploration!
Ga2Se3
Ga substitutional to As
Ge skew in the ~15-20%
Ga skew in the ~5-15%
Ge skew in the ~15-20% (@ lower As)
Ga skew in the ~5-15%
Keep As/Se lower w/o increased Ga + Ge
Targets config