## Slide 1: BiSM, an Alternative Memory
DerChang Kau, Prashant Majhi & Al Fazio, WW31.4, 2019 @ MAT-SC
Introduction
Value Proposition
Silicon Performance
Array Architecture
Critical Path to a-Product Definition

## Slide 2: Introduction to BiSM
In a typical selector-less (0S1R) cross point memory array, leakage and disturb fundamentally limit the density and usability of the technology. BiSM is working well because of the built-in selector to reduce leakage for high density and to increase immunity to read/write disturbance for nonvolatility; hence Built-in-Selector Memory, a.k.a. BiSM, is coined.
Pulse Polarity
TE
BE
SD
A SD only memory cell sandwiched between a X-Y cross point, BEOL stackable, compatible with mainstream CMOS.
VT,High
VT,Low
S15B SD-only, lot 8792062, 18nm SDd ver 4
Positive
Write
Negative
read
Negative
Write
Negative
read
−/−
+/−
Write/Read
Polarity
900mV
+/+
−/+
VTH [mV]
σ of bit distribution
It exhibits a window by applying programming pulses with opposite polarity.

## Slide 3: A Brief History
Subsequently, with 3DXP process improved, BiSM VT window became more evident. The concept of BiSM was conceived in the JDP with Micron and worked on jointly by both companies under the research initiative called Self-Select Memory, a.k.a. SSM.
In June, 2013, as 3DXP dual-deck development shifted to high gear, a subtle BiSM “window” was sighted by Arjun Kripanidhi at SC9 Device Lab.

## Slide 4: Value Proposition
  Simplified manufacturing with PM removed lower cell aspect-ratio No cross-contamination between Memory and Selector materials
  Improved performance and reliability
  Elimination of PM reliability constraint
  Lower write current to relaxes WL/BL requirements and array capacitance
  Fast write; no crystallization required An opportunity for symmetric memory access (read/set/reset)
  Theoretically simplified cell enables
  Tier Architecture (3D NAND like)
  to lower manufacturing cost
BiSM
3DXP

## Slide 5: 1st and 2nd cut profile CR6.5 demonstrated >70% PG4 structure yield & PG4 capable RWB
MTS Metric | SPEC | POR | FWD
HM thk (nm) | 18 | 17 | 23
W top CD (nm) | 21 | 18 | 22.5
W bot CD (nm) | 17.2 | 14 | 18.5
TEC CD (nm) | 21.3 | 18 | 19.2
SD top CD (nm) | 21.5 | 22 | 16.5
SD bot CD (nm) | 23 | 26 | 18.5
SD SWA (degree) | 89 | 84 | 87
Specs | MTS Metric | SPEC | POR | FWD
First partial | SD top (nm) | 18.1 | 16.3 | 15.6
 | SD bot (nm) | 18.9 | 24.9 | 18
 | SD SWA (degree) | 89 | 79 | 87.5
Last partial | SD top(nm) | 18.1 | 16.1 | 15.6
 | SD mid(nm) | 18.5 | 17.2 | 18
 | SD bot (nm) | 18.9 | 17.8 | 18.1
 | SD SWA(degree) | 89 | 88 | 87.5
 | W Sep (nm) | 20.8 | 18.7 | 18.5
 | W Bot (nm) | 21.2 | 22.3 | 22
2nd cut (single step)
July/12/2018

## Slide 6: Read/Write
Symmetric write pulses for set and reset operations: 44ns@±45µA
Read is identical to 3DXP (40ns pulse)
Read Window Budget (∆VT): 200 mV @ 5E-4 RBER
The best known ∆VT physics is an interfacial modulation subject to mass transport by E-field at an elevated temperature.
  Bipolar memory switching with elemental segregation are observed in wide range of Chalcogenide glasses

## Slide 7: Retention
85C 40C
10y
3m
2d
Window closure
EA ~ 1.25 eV
Window-based retention: EA in ~ 1.25 eV range; ~ 1 year retention @ 85C  Mainly due to lower drift of reset state. Additional segmentation wip.
@180C
-- 1ms
1e3 s
1e4 s
SET
RST
0193532w10 SDk-A14, r5.3
SET/RST Distrib. Vs. T-bake
The retention characteristics, both set and reset shifting up, suggests the dominant retention mechanism subject to structure relaxation at temperature range explored.
85C
5years

## Slide 8: Write Endurance
Iprogram – the same as 3DXP, subject to Tg
RWB – no worse than 3DXP
Read/Write Latency – no change
No window closure of 2K bits up to 2M FW cycles @ 10ms ipd, low ED
Scaling Expectation (No Scaling Data)

## Slide 9: Bipolar decoder architecture – Selected BL Path Shown
Unipolar
110Å TWN + P
VSS
AXN=VPPs
VSS
VSS
VSS
VPPs
VSS
ALF32
VPPs
LBL
VSS
VSS
VPPs
VSS
AXN=VPPs
VSS
HNREG
VSS
VNN
S24S
VPPs
VSS
LBL/LWL
BiSM32
VPP
VPP
VPPs
VSS
VPP
VSS
HNREG
AXN=VPPs
VPPs
VPPs
LBL/LWL
Bipolar
110Å TWN + P
2 extra global Xtrs.
Extra Xtrs. in tile predec
Bipolar
160Å TWN + tgP
VT: 1.2V @ 9.3 VB for TWN
9.6V compliant DR
AXN/HNREG Mux/tile

## Slide 10: Die Size and Energy Assessment
Architecture | Decoder | CMOS and Interconnect | Density [Gb/mm2] | Write [pJ/b] | Read [pJ/b] | Gap [%] |  | 
 |  |  |  |  |  | Density | Write | Read
ALF32 (POR) | Unipolar | P1240.0 | 1.28 | 104 | 44 |  |  | 
S24S | Bipolar | P1240.0 | 1.16 | 154 | 55 | 9% | 48% | 25%
BiSM32 | Bipolar | P1240.0+TGcMOST | 1.00 | 107 | 47 | 23% | 3% | 7%
S24S decoder creates big energy gap and lowers density
BiSM32 decoder Arch bridges the energy gap, but reduces density further.
Density gap of BiSM32 can be recovered by improving CMOS performance.

## Slide 11: Assessment & Critical Path to a-Product Definition
BiSM technology presents an opportunity for higher speed SCM with simplified manufacturing without obvious technology showstopper. It solves known 3DXP issues, likely introduces others which we are yet to fully see. Scaling is yet to be demonstrated.
Optane™ Memory Media has Circuit Under the Array (CUA) to reduce die size. The bidirectional circuit topology of BiSM is a key constraint of CUA for its ability to match or to beat present Optane™ product cost, despite the improved write latency. Currently die size is prohibitive with the speculative TGcMOST design rule. Efficient tile design is a key challenge to product viability.
Besides developing a smaller footprint transistor and/or inventing new bipolar decoding scheme, a more fundamental issue is high voltage supply rail constraint, which is driven by (voltage) window budget. Integrating new material and/or read/write algorithm to reduce BiSM VT sigma, drift and shift are the key enablers for voltage reduction.
Competitive landscape – We believe that Micron is pursuing this technology at a priority over the current Optane™ approach. Also, in the research segment of atomistic switches (intel sponsored or public domain), discussions and disclosures on the sighting of similar behavior are merging.

## Slide 12: BiSM Value Proposition (ref: 3DXP)
  Theoretically simplified cell enables
  Tier Architecture (3D NAND like)
  to lower manufacturing cost
BiSM
3DXP
  Simplified manufacturing with PM removed lower cell aspect-ratio (from 10:1 to 5:1) No cross-contamination between Memory and Selector materials
  Improved performance and reliability
  Elimination of PM reliability constraint
  Lower write current to relaxes WL/BL requirements and array capacitance
  Fast write; no crystallization required (from 240ns to 44ns set pulse) An opportunity for symmetric memory access (read/set/reset = 40/44/44)