## Slide 1: BiSM March Discussion
DerChang and Fuga, WW13.5/2019
Recap of Feb Review
Three physical models to be segmented
Fingerprint matching exercise
Fast-Fail decision process

## Slide 2: BiSM WW10 Recap
Gaps
  3X gap in Read Disturb count
  No gap in Inhibit disturb
Type of disturb | Spec | 3.54σ Capability (t1/ipd/t3)
E3 Read Disturb | 130K reads | 40k (10s/1us/1us)
E3, SET inhibit | 2.5M inhibits | > 2.5 M (1us/1us/1us)
E1, RST inhibit | 2.5M inhibits | > 2.5 M (1us/1us/1us)
E3 , Read inhibit | 140M inhibits | > 200M
Program Polarity Matches Mass Transport
V-NUI [1]
Segregation Index
N
Virgin
Rev-Disturb
Reverse Bias Disturb exhibits minor atom movement
EFA on SR71 Set(N), Reset (P), & rev-Disturb
V-NUI [1]
N-Pgm
P-Pgm
Virgin
Segregation Index
BL
WL
SD
TE
BE
Vertical El. profile
N-Pgm
P-Pgm
As/Se
N-Pgm
1us
10s
Reverse
Disturb
P-Pgm
n-read
1us

## Slide 3: One of Possible BiSM Model – Mass Transport to flip Heterojunction
(–) Bias Read, same polarity of write
  Space charge region maintained or little change. Potential drop evenly cross Chal glass.
(+) Bias Read, opposite polarity of Write
  Bias initially contributed in compensating built-in potential, shift I-V to right.
Heterogeneous junction model (band offset) supports the observed polarity effect
  Negative Bias increase 𝛘 (more negative)
Vacuum
SAG
C
C
As+/Ge+
0V
(−)
(+)
⊕
⊖
ϕ
⊕
⊖
ϕ
⊕
⊖
ϕ
Neg.
Write
0V
(−)

## Slide 4: Electrical Equivalent Circuit and Possible Underline Physics
A VT window (∆VT) has been observed by applying programming pulses with opposite polarity. One of possible ∆VT physics is an electrochemical potential modulation effect subject to mass transport by polarity.
  Near parallel shift on SubVt I-V on polarity effects
  The equivalent circuit – a programmable battery connected to a Chal Glass Resistor serially
  Programmable battery is formed by the band offset
  Write –Band offset switching subject to mass transport.
  Read – Space Charge modulation results in voltage shift
Likewise a modulation of Schottky barrier at C/SD interface due to SD composition change shares a similarly behavior
In another, this barrier modulation may be achieved by changing charged interface traps, which is deemed a trap generation / annihilation process at both cathode and anode subject to carrier injection direction. (A resemblance of dielectric bias stress effects)
SD Resistor
SAG
C
C
As+/Ge+
0V
(−)
(+)
⊕
⊖
ϕ
⊕
⊖
ϕ
⊕
⊖
ϕ
Neg
Write
0V
(−)
Read Polarity
Prog-Read
Neg-neg
Pop-pos
Neg-pos
Pos-neg
SET
Low-VT
RST
High-VT

## Slide 5: Fingerprint Matching
SubVt I-V can be generally modeled as I = (V-V0)/R·e(V-V0)/𝜎 V0 represents a potential offset of a tunneling junctions in DC charge transport continuity R exhibits an Arrhenius behavior on bulk thermally-assisted hopping, modeled as R0·exp(EA / q·VTH) 𝜎 is escape probability governed by an effective bulk trap density ([nBT]-1)
Manifestation | Structure Relaxation | Mass transport | Interface Traps
Eq. Circuit | FPE or PE (Polarity ind.) | FPE/PE + Battery | FPE/PE + Battery
Expectation of changes from Low to High Vt State |  |  | 
PFA | No change | Visible segregation Bulk: heterogenous Jx Interface: 𝜓ms change | No visibility @ Interface (regardless composition changes)
V0 | No change | ↑ | ↑
R0 | ↑ ([nBT-]1) | Small ↑ may be expected | No change
EA | ↑ (bandgap widening possible) | No change | ↓ when tunneling inj. limited
s | ↑ ([nBT]-1) | unchanged | May change due to ∆trap uniformity
Manifestation | Structure Relaxation | Mass transport | Interface Traps
Eq. Circuit | FPE or PE (Polarity ind.) | FPE/PE + Battery | FPE/PE + Battery
Expectation of changes from Low to High Vt State |  |  | 
PFA | No change | Visible segregation Bulk: heterogenous Jx Interface: 𝜓ms change | No visibility @ Interface (regardless composition changes)
V0 | No change | ↑ | ↑
R0 |  | Small ↑ may be expected | No change
EA | ↑ (bandgap widening possible) | No change | ↓ when tunneling inj. limited
s |  | unchanged | May change due to ∆trap uniformity
Retention characterization will be used for further segmentation.
Mass transport mechanism is expected with longer retention.

## Slide 6: Silicon Results (Changes observed from low VT state to high VT State)
Manifestation | Memory Switching | Reverse Bias Disturb
Eq. Circuit | FPE/PE + Battery | FPE/PE + Battery
PFA | Bulk Segregation | No visible segregation
V0 | ↑ | ↑
R0 | Small ↑ | No change
EA | No change | drops to low temp sensitivity
s | Some ↓ | Some ↓

## Slide 7: Model Segmentation (Base on the changes from low VT state to high VT state)
Results vs. Models
Memory Switching fits the profile of both Mass transport and Interface Traps
Reverse Bias Disturb fits Interface traps model but not Mass transport
Manifestation | Mass transport Predicts | Interface Traps Predicts | Memory Switching |  | Reverse Bias Disturb | 
 |  |  | MT | IT | MT | IT
Eq. Circuit | FPE/PE + Battery | FPE/PE + Battery | √ | √ | √ | √
PFA | Visible segregation Bulk: heterogenous Jx Interface: 𝜓ms change | No visibility @ Interface (regardless composition changes) | √ | N/A | × tbq | N/A
V0 | ↑ | ↑ | √ | √ | √ | √
R0 | Small ↑ may be expected | No change | √ | √ | √ | √
EA | No change | No Change or ↓ when tunneling inj. limited | √ | √ | × | √
𝜎 | unchanged | May change due to ∆trap uniformity | √(?) | √ | √(?) | √

## Slide 8: Fast Fail Logic
If (Disturb gap > Critical point) { /* Success criteria and test metrology validated */
  STOP;
  };
Else {
  Check sensitivity of disturb RBER vs. RWB (Vinh margin);  if yes  go
  Matching Memory Switch and Rev. Bias Disturb with all the best known physics;
  /* Interfacial modulation including mass transport and Interface traps */
  If (memory and disturb share the same mechanisms) {
    STOP; /* Spaces to manage the risk are limited */
    };
  Else {
    Validate Bipolar design and collateral on product landing;
    If (on-par with the incumbent) { /* density, energy */
      Develop pathfinding strategy and scaling enablers;
      };
    Else { Stop and go back to completive analysis } ;
    };
  };

## Slide 9: Backup

## Slide 10
Manifestation | Mass transport Predicts | Interface Traps Predicts | Memory Switching | Reverse Bias Disturb
Eq. Circuit | FPE/PE + Battery | FPE/PE + Battery | FPE/PE + Battery | FPE/PE + Battery
PFA | Visible segregation Bulk: heterogenous Jx Interface: 𝜓ms change | No visibility | Bulk Segregation | No visible segregation change
V0 | ↑ | ↑ | ↑ | ↑
R0 | Small ↑ may be expected | No change | Small ↑ | No change
EA | No change | No Change or ↓ when tunneling inj. limited | No change | drops to low temp sensitivity
s | Unchanged | May change | Some ↓ | Some ↓

## Slide 11
Quantify seg index on disturb of ”confidence” of not being mass transport (memory switching)
RWB risk of ITH reduction
RWB guardband