## Slide 1: 3D XPoint™ Memory Alternative
Team BiSM, WW31, 2019
Incumbent Technology
Introduction to BiSM
Cell Technology
Memory Switching Physics
Array Architecture
Critical Path to a-Product Definition

## Slide 2
Incumbent Technology
Introduction to BiSM
Cell Technology
Memory Switching Physics
Array Architecture
Critical Path to a-Product Definition

## Slide 3: 3D XPoint™ Technology Development Evolution
4Kb 200nm feature, 2-Mask Sublitho Heater
Damascene PM Subtractive SD
2003~2006 Santa Clara, CA
SD only
PM
SD
TiSiN
TiAlN
TiAlN
SXP cell
64Mb 180nm ½ Pitch 6-Mask Sublitho Heater Damascene PM, Subtractive SD
2007~2009 Santa Clara, CA
PM
SD
TiSiN
C
C
X-section along ROW
W
C
SD
PM
Mid Electrodes
64Mb 100nm feature, 2-Mask
Self-Aligned, Subtractive Cell
2010~2011 Agrate, Italy
64Mb 50nm ½ Pitch, 2-Mask
Dual Deck, Self Aligned Subtractive Cell
2012~2013 Agrate, Italy
128Gb 20nm ½ Pitch 7-Mask
Dual Deck Self Aligned Subtractive Cell
2013~2018 Boise, ID
256Gb 20nm ½ Pitch 13-Mask
Quad Deck Self Aligned Subtractive Cell
2015~2020 Lehi, UT & Rio Rancho, NM
256Gb 17nm ½ Pitch 13-Mask
Quad Deck Self Aligned Subtractive Cell
2020~2022 Rio Rancho, NM
512Gb 14nm ½ Pitch
Quad Deck BiSM
2020~2022, Rio Rancho, NM
?

## Slide 4: How SXP cell works
Demarcation Read on Quasi-static I-V curves
STEM-ADF: High throughput for c/a fraction
Fully crystalline (c1)
a corners
(c  0.85)
Fully a
(c  0)
Reset Operations : Melt-quench vitrification to produce glassy PM / high threshold switching state
Key attributes: IRESET, Vt,RESET
Set Operations: Solid-state recrystallization to produce crystalline PM / low threshold switching state
Key attributes: ISET, Vt,SET, 𝜏SET
Amorphous (a)
Amorphous
SET
State
RST
State
On-bias
a.k.a.
Snapback NDR
Off-bias
a.k.a.
SubVt
VDM

## Slide 5: PM: Memory Switching Model (Ge2Sb2Te5 example)
PM
SD
TE
ME
BE
FCC
Amorphous
Crystalline
10% structural vacancies result in localized states near LP band, exhibiting p-type semiconducting characteristics
Over- and under-coordinated Tellurium lead to defects/traps
Glassy PM exhibits threshold switch characteristics
Ec
Ev
Ef
E
CB
VB
Te
V
Ec
Ev
Ef
E
CB
VB
Te
HCP

## Slide 6
(120nm)2
(45nm)2
J [A/nm2]
V [Volts]
Full-STACK
Electrode only
V [Volts]
J [MA/cm2]
48
32
16
64
Bottom
Electrode
Top
Electrode
BE
TE
Near Threshold
BE
TE
Threshold,
(positive feedback)
Snapback Regime
TE
BE
Ambipolar
On-state
1.7
BE
TE
3.0eV
4.4eV
φB=.85eV
EF
1.7eV
TE
BE
SubThreshold
PF conduction
SD: Threshold Switching Model
Selector
Bi-directional I-V

## Slide 7: Role of Electrode
Graphitic carbon servers two roles
  Physical barriers to eliminate cross contamination between PM, SD and WL/BL metals during manufacturing and product operations
  Heating elements for phase change
Irreversible resistance change subject to thermal budget
Electrode Success Criteria
Interfacial liner, W, is needed to improve contact specific resistance to PM.
Component | L0 Spec (mW∙cm) | 
Electrode (El.) Bulk resistivity | As dep | 1~200
 | 300C cycled | 1~30
 | 600C cycled | 1~2.5
E/PM Interface | < 10MW∙nm2@1mA | 
E/SD Interface | < 100MW∙nm2@1mA | 
C/PM/C
C/PM/W/C

## Slide 8
Incumbent Technology
Introduction to BiSM
Cell Technology
Memory Switching Physics
Array Architecture
Critical Path to a-Product Definition

## Slide 9: Introduction to BiSM
In a typical selector-less (0S1R) cross point memory array, leakage and disturb fundamentally limit the density and usability of the technology. BiSM is working well because of the built-in selector to reduce leakage for high density and to increase immunity to read/write disturbance for nonvolatility; hence Built-in-Selector Memory, a.k.a. BiSM, is coined.
Pulse Polarity
TE
BE
SD
A SD only memory cell sandwiched between a X-Y cross point, BEOL stackable, compatible with mainstream CMOS.
VT,High
VT,Low
S15B SD-only, lot 8792062, 18nm SDd ver 4
Positive
Write
Negative
read
Negative
Write
Negative
read
−/−
+/−
Write/Read
Polarity
900mV
+/+
−/+
VTH [mV]
σ of bit distribution
It exhibits a window by applying programming pulses with opposite polarity.

## Slide 10: Bipolar Switching: Program Transfer curves
Program Transfer Curve in the 4 quadrants (I, II, III, IV) by exploiting on-chip dual-polarity.
Ir(i)
Read (i)
Ir(N)
Read (N)
Ir,max
…
@20.5nm
~
~
~
~
I
[POS-POS]
IV
[POS-NEG]
II
[NEG-POS]
III
[NEG-NEG]
[Prg-Rd]

## Slide 11: A Brief History
Subsequently, with 3DXP process improved, BiSM VT window became more evident. The concept of BiSM was conceived in the JDP with Micron and worked on jointly by both companies under the research initiative called Self-Select Memory, a.k.a. SSM.
In June, 2013, as 3DXP dual-deck development shifted to high gear, a subtle BiSM “window” was sighted by Arjun Kripanidhi at SC9 Device Lab.

## Slide 12: Value Proposition
  Simplified manufacturing with PM removed lower cell aspect-ratio No cross-contamination between Memory and Selector materials
  Improved performance and reliability
  Elimination of PM reliability constraint
  Lower write current to relaxes WL/BL requirements and array capacitance
  Fast write; no crystallization required An opportunity for symmetric memory access (read/set/reset)
  Theoretically simplified cell enables
  Tier Architecture (3D NAND like)
  to lower manufacturing cost
BiSM
3DXP

## Slide 13
Incumbent Technology
Introduction to BiSM
Cell Technology
Memory Switching Physics
Array Architecture
Critical Path to a-Product Definition

## Slide 14: 1st and 2nd cut profile CR6.5 demonstrated >70% PG4 structure yield & PG4 capable RWB
MTS Metric | SPEC | POR | FWD
HM thk (nm) | 18 | 17 | 23
W top CD (nm) | 21 | 18 | 22.5
W bot CD (nm) | 17.2 | 14 | 18.5
TEC CD (nm) | 21.3 | 18 | 19.2
SD top CD (nm) | 21.5 | 22 | 16.5
SD bot CD (nm) | 23 | 26 | 18.5
SD SWA (degree) | 89 | 84 | 87
Specs | MTS Metric | SPEC | POR | FWD
First partial | SD top (nm) | 18.1 | 16.3 | 15.6
 | SD bot (nm) | 18.9 | 24.9 | 18
 | SD SWA (degree) | 89 | 79 | 87.5
Last partial | SD top(nm) | 18.1 | 16.1 | 15.6
 | SD mid(nm) | 18.5 | 17.2 | 18
 | SD bot (nm) | 18.9 | 17.8 | 18.1
 | SD SWA(degree) | 89 | 88 | 87.5
 | W Sep (nm) | 20.8 | 18.7 | 18.5
 | W Bot (nm) | 21.2 | 22.3 | 22
2nd cut (single step)
July/12/2018

## Slide 15: Read/Write
Symmetric write pulses for set and reset operations: 44ns@±45µA
Read is identical to 3DXP (40ns pulse)
Read Window Budget (∆VT): 200 mV @ 5E-4 RBER
The best known ∆VT physics is an interfacial modulation subject to mass transport by E-field at an elevated temperature.
  Bipolar memory switching with elemental segregation are observed in wide range of Chalcogenide glasses

## Slide 16: Retention
85C 40C
10y
3m
2d
Window closure
EA ~ 1.25 eV
Window-based retention: EA in ~ 1.25 eV range; ~ 1 year retention @ 85C  Mainly due to lower drift of reset state. Additional segmentation wip.
@180C
-- 1ms
1e3 s
1e4 s
SET
RST
0193532w10 SDk-A14, r5.3
SET/RST Distrib. Vs. T-bake
The retention characteristics, both set and reset shifting up, suggests the dominant retention mechanism subject to structure relaxation at temperature range explored.
85C
5years

## Slide 17: Write Endurance
Iprogram – the same as 3DXP, subject to Tg
RWB – no worse than 3DXP
Read/Write Latency – no change
No window closure of 2K bits up to 2M FW cycles @ 10ms ipd, low ED
Scaling Expectation (No Scaling Data)

## Slide 18
Incumbent Technology
Introduction to BiSM
Cell Technology
Memory Switching Physics
Array Architecture
Critical Path to a-Product Definition

## Slide 19: SAG20 Elements Movement (Positive Pulse), similar to GST
1k cycles
PFA-396 (SD1)
1us
50ns
1us
50ns
Hefei
50 ns | 1000 ns | 50 ns | 1000 ns
50 uA |  | 150 uA | 
1k cycles

## Slide 20: Electrical Equivalent Circuit and Possible Underline Physics
Chal Glass Res
A VT window (∆VT) has been observed by applying programming pulses with opposite polarity. The best known ∆VT physics is an electrochemical potential modulation effect subject to mass transport by polarity.
  Leakage characteristics of SD is unlikely to sustain a charge-trap nonvolatile memory model.
  Bipolar Read signature refutes filamentation.
  Bipolar Write supports mass transport between electrodes.
Near parallel shift on SubVt I-V subject to polarity
  For ‘neg read’ – 1V of ∆VT in SubVt
  The equivalent circuit – a programmable battery connected to a Chal Glass Resistor serially
Where and what is the battery modulation (near 1V)
  Fermi Level (homogeneous junction)
  Band structure (heterogeneous junction) in Electronegativity or Work Function (Bandgap is 2ndary augmentation)
  Assuming Electrode to Chal Glass junction is subject to defect tunneling therefore voltage contribution is insignificant (On-State I-V and other evidence?)

## Slide 21: Basic Band Diagram of SAG and Model assumptions Electronic Structure of Amorphous Semiconductors, D. Adler and E. J. Yoffa, Phys. Rev. Lett. 36, 1197-1200 (1976)
Assumptions:
  EG:2eV
  Effective intrasite electronic correlation energy is negative therefore P-type is exhibited (pinned)
3 Electronic models on with SAG mass transport by polarity
  As (Ge?) moves toward cathode
  Homojunction – Correlation energy changed to positive therefore n-type (similar to tetrahedrally coordinated amorphous semiconductor)
  Heterojunction-I – Band offset due to coordination changes (Michaelson’s Electronegativity Scales & The work Function, IBM JRD 1978), higher Work Function
  Heterojunction-II – Band offset, but lower Work Function
  0.8eV Change is used to illustrate all 3 models
Vacuum
Ec
Ev
Ef
ϕe
Vacuum
(I)
(II)
(III)
∆Ef=+0.8eV
∆χ=−0.8eV
∆χ=+0.8eV
As-GeSex
C
C
As+/Ge+

## Slide 22: 1D Space Charge and Built-in Field
Trap Density [cc-1]
ε[MV/cm]
εmax
Space Charge Width
Trap Density [cc-1]
εmax [MV/cm]
Space Charge Width [nm]
Vbi=1V
Vbi=.1V
ϵSD = 10
EBD : Si ~0.3MV/cm SiO2 10~15MV/cm, GST ~0.3MV/cm, TAG ~1MV/cm, SAG ~3MV/cm

## Slide 23: Physical model – working principles & assumptions
SSM device is a string of domains serially concatenated. Node is an abstract point junction between domains.
  Simplified with 1D model
Per Kirchhoff law
  The nodal current is zero
  Assumption – Qausi-static SubVt I-V represents device I-V at nano-second regime
  The “domain” voltage drop for a current level will determine the shape of the I-V curve;
  Shift right is higher threshold voltage and Voltage contribution of shifting is the memory effects
4 carrier transport mechanisms –
  Conduction in delocalized state such as Diffusion and Drift
  Conduction between localized and delocalized states such Poole-Frankel
  Direct tunneling such as band to band and defect to defect between metallurgical junctions
Drift is linear function of electrical field – contribution is very low due to low free carrier and low mean-free path
  Likewise, Diffusion contribution is also low (Einstein relation)
Electronic trap density is in the order of 1% of atomic density (inactive or pinned) ~1021/cc
  10% structural vacancies in typical crystalline GST225, If electronically active, Debye length is < lattice constant; CV measurement exhibits Debye length in the order of μm or longer
  Space charge region @ junction established by direct tunneling with build-in potential

## Slide 24: 1D Space Charge and Built-in Field in SAG
Trap Density [cc-1]
Space Charge Width
ε[MV/cm]
εBD
EBD : SAG ~3MV/cm
Vbi [volt]

## Slide 25: Model Comparison
Vacuum
GeSex
C
C
As+
0V
(−)
(+)
⊕
⊖
ϕ
⊕
⊖
ϕ
⊕
⊖
ϕ
Bias
Model (I) – Homojunction
Model (II) – Heterojunction, higher 𝛘
Model (III) – Heterojunction, lower 𝛘
Vacuum
GeSex
C
C
As+
0V
(−)
(+)
⊕
⊖
ϕ
⊕
⊖
ϕ
⊕
⊖
ϕ
Bias
0V
(−)
Vacuum
GeSex
C
C
As+
0V
(−)
(+)
⊕
⊖
ϕ
⊕
⊖
ϕ
⊕
⊖
ϕ
Bias

## Slide 26: Model (I) – Homojunction
(–) Bias Read, same polarity of write
  Bias initially contributed to barrier reduction, very low current, shift I-V to right.
(+) Bias Read, opposite polarity of Write
  Space charge region maintained or no change. Potential drop evenly cross Chal glass.
Homogeneous junction model does not support the observed polarity effect
Vacuum
GeSex
C
C
As+
0V
(−)
(+)
⊕
⊖
ϕ
⊕
⊖
ϕ
⊕
⊖
ϕ
Bias

## Slide 27: Model (II) – Heterojunction, higher 𝛘
(–) Bias Read, same polarity of write
  Space charge region maintained or little change. Potential drop evenly cross Chal glass.
(+) Bias Read, opposite polarity of Write
  Bias initially contributed in compensating built-in potential, shift I-V to right.
Higher 𝛘 heterogeneous junction model supports the observed polarity effect
Vacuum
GeSex
C
C
As+
0V
(−)
(+)
⊕
⊖
ϕ
⊕
⊖
ϕ
⊕
⊖
ϕ
Bias
0V
(−)

## Slide 28: Model (III) – Heterojunction, lower 𝛘
(–) Bias Read, same polarity of write
  Bias initially contributed in compensating built-in potential, shift I-V to right.
(+) Bias Read, opposite polarity of Write
  Space charge region maintained or very low. Potential drop evenly cross Chal glass.
Lower 𝛘 heterogeneous junction model does not support the observed polarity effect
Vacuum
GeSex
C
C
As+
0V
(−)
(+)
⊕
⊖
ϕ
⊕
⊖
ϕ
⊕
⊖
ϕ
Bias

## Slide 29: Electrical Equivalent Circuit and Possible Underline Physics
A VT window (∆VT) has been observed by applying programming pulses with opposite polarity. The best known ∆VT physics is an electrochemical potential modulation effect subject to mass transport by polarity.
  Near parallel shift on SubVt I-V on polarity effects
  The equivalent circuit – a programmable battery connected to a Chal Glass Resistor serially
From empirical to physical
  Pursuing the validation of heterogeneous junction model
  Programmable battery is formed by the band offset
  Write –Band offset switching subject to mass transport.
  Read – Space Charge modulation results in voltage shift
SD Resistor
GeSex
C
C
As+
0V
(−)
(+)
⊕
⊖
ϕ
⊕
⊖
ϕ
⊕
⊖
ϕ
Post
Neg
Write
0V
(−)
Read Polarity

## Slide 30
Incumbent Technology
Introduction to BiSM
Cell Technology
Memory Switching Physics
Array Architecture
Critical Path to a-Product Definition

## Slide 31: Unipolar vs. Bipolar
Unipolar
Bipolar

## Slide 32: Challenge in Decoder Size & Energy
Invention | Architecture & Key Features | Problem addressed | Embodiments
Current Art of Unipolar Architecture | One MOSFET to select or inhibit in each of global decoder | Best Known Architecture for most compact decoder (die size) and lowest operation energy | S26A POR
Current Art of Bipolar Architecture | Inverters for global select and inhibit bias for bipolar operation, one inverter for each polarity | To address bipolar bias for wordline and bitline potential but double transistor count for global decoder & higher operating energy required | SR71 POR S24S POR
Idea #1 | Global bipolar select bias and one MOSFET for global inhibit bias | To reduce global decoder footprint and reduce energy from current art of bipolar architecture | Embodiment #1 Embodiment #2
Idea #2 | Global bipolar select bias and one MOSFET for global inhibit bias with additional high voltage MOSFET | To further reduce operating energy of idea #1 And reduce address transition sequencing | Embodiment #3 Embodiment #4 Embodiment #5 Embodiment #6

## Slide 33: Embodiments of Bipolar Decoder
“TO”  HV Transistor
Embodiment1
Embodiment2
Embodiment3
Embodiment4
Embodiment5
Embodiment6
S24S POR
SR71 POR
S26A POR

## Slide 34: S24S decoder
Uses separate paths to support positive and negative polarity biases.

## Slide 35: Voltage Stress
Oxide Stress MAX (purple)
  VPP or |VNN|
Jn Stress MAX (green)
  VPP-VNN
POSITIVE POLARITY
POSITIVE POLARITY
VSS
VPP
“Uses S26S CMOS”
NEGATIVE POLARITY
NEGATIVE POLARITY
VPP
VSS
Selected decoder
Deselected decoder
Selected decoder
Deselected decoder

## Slide 36: Why S24S decoder has higher energy?
Deselects gates need to toggle from VPP  VNN
or VNN  VPP when switching polarity.
This node has high fanout causing a large CV^2 component of energy when compared with the POR S26A. ~50% higher.

## Slide 37: Bipolar decoder architecture – Selected BL Path Shown
Unipolar
110Å TWN + P
VSS
AXN=VPPs
VSS
VSS
VSS
VPPs
VSS
ALF32
VPPs
LBL
VSS
VSS
VPPs
VSS
AXN=VPPs
VSS
HNREG
VSS
VNN
S24S
VPPs
VSS
LBL/LWL
BiSM32
VPP
VPP
VPPs
VSS
VPP
VSS
HNREG
AXN=VPPs
VPPs
VPPs
LBL/LWL
Bipolar
110Å TWN + P
2 extra global Xtrs.
Extra Xtrs. in tile predec
Bipolar
160Å TWN + tgP
VT: 1.2V @ 9.3 VB for TWN
9.6V compliant DR
AXN/HNREG Mux/tile

## Slide 38: Die Size and Energy Assessment
Architecture | Decoder | CMOS and Interconnect | Density [Gb/mm2] | Write [pJ/b] | Read [pJ/b] | Gap [%] |  | 
 |  |  |  |  |  | Density | Write | Read
ALF32 (POR) | Unipolar | P1240.0 | 1.28 | 104 | 44 |  |  | 
S24S | Bipolar | P1240.0 | 1.16 | 154 | 55 | 9% | 48% | 25%
BiSM32 | Bipolar | P1240.0+TGcMOST | 1.00 | 107 | 47 | 23% | 3% | 7%
S24S decoder creates big energy gap and lowers density
BiSM32 decoder Arch bridges the energy gap, but reduces density further.
Density gap of BiSM32 can be recovered by improving CMOS performance.

## Slide 39
Incumbent Technology
Introduction to BiSM
Cell Technology
Memory Switching Physics
Array Architecture
Critical Path to a-Product Definition

## Slide 40: Assessment & Critical Path to a-Product Definition
BiSM technology presents an opportunity for higher speed SCM with simplified manufacturing without obvious technology showstopper. It solves known 3DXP issues, likely introduces others which we are yet to fully see. Scaling is yet to be demonstrated.
Optane™ Memory Media has Circuit Under the Array (CUA) to reduce die size. The bidirectional circuit topology of BiSM is a key constraint of CUA for its ability to match or to beat present Optane™ product cost, despite the improved write latency. Currently die size is prohibitive with the speculative TGcMOST design rule. Efficient tile design is a key challenge to product viability.
Besides developing a smaller footprint transistor and/or inventing new bipolar decoding scheme, a more fundamental issue is high voltage supply rail constraint, which is driven by (voltage) window budget. Integrating new material and/or read/write algorithm to reduce BiSM VT sigma, drift and shift are the key enablers for voltage reduction.
Competitive landscape – We believe that Micron is pursuing this technology at a priority over the current Optane™ approach. Also, in the research segment of atomistic switches (intel sponsored or public domain), discussions and disclosures on the sighting of similar behavior are merging.

## Slide 41: Backup Materials

## Slide 42: “Hysteresis” of Transfer characteristics
Output traces subject to input and prior history in a cyclic loop SRAM PCM
Input (WRITE) metrology actuates the switching mechanism
Output (READ) metrology manifests the switched physics
It’s a phenomenological “duck test”. Using abductive reasoning to prioritize possible switching mechanism for SSM risk assessment – also to eliminate unlike mechanisms.
It can also serve for inductive reasoning to derive physics from specific observations – assumptions will be called out for additional tests.
i/p
o/p
i/p [v]
o/p [v]
Pulse [μA]
VT [v]

## Slide 43: Atomistic memory switching
2-T NVM (focus on memory element)
PCM (Samsung, Micron, IBM/Macronix)
SSM (Intel/Micron)
VMCO/CMOx (IMEC, Unity)
  4DS: PCMO (CMOSx) with HGST/WD partnership?
  WD/Toshiba: Binary conductive oxide instead of PCMO
  IMEC: VMCO
  CMOx: Unity (Rambus)
VORAM/CBRAM (Redox)
  Weebit: Porous SiO, TaO
  Panasonic/Fujitsu/HP: TaO
  TSMC/ITRI: HfO
  Macronix: WO
  Adesto: Te in AlO
  Micron/Sony: Cu in GdO
  NEC: Cu in oxide(?) – targeting FPGA
  Crossbar: Ag/Cu in α-Si (with Si/SiO diode)
STT (too many)
FTJ
  Toshiba: HfO + interface layer
  AIST consortium: UoTokyo and etc
Other NVMs
SXP-like (1S1R)
  Intel
  Micron
  Macronix/IBM: Si-STAG + N doped 225
  Hynix: As doped SiO + ReRAM(?)
  IMEC: N doped GeSe (selector only)
  LETI: GeSe + HfO
FECAP as in 1T1C
  IMEC, NAMLAB (GF), MFC, Hynix/LAM : HfO
  TI: PZT in production/ research HfO
  Panasonic: PZT in production
  Sony: SBT in production
FEFET
NRAM (Nantero)
Charge trap

## Slide 44: Transfer Charx Summary
Pulse [μA]
Log(I@0.4V]
❷
❶
❸
❹
Pulse [μA]
Log(I@3.5V)
Pulse [V]
Log(I@0.5V)
❷
❶
❸
❹
Pulse [V]
I@0.1V
Pulse [V]
Log(I@3V)
❷
❶
❸
❹
PCM
SSM
VMCO/CMOx
VORAM/CBRAM
STT
FTJ
❷
❶
❸
❹
❷
❶
❸
❹
Pulse [V]
Log(I@3V)
❷
❶
❸
❹

## Slide 45: Transfer Charx Summary
Set
❷
❶
❸
❹
SXP
VMCO/CMOx
VORAM/CBRAM
STT
FTJ
E
E
Reset
Set
Reset
SSM
Reset
Set
Set
Reset
?
?
Quad-1
Quad-3