## Slide 1
Current Status
Critical Paths to be considered for Bow Falls

## Slide 2: Current Status

## Slide 3: BiSM Silicon Empiricals
Last silicon Rev 6.6, In doped SAG and DOE, in June/2018.
Yield learning curves with 100s of wafers (one lot every 2 weeks)
Rev 6.6 SD.k2 BKM process demonstrated PG1 structure yield (S26 live die): >75% 1D & >40% 2D (on par with full stack at the same time frame)
1st & 2nd cut profile meets MTS; SWA @ 87.5° & 88.5° correspondingly.
Parametric and reliability sampling – 8 lots, 40 wafers, 5 die per wafer.
PG4 capable RWB (SR71 based, limited by array size 3.3s)
PG1 capable of endurance; good/upper quartile die passing 2M cycles FW
No ULR performed

## Slide 4: SLC RWB @ 41nm Pitch
Full Stack op. (unipolar)
Metric | Unit | Full Stack^ | BiSM^
DVT @ 1ms ( = RST-SET ) | mV | 1140 | 1380
E2 Consumers |  |  | 
sVt | mV | 95 | 100
Drift: 1ms-10s (3s-48h) | mV | 260 (320) | 330 (220)
GB (WE,RD,BD) | mV | - | -
E3 Consumers |  |  | 
sVt | mV | 100 | 105
Drift: 1ms-10s (3s-48h) | mV | 630 (>1100) | 590 (1050)
GB (WE,RD,BD) | mV | 100 | 100
Array Op. |  |  | 
x-tile | mV | 30 | 30
Leakage: SET (RST) | mV | 5nA (2nA) | 5nA (0.2nA)
E1 | mV | 4030 | 4040
E4 | mV | 7600 | 7500
^ 10s Qual SORT for full-stack, while non-opt. TBD for BiSM
BiSM op. (bipolar)
E2
10s
E3
10k FW
RBER goal
RWB
Vinh
1ms
time
time
Pulse Amplitude
RST
SET
RST
SET

## Slide 5: BiSM vs. Full Stack @ 41P

## Slide 6: Process Technology
Metric | Full Stack |  |  |  |  |  |  |  |  | BiSM |  |  |  |  | Scaling Challenge
Periphery | LVT, HVT + 5~6 interconnect |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Cell Stack | BE | SD | ME1 | ME2 |  | PM |  | TE |  |  | BE | SD | TE |  | 
Array Metals | W, 30nm First Cut, 30/40 nm 2nd Cut |  |  |  |  |  |  |  |  | ½ or more metal thickness reduction possible (>50% Ipgm/Ilkg reduction) |  |  |  |  | 
Patterning | Partial etch and Liner are required |  |  |  |  |  |  |  |  | Single etch, no liner required; lower AR, lower scope for hard-mask |  |  |  |  | 
Seal | Nitride seal required |  |  |  |  |  |  |  |  | Required, lower AR, more options |  |  |  |  | 
Gap fill | No air gap, 1st/2nd Rq tuning for TD |  |  |  |  |  |  |  |  | No air gap, no visible TD issue |  |  |  |  | 
CMP | Similar challenges as nodes scale, socket size scaling limitations may impact |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Ambient | Required |  |  |  |  |  |  |  |  |  |  |  |  |  | 
On Pitch Via | Scaling challenges expected at 28 pitch and below for via resistance |  |  |  |  |  |  |  |  |  |  |  |  |  | 

## Slide 7: Set State
Metric | 41nm Pitch Full Stack | 41nm Pitch BiSM | Scaling Challenge
VT | Tunable by SD MTS (thickness, alloy, transfer function) |  | 
MLC feasibility | Lower tuneability by waveform | More flexibility (without PM) | 
sVt | SD MTS + cross contaminations | SD MTS | 
Drift | SD structure relaxation |  | 
EvolutionVt | SD + PM WE, higher VT turn-around | SD WE at lower power | 
Leakage | SD MTS + cross contaminations | SD MTS | 
E1 | SD WE + cross contamination | SD WE | 
E2 | SD WE + PM set-ability + RD | SD WE | 

## Slide 8: Reset State
Metric | Full Stack | BiSM | Scaling Challenge
VT | Tunable by PM material & thickness | Tunable by SD material | 
MLC feasibility | Tunable by waveform | Tunable by waveform | 
sVt | (SD + PM) MTS + cross contamination | SD MTS | 
Drift | SD + PM structure relaxation | SD structure relaxation | 
EvolutionVt | SD + PM WE | SD WE at lower power | 
Leakage | SD intrinsic (low a-PM contribution) | SD intrinsic subVt shift right | 
E3 | SD + PM WE + TD | SD WE + RD | 
E4 | SD + PM WE + PM drift + Leakage | SD WE | 

## Slide 9: Set Operation
Metric | Full Stack | BiSM | Scaling Challenge
Mechanism | Crystallization: Nucleation/Growth | Mass transport @ TG (Segregation) | 
IProgram | 25uA + 60uA (ambipolar) | 50uA (polarity dependent) | 
tpulse | 130ns+70ns | 50ns | 
VSelection | E4 | E4 | 
Spike Miti. | Needed for PM endurance | No | 

## Slide 10: Reset Operation
Metric | Full Stack | BiSM | Scaling Challenge
Mechanism | Vitrification (Glass) | Mass Transport @ TG (Segregation) | 
IProgram | 110uA (ambipolar) | 50uA (polarity dependent) | 
tpulse | 5ns | 50ns | 
VSelection | E2 | ”E4” | 
Spike Miti. | Needed for PM endurance | No | 

## Slide 11: Read Operation
Metric | Full Stack | BiSM | Scaling Challenge
Mechanism | Demarcation Read/Set Back/Termination | Demarcation Read(/termination?) | 
Iread | 25uA/60uA/25uA | 25uA or higher (/25uA) | 
tpulse | 35ns/35ns/30ns | 35ns(/35ns) | 
VSelection | E2 | E2 | 
Spike Miti. | Needed to PM RD | No | 

## Slide 12: Reliability
Metric | Full Stack | BiSM | Scaling Challenge
WE (Write End.) | Limiter: E2 (PM turn-around) Tuning: (SD + PM) MTS, waveform | Limiter: Extrinsic E1/E4 Tuning: SD MTS (SD ‘health’) | 
Array init. (Seasoning) | SD stabilization (low PM contribution) Tuning: SD MTS (SD ‘health’) | SD stabilization Tuning: SD MTS (SD ‘health’) | 
WD (Write dist.) | PM proximity disturb + (SD+PM) BD Tuning: Stack MTS, waveform | SD BD (‘reverse’ dominating) Tuning: SD MTS | 
RE (Read End.) | SD WE + (PM+SD) disturb Tuning: (PM + SD) MTS, waveform | SD WE Tuning: SD MTS | 
RD (Read Dist.) | PM disturb (low SD contribution) Tuning: PM MTS, and waveform | SD WE + SD BD (‘reverse’) Tuning: SD MTS and waveform | 
Retention | SD + PM structure relaxation Tuning: (SD+PM) MTS, and waveform | SD structure relaxation Tuning: (SD) MTS, and waveform | 

## Slide 13: 3T Bipolar Decoder circuit and layout assessment based on 41P DTS
-3.7
0
-3.7
0
0
0
-3.7
3.7
1.2
0
-3.7
3.7
0
0
-3.7
3.7
-3.7
3.7
1.2
1.2
IDLE
0
3.7
3.7
0
0
0
-3.7
3.7
1.2
0
POS
NEG
3T Solves the energy problem present in 2T POR
  No Deselect Toggle
  At Cost of adding on transistor. (Small N Xtr.)
Decoder footprint is expected on par with 2T POR
  [Med P + Med N + Small N] vs. [Big N (or P) + small P (or N)]
Interconnect track density increases due to bipolar operations
  Metal pitch reduction is expected
 | ALF32 | S24S | 3T
Status | POR | POR | Pre POR
Cell Arch | Unipolar | Bipolar | Bipolar
Decode Type | 2T | 2T | 3T
Deselect Togl. | No | Yes | No
Float Deselects | No | No | No
Energy | 104 | 154 | ~104
Die size | 198 | 221 | 227
 | 3T |  |  |  | 
 | POS |  | NEG |  | IDLE
 | SEL | DESEL | SEL | DESEL | 
gp | 3.7 | 3.7 | 0 | 0 | 0
lselp | 0 | 3.7 | 0 | 3.7 | 3.7
lbwl | 3.7 | 0 | -3.7 | 0 | 0
lseln | 0 | -3.7 | 0 | -3.7 | -3.7
gn | 0 | 0 | -3.7 | -3.7 | 0
lselg | 0 | 1.2 | -3.7 | 1.2 | 1.2
vss | 0 | 0 | 0 | 0 | 0
#/patch | 32 | 992 | 32 | 992 | 1024

## Slide 14: Read
3DXP Full Stack
BiSM Read
Read Pulse incl. Ramp
(37.5ns)
Sense Amp Latch
(12.5ns)
BL 1st Termination (20ns)
Start
Read Pulse incl. Ramp
(37.5ns)
Sense Amp &
Latch
(12.5ns)
SET Pulse 3 (25ns)
BL 1st Termination (20ns)
Set? (5ns)
Yes
No
Start

## Slide 15: Set a reset cell
3DXP Full Stack
BiSM
WL/BL Ramp
(211ns)
Incl.
Spike Miti (71ns)
Snap Detect (45ns)
C-cell (95ns)
Ilow (P1)
(30ns)
Ihigh (P3)
(103ns)
P4
(30ns)
Start
BL1st
(20ns)
WL/BL Ramp
(140ns)
Incl.
Snap Detect (45ns)
C-cell (95ns)
Ihigh (P3)
(50ns)
Start
BL1st
(20ns)

## Slide 16: Reset a set cell
3DXP full Stack
BiSM
WL/BL Ramp
(37.5ns)
Sense
(12.5ns)
Reset Pulse (15ns)
Set? (5ns)
Yes
No
Start
WL/BL Ramp
(140ns)
Incl.
Snap Detect (45ns)
C-cell (95ns)
Ihigh (P3)
(50ns)
Start
BL1st
(20ns)