## Slide 1: CLV-B194 & CLV-B212 sub-IVs at temperature 25C-125C
TiN BE/TE
C. Papagianni, P. Fantini, D. Kau

## Slide 2: Wafers Tested
Wafers Tested:
CLVB194_w7, TiN_BE/35nm SD1/TiN/C
CLVB194_w17: TiN_BE/35nm SD1/C
CLVB212_w2: C_BE/35nm SD1/C.

## Slide 3: Preparing Bits
At Room temperature:
  8 Virgin Bits (Spine/Module: 41J)
  8 Bits Cycled with 1E3cyc (POR CLV cycling with Ramp pulses ~300uA) (Spine/Module: 81K).
  Dies: [-1,2;1,2;0,1;-1,0;1,0;0,-1;-1,-2;1,-2]
  Total 16bits/wfr were tested.

## Slide 4: Vth 1 to 1E3cyc
LOT_ID | Wafer | Thickness | Alloy | VTH_FF | VTH_SF | Vform | VTH_1E3cyc | Vth_SF-Vth_1E3cyc
CLVB212 | 2 | 35nm | C/SD1/C | 9.23 | 6.41 | 2.74 | 4.60 | 1.82
CLVB194 | 17 | 35nm | TiN/SD1/C | 8.09 | 4.36 | 3.52 | 4.53 | -0.17
CLVB194 | 7 | 35nm | TiN/SD1/TiN/C | 8.22 | 5.58 | 2.57 | 5.44 | 0.14
Devices behave as expected. Data in agreement with L1P1.
Negligible cycling degradation when TiN is used as BE.

## Slide 5: DC Sweeps_Virgin & 1E3cyc
Exclude

## Slide 6: Idut Vs sqrt(Vdut) by Cycle
After 1E3cyc, Io & STS is lower with TiN TE.
IVs shifted to the right with C BE.
STS approximately the same for the 3 splits.
Virgin
1E3cyc

## Slide 7: Io & STS_Virgin & 1E3cyc
LOT_ID | Wafer | Thickness | Alloy | Io_PF_Virgin | STS_PF_Virgin | Io_PF_1E3cyc | STS_PF_1E3cyc
CLVB212 | 2 | 35nm | C/SD1/C | 1.16E-19 | 9.13 | 2.67E-18 | 9.83
CLVB194 | 17 | 35nm | TiN/SD1/C | 2.38E-18 | 9.83 | 3.22E-17 | 9.04
CLVB194 | 7 | 35nm | TiN/SD1/TiN/C | 1.42E-17 | 8.42 | 8.08E-14 | 5.86
Virgin State:
  1-2orders of magnitude leakage increase with TiN BE.
  STS ~ the same for the 3 splits.
Post 1E3cyc:
  3orders of magnitude leakage increase with TiN TE.
  STS ~2X decrease with TiN TE.

## Slide 8: STS Vs tSD_calc
Wafer | Thickness | Alloy | Io_PF_Virgin | STS_PF_Virgin | tSD_calc (nm) | Io_PF_1E3cyc | STS_PF_1E3cyc | tSD_calc (nm)
2 | 35nm | C/SD1/C | 1.16E-19 | 9.13 | 14 | 2.67E-18 | 9.83 | 12
17 | 35nm | TiN/SD1/C | 2.38E-18 | 9.83 | 12 | 3.22E-17 | 9.04 | 14
7 | 35nm | TiN/SD1/TiN/C | 1.42E-17 | 8.42 | 16 | 8.08E-14 | 5.86 | 34
Considering: and ε=7.5 (optical measurements):
At Virgin, Thickness ~1/2 of nominal thickness.
Considering for ε, the fitting results (analysis at next slides),
CYCLE | FF |  | 1E3cyc | 
Alloy | ε_SD | tSD_calc (nm) | ε_SD | tSD_calc (nm)
C/SD1/C | 2.23 | 47 | 1.72 | 52
TiN/SD1/C | 1.62 | 56 | 0.81 | 131
TiN/SD1/TiN/C | 2.10 | 58 | 96.36 | 3

## Slide 9: Etest Flow
Wfrs were baked at 150C/1hour to saturate drift.
IVs were collected at 4 different temperatures in the following order:
  125C, 85C, 65C, 45C, 25C.
IV sweep up to 70%Vth (based on L1P1 data; Iclamp=1nA).

## Slide 10: IVs Vs Temp
Virgin
Post 1E3cyc
TiN_BE/35nm SD1/TiN/C
TiN_BE/35nm SD1/C
C_BE/35nm SD1/C
C TE film is not seasoned; devices are virgin.
PF fitting:
If T=125C, fitting range: 1E-11 <Idut<1E-9,
Else
fitting range: 2E-12 <Idut<1E-9.
Poole-Frenkel equation:
C TE related conduction mechanism at low field?

## Slide 11: Idut Vs sqrt(Vdut) by Cycle @ 65C
After 1E3cyc, Io & STS is smaller with TiN TE.
IVs shifted to the right with C BE.
STS approximately the same for the 3 splits.
Virgin
1E3cyc
STS

## Slide 12: DC Sweeps & Bake Recovery after 150C/1h
Virgin & Post_1E3cyc IVs overlap quite well after the 150C/1hour bake for the C TE splits.
Full recovery is not observed for the TiN BE & TE split, after 150C/1h bake.

## Slide 13: Methodology
2 methods were used to extract Ea and STS (εSD):
  1st method:
    I Vs sqrt (V)  Slope=STS and Intercept=IoPF.
    Verify STS  1/KT  Get β and extract ε.
    From Intercept, extract Ea & Io1.
  2nd method:
    I Vs 1/KT Slope=Ea-β*sqrt(V) and Intercept=Io1.
    Verify Slope  sqrt(V)  Extract Ea and β.
Both Methods give essentially the same results.
, where

## Slide 14: 1st Method: Ea & β
CYCLE | FF |  | 1E3cyc | 
Alloy | Ea (eV) | β [e*sqrt(V)] | Ea (eV) | β [e*sqrt(V)]
C/SD1/C | 1.20 | 0.38 | 1.37 | 0.50
TiN/SD1/C | 0.81 | 0.28 | 0.88 | 0.33
TiN/SD1/TiN/C | 0.68 | 0.20 | 0.35 | 0.08
Lower Ea for TiN TE split.

## Slide 15: 2nd Method: Ea & β
Ea ~1eV for C TE splits. Ea decreases to 0.82eV with TiN TE.
Results show lower barrier height with TiN TE.
Considering metal/p-semiconductor contact, results are in agreement with smaller work function in C TE. Results are corroborated by φm measurements in F4.
Bit by Bit | FF |  | 1E3cyc | 
Level | Ea (eV) | β [e*sqrt(V)] | Ea (eV) | β [e*sqrt(V)]
C/SD1/C | 0.96 | 0.27 | 1.00 | 0.31
TiN/SD1/C | 0.85 | 0.32 | 1.10 | 0.45
TiN/SD1/TiN/C | 0.82 | 0.28 | 0.30 | 0.04
φm (eV) | Metal
4.763 | TiN
4.405 | 300A Endura BKM Carbon
4.4 | 300A ULVAC Biased Carbon

## Slide 16: εSD
Bit by Bit | FF |  |  | 1E3cyc |  | 
Level | Ea (eV) | β [e*sqrt(V)] | ε_SD | Ea (eV) | β [e*sqrt(V)] | ε_SD
C/SD1/C | 0.96 | 0.27 | 2.23 | 1.00 | 0.31 | 1.72
TiN/SD1/C | 0.85 | 0.32 | 1.62 | 1.10 | 0.45 | 0.81
TiN/SD1/TiN/C | 0.82 | 0.28 | 2.10 | 0.30 | 0.04 | 96.36
At Virgin state: εSD ~2.
After 1E3cyc: εSD significantly increases for the TiN TE split.

## Slide 17: Summary Table_Method#2
Bit by Bit | FF |  |  | 1E3cyc |  | 
Level | Ea (eV) | β [e*sqrt(V)] | Io_1 | Ea (eV) | β [e*sqrt(V)] | Io_1
C/SD1/C | 0.96 | 0.27 | 4.03E-05 | 1.00 | 0.31 | 1.79E-05
TiN/SD1/C | 0.85 | 0.32 | 2.44E-05 | 1.10 | 0.45 | 1.26E-05
TiN/SD1/TiN/C | 0.82 | 0.28 | 6.61E-06 | 0.30 | 0.04 | 6.30E-07

## Slide 18: Summary
Activation energy was extrapolated from sub-threshold IVs at temperatures 25C to 125C.
Ea is lower for TiN TE split. Results are in agreement with lower work function in C TE splits.

## Slide 19: Follow up test
Repeat experiment (IVs Vs temperature) for 25nm,and 30nm SD1 wafers.
Enrico’s work function measurements in SD1/TiN & SD1/C wafers. Is it available?

## Slide 21: CLV-B194_Scorecard Summary_L1P1 (cont.)
Comparison to CLVB126_C/SD1/C (split 5, 6 Vs 7):
Vth_FF is ~2V lower with TiN BE. Vth_SF ~1V lower with TiN BE.
Leakage has increased 2.5X with TiN BE.
Cycling degradation larger for C/SD1/C split; Vth reduction ~1V after SF.
Drift & Bounce are comparable.
Comparison to CLVA163 (Splits 11,12 Vs 6):
Vth_FF ~2V higher with C BE (with or without TiN TE).
Vth_SF~1V higher with C BE (with or without TiN TE).
Cycling degradation improved for C BE splits by using TiN top electrode ( Vth decreased 0.7V from SF Vs 1.6V in C/SD1/C split).
Cycling degradation minimized for TiN/SD1/TiN/C split.
Comment | Material | Split | Vth_FF [V] | Vth SF [V] | VFORM [V] | Vth_min@1E3 [V] | I @ 0.85Vt (@1E3) [nA] | I_leak Yield | Vth_max-Vth_min (ME) [V] | Drift [mV/dec] | Bounce [mV/sigma]
 | preferred value |  | <7.9 (info) | >4 | info | >3.6 | <30 | >80% | <0.5 | <20 | <50
 | BE/SD/TE |  |  |  |  |  |  |  |  |  | 
CLVB194 | TiN/25nm SD1/C | 1 | 5.5 | 3.1 | 2.4 | 3.3 | 21 | 63 | 0.31 | 38 | 73
 | TiN/25nm SD1/TiN/C | 2 | 6.0 | 4.0 | 1.9 | 4.1 | 46 | 29 | 0.37 | 51 | 98
 | TiN/30nm SD1/C | 3 | 6.4 | 3.7 | 2.8 | 4.0 | 6 | 85 | 0.38 | 29 | 78
 | TiN/30nm SD1/TiN/C | 4 | 6.8 | 4.6 | 2.1 | 4.7 | 53 | 21 | 0.41 | 32 | 170
 | TiN/35nm SD1/C | 5 | 7.1 | 4.2 | 2.9 | 4.3 | 5 | 85 | 0.49 | 36 | 84
 | TiN/35nm SD1/TiN/C | 6 | 7.6 | 5.4 | 2.3 | 5.2 | 41 | 40 | 0.50 | 30 | 149
CLVB126 | C/Endura SD1 35nm/C | 7 | 9.1 | 6.3 | 2.7 | 5.1 | 2 |  | 0.49 | 24 | 87
CLVA122 | C/Endura SD1 35nm/C | 8 | 9.0 | 6.2 | 3.1 | 5.4 | 7 |  | 0.38 | 41 | 83
CLVA163 | C/Endura SD1 25nm/TiN/C | 9 | 7.9 | 5.0 | 2.7 | 4.3 | 8.9 | 89 | 0.79 | 31 | 166
 | C/Endura SD1 30nm/TiN/C | 10 | 8.8 | 5.8 | 3 | 4.9 | 8.2 | 92 | 0.72 | 0.3 | 148
 | C/Endura SD1 35nm/TiN/C | 11 | 9.4 | 6.6 | 2.9 | 5.9 | 10.5 | 85 | 1.13 | 111 | 257
 | C/Endura SD1 35nm/C | 12 | 9.4 | 6.5 | 2.8 | 4.9 | 13 | 95 | 0.50 | 32 | 101

## Slide 22
VTH_FF, VTH_SF, Vform & VTH_1E3cyc
LOT_ID | Wafer | Thickness | Alloy | VTH_FF | VTH_SF | Vform | VTH_1E3cyc | Vth_SF-Vth_1E3cyc
CLVB212 | 2 | 35nm | C/SD1/C | 9.23 | 6.41 | 2.74 | 4.60 | 1.82
CLVB194 | 17 | 35nm | TiN/SD1/C | 8.09 | 4.36 | 3.52 | 4.53 | -0.17
CLVB194 | 7 | 35nm | TiN/SD1/TiN/C | 8.22 | 5.58 | 2.57 | 5.44 | 0.14

## Slide 23: Idut Vs sqrt(Vdut) by split

## Slide 24: Method#1: STS VS 1/KT
Virgin
Post 1E3cyc
Excluded
Indeed, STS increases with 1/KT.

## Slide 25: 1st Method: ε _excluding all 125C
CYCLE | FF |  |  | 1E3cyc |  | 
Alloy | Ea (eV) | β [e*sqrt(V)] | ε_SD | Ea (eV) | β [e*sqrt(V)] | ε_SD
C/SD1/C | 1.20 | 0.38 | 1.11 | 1.37 | 0.50 | 0.66
TiN/SD1/C | 0.81 | 0.28 | 2.04 | 0.88 | 0.33 | 1.58
TiN/SD1/TiN/C | 0.68 | 0.20 | 4.15 | 0.35 | 0.08 | 24.35

## Slide 26: 2nd method: Slope Vs Sqrt (V)
Slope=Ea-β*√V
    I=Io*exp(STS*√V)
STS=β*q/KT
Io=Io1exp(-Slope/KT)
Please note that lines are added for guidance. Ea & β are extracted in bit by bit case.
Bit by Bit | FF |  | 1E3cyc | 
Level | Ea (eV) | β [e*sqrt(V)] | Ea (eV) | β [e*sqrt(V)]
C/SD1/C | 0.96 | 0.27 | 1.00 | 0.31
TiN/SD1/C | 0.85 | 0.32 | 1.10 | 0.45
TiN/SD1/TiN/C | 0.82 | 0.28 | 0.30 | 0.04