## Slide 1: AC_IV Vs Temp on Virgin Bits Vs CD
Christina Papagianni

## Slide 2: Etest flow
ACIV at FF was measured for Virgin Spines @ Temperature (50x50nm^2):
  PTX-A364 w24 (spl1),w23(spl2), w4 (spl4), w6 (spl5)
  Code dev: code_dev_PTX14_IG88_ACIV_Virgin
  Die: [-1,-1]
  Spines: 71O @ 85C file: A365V85C
  72O @65C file: A365V65C
  73O @ 45C file: A365V45C
  72M @ 30C file: A365V30C

## Slide 3: VTH Vs Temperature @ Virgin _50x50cells
VTH decreases with Temperature, as expected.
Temperature coefficient meets DTS requirements; is less than -5mV/C for all splits.

## Slide 4: ITH Vs Temperature @ Virgin _50x50cells
Ith does not show strong dependence on temperature!
Ith is ~5X higher in SD1.
Please see distributions in bonus slide: While Vth is normally distributed, Ith is not! Tail bits have Vth values uniformly distributed.

## Slide 5: Switching Power Density
Pth (as Ith) does not show dependence on temperature!

## Slide 6: Virgin AC_IV VS CD & Temperature

## Slide 7: Etest flow
ACIV at FF was measured for Virgin Spines @ Temperature:
  Spines: 73I_45x45, 72L_50x50,73F_60x60, & 73K_70x70
  Dies: [0,1] 85C file: A364CD85C
  [0,0] 65C file: A364CD65C
  [1,0] 45C file: A364CD45C
  [0,-1] 30C file: A364CD30C
  A few spines measured at 65C were found tested and were excluded from the analysis.

## Slide 8: VTH, ITH, PTH VS Temp & CD
While VTH does not depend on CD, Ith increases with CDs.
Normalized Ith using actual CDs should result to better data overlap.
In this data set , Ith shows slight temperature increase (mainly due to the 85C data; max 30-40% Ith increase with temperature).

## Slide 9: VTH VS Temp (considering differences due to CD negligible)
If we exclude 85C data for SD1 (split1), then slope in better agreement with data set at 50x50 cell.
VTH decreases with Temperature, as expected.
Temperature coefficient for SD.F3 alloy meets DTS requirements; is less than -5mV/C.

## Slide 10: VTH VS Temp by CD

## Slide 12: Vth Vs Temperature
 |  | PTXA298 | 
Pulse | Split | 25nm SDδ.B2 | 25nm SDδ.B4
RESET | Temp Coefficient (mV/C) | -2.31 | -2.69
SET | Temp Coefficient (mV/C) | -3.19 | -1.32
Temperature coefficient for 25nm SDδ.B2 & SDδ.B4 alloys is <-3mV/C; and lower than DTS requirement of -5mV/C.

## Slide 13: 19nm SD1_50x50

## Slide 14: 19nm SD.F3_50x50

## Slide 15: 22nm SD.F3_50x50

## Slide 16: 25nm SD.F3_50x50

## Slide 17: 19nm SD1_45x45
Please note, high Ith tail bits have Vth uniformly distributed.

## Slide 18: 19nm SD.F3_45x45
Please note, high Ith tail bits have Vth uniformly distributed.

## Slide 19: 19nm SD1 Vs CD
Tail on Ith distribution does not depend on device CD.

## Slide 20: 19nm SD.F3 Vs CD
Tail on Ith distribution does not depend on device CD.

## Slide 21: 22nm SD.F3 Vs CD
Tail on Ith distribution does not depend on device CD.

## Slide 22: 25nm SD.F3 Vs CD
Tail on Ith distribution does not depend on device CD.