## Slide 1: SxP Device Physics
Phase Change
Structure and band diagram to illustrate the origin of conductivity of a chalcogenide material.
Evidence of phase change from thermal hysteresis.
Power delivery with pulse to change phase
Physics and model of phase change in SxP technology (electrode is the heater)
Threshold Switching
Structure and Band diagram of a SD devices, electrode included.
Subthreshold conduction is a Poole-Frankel emission process
Space charge injection delocalizes, the mobility gap decreases and carriers multiply at cathode as device biased in near threshold.
Carrier multiplication at both electrodes is the positive feedback mechanism leading into threshold, snapback as shown in negative differential resistance regime.
On-state is due to carrier injection (tunneling) from both electrodes. Injected carrier recombine in the bulk or drift through to other electrodes.

## Slide 2
PM
SD
TE
ME
BE
Acceptor-like
localized states
Ec
Ev
Ef
E
CB
VB
10% structural vacancies result in localized states near LP band
Over- and under-coordinated Tellurium lead to defects/traps
Amorphous
Crystalline
Acceptor ( C1- )
Ec
Ev
Ef
E
CB
VB
Donor( C3+ )
LPTe ( C20 )
LPTe

## Slide 3
(120nm)2
(45nm)2
J [A/nm2]
V [Volts]
40s/SD2’/40s
20s/SD2’/60s
30s/SD2’/30s
502 nm2 Cell
J [MA/cm2]
48
32
16
64
V [Volts]
Bottom
Electrode
Top
Electrode
TE
BE
SubThreshold
PFE conduction
BE
TE
Neal Threshold
BE
TE
(1)
(2)
(3)
(4e)
(4h)
(5)
(6)
(7e)
(7h)
Threshold,
(positive feedback)
Snapback, NDR Regime
(1)
(2)
(3)
(1)
(4)
(2)
(4)
TE
BE
(3)
On-state
(2R)
(2R)
1.7
BE
TE
3.0eV
4.4eV
φB=.85eV
EF
1.7eV

## Slide 4
1.7
SD
E
E
3.0
4.4
Depleted region
Ebarrier= 0.85 eV
Acceptor/Donor traps placed uniformly in the gap
(conc=1e21 cm-3)

## Slide 5
SD
1.7
BE
TE
3.0eV
4.4eV
φB=.85eV
EF
1.7eV
TE
BE