## Slide 2: BLBL
Goal: 1E-3

## Slide 3: NOBL
Goal: 3E-4

## Slide 4: OPENs
Goal: 1E-5

## Slide 5: Leakge vs VT
There is a shift related to CSOD/C7/other?

## Slide 6: Drift 1us-10s
Need to update with WLR drift 1us-10min, including t0 and slope
Goal: 1us-10min  80mV

## Slide 7: Median Drift @ED4 @RT
Drift increases with Ge% within A2* lot. 15-20mV/Ge%
Based on V4/V10 data on LQ30, toggle driven by t0 rather than drift slope (Unbiased drift slope ~75mV @90C). Lower Ge% will help but not meet goal.
Lot to lot/Wf to Wf variation within V10 significant  Further segmentation WIP
Each point is die
Each point is median by zone
1us-10min
1us-10s
Feng
Goal (estimated): ~80mV
BQ34
LQ31 2E
LQ30 2E

## Slide 8: SET VT Sigma
Need to add variability plot

## Slide 9: SET VT Sigma
SET VT Sigma driven by Si%. ~11.5mV/at% [fit within A2* splits]
Significant lot to lot variation. Segmentation WIP.
Need to update with 1us data
Data measured with std. histo @300ms wait-time

## Slide 10: E2 Knee