## Slide 1: Common VDM – Next Rev ?

## Slide 2: Binning / Strategy
Trending Register | Bin | Sigma | Drift Coverage | Forgiveness
Nevil | WF:* | 2 | >=8 | 8
Sanjay | WF:* | >=2 | 10 | 8
Russ | WF:* | >=2.5 | 10 | 7 ?
Al | WF:* | 3 | >=10 | 6 ?
Problem Statement:
  Systematic defect can be covered by AO.
  Random defects cannot be covered by AO
Strategy for probe
  Move to “Sanjay” Category
  Select VDM based on 10 decade drift margin at probe
    Probe Test Set at 10sec VDM and Reset at 25usec VDM
  Create a trend register or add bin for visibility/selecting units for probe
    RBER Trend : 1usec,10sec and predict 10K sec rber
    Drift Trend
    Request custom crunch based on Sanjay’s AO script
10dec
VDM1
Xs/3s
E2
E3
10Ksec
1usec
1usec

## Slide 3: Die Loss from Yielding Dice
LQ27 and LQ29 show about 7-12% die loss from WF:*
V8 51LP lot, shows about 30% die loss at WF:*
76 dice
413 dice
835 dice

## Slide 4: Proposal for VDM1 at probe
VDM1 = Best RBER(10sec E2 / 1usec E3) + drift ( 3 dec)
  Dynamic Drift => Probe collect E2 at 1sec and 10sec
    7 decade [1usec – 10sec] + 3 decade [calculated based on 1sec to 10sec by die]
  Limit BER at VDM1 to 3s
    Increase drift coverage
  Trend : RBER and MAX_DRIFT_COVERAGE
VDM2 = (VDM1 + VDM3 ) / 2
VDM3 = VDM1 + (4dec * 100mv E3 drift), only allow to Max 7v
Si
E2
E3
1usec
1usec
VDM1
10sec
1E4sec
predict
1E8sec
VDM3
VDM2
RBER
VTH
400mv
200mv
Drift
2sigma
Current VDM1
VDMx

## Slide 5: Previous to Proposed
Current Method
Anchored on 2sigma
No trending for Drift (assumed 8dec)
  Die may fail EC at probe if drift > E2 Margin
Rber Trending
  10sec
True window Trending
Testing : EC = VDM1-50mv, FC = VDM1 – 100mv
8dec
VDM1
2s
-2s
E2
E3
100sec
1usec
1usec
10dec
VDM1
xs
E2
E3
10Ksec
1usec
1usec
Proposed Method
Anchored on 10decades of drift
Drift trending based on 2sigma
RBER Trending (limited to 3s)
  1usec, 10sec
True window trending
Testing : EC = VDMx, FC = VDM1 – 100mv

## Slide 6: Validation Plans
Sanjay’s Crunch
  Predict RBER needed with AO and C7 enabled (LQ29)
WCF Runs
  Check for the longer drift times
  Check for endurance requirements for 1k cycles
  Sigma
Burn Run
  Validate full dice testing at longer times
Probe Run
  Validate > 10sec at probe

## Slide 7: V4 Vs V10 comparisons
SD V10 => LQ30 – 2E and LQ31 – 2E
Median SET Knee improvement by 0.3sigma, True Window (2sigma) improved by 50mv, driven by drift improvements
Better Set knee and True Window

## Slide 8: Forgiveness tightening
Comparing LQ30 Vs LQ31 V10
1E-3 we see about 30% yield hit at bin EC

## Slide 9: backup

## Slide 10: Median by ED Vs 99% by ED
Using Worst 1% of all 2.5k unit will select wrong VDM (based on new method)
Method should be
  Median RBER by ED Groups
  Select Worst ED ? because this will minimize the failing rate of blocks and will give correct signature to quantify for FAB
9108202:24:P11:04:12