## Slide 1: SD𝛅 Ver 10 vs. Ver 4
SD FT, WW25.3/2015
Problem Statement – V10 incremental yield loss (from 7 dec to 10 dec) worse than V4’s
Models of the problem
  SDδ V10 drift higher
  Set tail subject to SDδ V10 integration
  Line stability and control
Segmentations and analysis
  AMG:
  Electrical characterization
    1) structure yield 2) Leakage 3) E1 inhibiting failure, 4) E2 to E3 true window 5) cycling degradation 6) 2ndary effects, high in BER Pareto
 | R6.27 Base Line | SD V4 vs. V10 SWR | Hot PM thin DARC
Ver-10 | BQ34 | LQ30-2E | LQ31-2E
Ver-4 | BQ32 | LQ30-1E | LQ32-1E

## Slide 2: Structure Yield: Comparable
Paramters | Goal | V10 status | Analysis and coment
NOBL | 3.00E-04 | 1E-5~2E-4 wafer mean | comparable to or slightly worse than V4 yield best yield (1E-5) from hot-pm split (LQ31-2E, -4E) ~10X improvement (irrealvent to V10)
BLICS | 1.00E-03 | <1E-3 | comparable to or slightly better than V4 yield
Open | 1.00E-05 | <1E-5 | comparable to or slightly better than V4 yield
Leakage and E1
Paramters | Goal | V10 status | Analysis and coment
leakage | 2uA | < 1.5uA | 80% (lower than V4) leakage at the same Vt trend: varied from run to run; LQ31 splits failed spec requirement. True spec characterization still needed
False select |  | Probe bit map analysis to be developed: consecutive open bits along WL and BL and it's cross points Window budget analysis WIP | 

## Slide 3: E2
Paramters | Goal | V10 status | Analysis and coment
med Vt | 5.45V | 5.25~5.4V | 100-150mV lower than V4 trend: 250mV run to run
Sigma | 130mV | 130~140mV | 10mV improved from V4 (150mV) trend stabilized around 130mV to 140mV
Set Knee | > 3sigma | 2.8~3.3 | match to V4
10min Drift | 100mV | 257mV | 60mV higher than V4; due to ~1 decade earlier on drift clock initialization (~10msec)
ub. Drift rate | < 20mV/dec | 57mV/dec | Same drift rate as V4
slope 1 | < 1KΩ | 0.5~3KΩ | match V4
RMS of slope 1 | <70mV | 65~83mV | Match V4
Ihold |  |  | 
10K yield loss (vs. 10sec ) | < 10% |  | 

## Slide 4: E3
Paramters | Goal | V10 status | Analysis and coment
med Vt | 6.75V | 6.3~6.7V | Similar to Set Vt; ie. No additional integration difference between V4 and V10 (cross contamination)
Sigma | 130mV | 130~170mV | Equal to V4 (150~160mV)
∆VT | > 1.3V | 1.15~1.25 | Equal to or slightly lower than V4 (< 50mV)
True Window | ?? | 320mV | Match or slightly lower than V4; earlier drift clock compensated by better Vt sigma
slope 3 | < 1KΩ | 1~3.5KΩ | match V4
RMS of slope 3 | <70mV | 75mV | Match V4

## Slide 5: Endurance
Paramters | Goal | V10 status | Analysis and coment
Open BER@1E5 | <1E-4 | 2.5E-3@med | Comparable to or slightly worse than V4
¦∆Vt,set@1E5¦ | <50mV | ~250mV@med | Comparable to or slightly worse than V4
¦∆Vt,rst@1E5¦ | <50mV | 50mV@med | Slightly worse than V4
¦∆Vt,win@1E5¦ | 0 | -200mV | Comparable to V4
Disturb
Paramters | Goal | V10 status | Analysis and coment
RD | <1E-3 | 2.5E-2@med | Comparable to V4
TD | <1E-3 | 1E-5~1E-3 | Comparable to V4

## Slide 6: 1us to 10sec @2 sigma window
True window on V4 and V10 are realtvely matched even when VDM is picked for 10ksec drift. Worse Drift and better sigma on V10 offset each other.
E2 knee is >=3sigma for LQ32,1E and LQ31,2E so that is not affecting true window.

## Slide 7: Summary and Recommendation
V10 matches V4 performances.
10 decades yield loss, subject to SET tail degradation, is uncorrelated to V10 integrations.
Window budget characterization needed for centering V10 and V4 thickness target
We should fully exploit V10 capability and capacity to process integration and Probe/backend debug