## Slide 1: SD / Electrode Schottky barrier
Modeling and Silicon data overview
Agrate TCAD team wk5-2014

## Slide 2: Outline
Metal/SD1/Metal band structure
  Dielectric like  fully depleted
  Semiconductor  large trap density in the energy gap
CV check (Dielectric vs Semiconductor)
Schottky SD/Metal model
  Room Temp IV fitting
Carbon work-function?
  CAP vs XPS data (F14)
LOT_ID | Wafer | Thickness | Alloy | Io_PF_1E3cyc | STS_PF_1E3cyc
CLVB212 | 2 | 35nm | C/SD1/C | 2.67E-18 | 9.83
CLVB194 | 17 | 35nm | TiN/SD1/C | 3.22E-17 | 9.04
CLVB194 | 7 | 35nm | TiN/SD1/TiN/C | 8.08E-14 | 5.86
CLV EXP IV DATA (C vs TiN)

## Slide 3: Metal/SD(Ptype)/Metal band structure 1
Fermi level in SD held by the electrode work-function
Hole accumulation in the whole SD layer (if electrode wf is larger than SD one)
SD works as dielectric
SD
(fully-depleted)
E
E
3.0
4.4
SD
stand-alone
1.7
Ebarrier= 0.3 eV
SD Fermi level pinned in the middle of the gap by the traps in the energy gap
Hole accumulation only close to the electrodes interface
Ebarrier does not depend on electrode material
1.7
SD
E
E
3.0
4.4
Depleted region
Ebarrier= 0.85 eV
Acceptor/Donor traps placed uniformly in the gap
(conc=1e21 cm-3)

## Slide 4: Which scenario?  W/SD1/Si (P-) CV
CAPACITOR data compatible only with no traps case
W (Metal) | 
Φ [eV] | 4.55
SD1 (Semiconductor) | 
Eg [eV]* | 1.7
Χ [eV]* | 3.0
ε [1] | 10.5
* Do not toggle the CV curve  none info can be extracted from CV fitting
- 5V
0V
Weaker hole accumulation @ Si/SD interface with traps

## Slide 5: Optical spectra
Absorption optical spectra in agreement with the no traps scenario
GST data shows large traps concentration close to the bands (true also for SD?)
  Need low energy – hi resolution optical spectra on SD1 sample
GST
SD1
ET
DOS
EG
cond
val
No states here
L. Laurin switching modeling 2010
P. Fantini EPCOS 2012

## Slide 6: Schottky model
Assumptions
  SD slightly Ptype semiconductor (EG=1.7)
  No traps in the middle of the gap of SD
  Large traps density close to the valence bands (PF conduction)
  Electrode modeled as metal material (no energy gap)
  SD Fermi level held by electrode work-function (SD fully depleted)
  TiN wf deeper than C one (4.7 vs 4.4 eV  F4 data)*
Conduction Band
Trap band (PF)
C wf
TiN wf
EA C
EA TiN
Valence Band
  * Not in agreement with F14 and lit data  C wf ~ 5.1 eV, TiN wf ~ 4.7 eV
Ebarrier
ETPF
SD
E
E

## Slide 7: CLV ST IV fitting
*No barrier lowering @ SD/TiN interface (its contribute should be negligible since the highest barrier is the SD bulk traps one)
1D mesh
1e3 cycled
Trap band (PF)
Trap band (PF)
Trap band (PF)
Trap band (PF)
Ebarrier
Ebarrier
ETPF
ETPF
TiN electrode
C electrode
SD1 (semiconductor) | 
Eg [eV] | 1.7
Χ [eV] | 3.0
ETPF [eV] | 0.3
ε∞ (PF)[1] | 7.8
C (Metal) | 
Φ [eV] | 4.4
ε∞ (schottky)[1] | 3.78
TiN (Metal) | 
Φ [eV] | 4.7
ε∞ (schottky)[1] | ∞*
Model params

## Slide 8: Carbon Work-Function
C/SD/Si CAP 
W+C/SiO2/Si CAP 
XPS (wrt TEOS) 
C/SD/Si
CLV CAPACITOR DATA
CLV CAPACITOR DATA 1
XPS data

## Slide 9: Schottky model: conclusions
Good agreement between TCAD and EXP IV using the same model parameters for SD1 material (only electrode ones were changed)
Electrode material can toggle the activation energy of conduction
TiN/SD1/TiN STS handled by SD1 bulk PF barrier lowering while C/SD1/C STS by the C/SD1 schottky one
Not in agreement with F14 and lit. material params (C wf deeper than TiN one)
Not able to explain why the post bake carbon sample comes back to the virgin state while the TiN one not
EXP check: Electrode material with deeper work-function should minimize the interface barrier (and thus its contribute to the ST conduction)

## Slide 10: Bonus slides

## Slide 11: SD Optical characterization

## Slide 12: SD1 POR Optical Characterization
Experimental
  25,50,75nm on 100Å oxide and silicon
  KT F5 (OXMEAS1)
    Wider but noisier in IR region
  KT SpectraFX (OXMEAS11)
Low rough./native contrib.
  Low confidence on quantification: <7Å
  Consistent with low oxidation (XPS)
Models
  Tauc-Lorentz (4 parms , off-line model)
  Lorentz 2xHO (7 parms., in-line/off-line)
    Eg=1.77±.01eV (s 13pts/6wfs)
Chart: Energy (eV)
| 2.6666666666666665 | 2.6382978723404289 | 2.6105263157894742 | 2.5833333333333366 | 2.5567010309278349 | 2.5306122448979602 | 2.5050505050505047 | 2.48 | 2.4554455445544527 | 2.4313725490196068 | 2.407766990291262 | 2.3846153846153837 | 2.3619047619047642 | 2.3396226415094339 | 2.3177570093457938 | 2.2962962962962972 | 2.2752293577981653 | 2.2545454545454544 | 2.2342342342342341 | 2.2142857142857144 | 2.1946902654867255 | 2.1754385964912277 | 2.1565217391304352 | 2.1379310344827602 | 2.119658119658113 | 2.1016949152542375 | 2.0840336134453792 | 2.0666666666666669 | 2.0495867768595071 | 2.0327868852459017 | 2.0162601626016237 | 2 | 1.9840000000000009 | 1.9682539682539701 | 1.952755905511814 | 1.9374999999999993 | 1.9224806201550397 | 1.9076923076923071 | 1.8931297709923658 | 1.8787878787878807 | 1.8646616541353378 | 1.8507462686567182 | 1.837037037037037 | 1.8235294117647058 | 1.81021897810219 | 1.7971014492753621 | 1.7841726618705065 | 1.7714285714285725 | 1.75886524822695
TL a | 695.0658 | 674.5293 | 654.3371 | 634.4812 | 614.9546 | 595.7501 | 576.8597 | 558.2766 | 539.9937 | 522.0047 | 504.3021 | 486.8799 | 469.7308 | 452.8497 | 436.2299 | 419.8652 | 403.7497 | 387.8773 | 372.2425 | 356.8405 | 341.6652 | 326.7115 | 311.9741 | 297.4482 | 283.1288 | 269.0104 | 255.0899 | 241.3613 | 227.8213 | 214.4649 | 201.2885 | 188.2874 | 175.4595 | 162.7982 | 150.303 | 137.9676 | 125.7908 | 113.7693 | 101.8999 | 90.1799 | 78.6067 | 67.1784 | 55.8911 | 44.7442 | 33.74 | 22.8694 | 12.142 | 1.595 | 0
Chart: Wavelength (nm)

## Slide 13: SD0 – SD1 comparison
SD1 has lower n and k
Higher Eg
  1.77eV vs ~1.2eV
Follow up
  New alloys characterization
    2 thicknesses on Si
  Capping
  Inline monitor of SD1
Chart: Wavelength (nm)
Chart: Energy (eV)
SD0
SD1

## Slide 14: SD CAPACITOR DATA
CLV CAPACITOR DATA (PFantini)
CLV CAPACITOR DATA 1 (PFantini)

## Slide 15: W/SD/Si capacitor
CLV-Capacitor with PAD mask
Native P-type Si substrate

## Slide 16
Si/SD/C
We are improving the structure terminating the Carbon electrode with a Tungsten layer that should drive the signal on the entire capacitor area
W
JAP 90, 2024 (2001)
a-C with higher and higher amount of sp2 (up to 70%)
WF measured via field-emission
Non-quasi-static effects are expected for the Carbon film resistance
The ‘effective area’ explored decreases with frequency
C/SD/Si capacitor