## Slide 1: SxP Device Physics
Phase Change
Structure and band diagram to illustrate the origin of conductivity of a chalcogenide material.
Evidence of phase change from thermal hysteresis.
Power delivery with pulse to change phase
Physics and model of phase change in SxP technology (electrode is the heater)
Threshold Switching
Structure and Band diagram of a SD devices, electrode included.
Subthreshold conduction is a Poole-Frankel emission process
Space charge injection delocalizes, the mobility gap decreases and carriers multiply at cathode as device biased in near threshold.
Carrier multiplication at both electrodes is the positive feedback mechanism leading into threshold, snapback as shown in negative differential resistance regime.
On-state is due to carrier injection (tunneling) from both electrodes. Injected carrier recombine in the bulk or drift through to other electrodes.

## Slide 2
PM
SD
TE
ME
BE
Acceptor-like
localized states
Ec
Ev
Ef
E
CB
VB
10% structural vacancies result in localized states near LP band
Over- and under-coordinated Tellurium lead to defects/traps
Amorphous
Crystalline
Acceptor ( C1- )
Ec
Ev
Ef
E
CB
VB
Donor( C3+ )
LPTe ( C20 )
LPTe

## Slide 3
(120nm)2
(45nm)2
J [A/nm2]
V [Volts]
Bottom
Electrode
Top
Electrode
TE
BE
TE
BE
SubThreshold
PFE conduction
BE
TE
Neal Threshold

## Slide 4
Bottom
Electrode
Top
Electrode
TE
BE
40s/SD2’/40s
20s/SD2’/60s
30s/SD2’/30s
502 nm2 Cell
J [MA/cm2]
48
32
16
64
V [Volts]
BE
TE
(1)
(2)
(3)
(4e)
(4h)
(5)
(6)
(7e)
(7h)
Threshold,
Snapback, NDR Regime
(1)
(2)
(3)
(1)
(4)
(2)
(4)
TE
BE
(3)
On-state
(2R)
(2R)

## Slide 5: Sub-threshold I-V is a Poole-Frankel Emission
(120nm)2
(45nm)2
J [A/nm2]
V [Volts]
nm
nm
nm
Sub Threshold: Experimental validation of trap hopping conduction behavior; EA matches ½ of optical bandgap
Near threshold: Due to space charge injection exponentially as the Poole–Frenkel effect delocalizes, tail states increases; the mobility gap decreases.

## Slide 6: Threshold Switching is a current density triggering event: Refute prior bulk model of filamentation subject to electron-phonon interaction or band to band tunneling
JTH [A/cm2]
VTH [Volts]
15nm x 15nm Cell
23nm x 30nm cell
38MA/cm2
43MA/cm2
33MA/cm2
110uA
125uA
55MA/cm2
110uA
97uA
43MA/cm2
Other evidences of threshold switching an current density triggering but not a critical field event 1) VTH is linear scalable but ETH is not a constant per thickness experiment; 2) JTH is constant from 25℃ to 120℃ (with subVt conductive EA=~1eV); 3) JTH depends on electrode (Mo vs. C on αPM2 with identical SubVt I-V)
Delocalized carriers multiplied
near interface in Electrode
Threshold Point Characteristics
per Cycling Effects

## Slide 7: On-State and Speculative Models Early Phase of Model Development, with a focus on Electrode/Bulk Interaction
Melting TempPM
1.2
1.4
V[Volts]
20
12
4
J [MA/cm2]
Various Electrodes (𝛒)
NDR: ∆VT,SD ↘ as J↗
20
12
4
J [MA/cm2]
.5
1
1.5
V[Volts]
Electrode only
Electrode + SD
Negative Differential Resistance Regime: High potential carriers leaving SD mobility edge falling on electrode multiply at Interface; EHPs are generated and E-field push the charged particles as a positive feedback mechanism; The excess carriers fill the traps forming a sharp and narrow tunneling barrier at both interfaces, collapse the voltage cross the SD bulk; the current controlled S-type NDR leads dual carrier conductions in on-state; Energy dissipation similar to Joule-heating effects (evidence on melting of PM) Still need to validate the evidences on E-H recombination by Vezzoli et.al. [JAP 45 (1974)]
Experimental evidence of sustainable current density > 200MA/cm2 for > 10sec using un-confined structures (intrinsic)