## Slide 1: SSM Update to JDP COMM
Apr/4/2018
Status and Plan:
Improving confidence on composition tuning
  Monolithic target (SD.K1) match Alloy6 (POR) expectation (RWB gap to goal 430mV).
  Lot SSM43 (K* campaign expansion) delivered 400~450mV median window improvement; SD.K2 definition confirmed, detailed RWB and reliability characterization to be followed.
  Additional first cut module improvement in E1/C1 etch required for robust structure health.
Dual Deck lead lot on screamer in D0 array via/CMP module on track to begin D1 targeting for WW14. D0 probe WW15. DD probe WW18-20.
S24S bipolar decode and polarity logic completed. Initial layout fits under tile, routing in progress. Overall on track to rev2 in WW19 and DBR in WW39.
Stepping-up Strategies and milestones defined to exit pathfinding
  Solid fundamental of SSM switching mechanism using SR71
  Statistical validation with S24S
  Technology/Design/Collateral for Alpha product Development
  Product/Technology scaling direction beyond Alpha product

## Slide 2: K* SD Alloy / CR5.3 Learning
Baseline (CR5.3): SD.K1 monolithic target initial results close to expectations (within 20mV from POR Alloy6), despite composition offset (~2%)
  Volume read data populated WW14-15 for lot-to-lot var. components
Cell Roadmap: K* SWR (SSM43) demoed median DVt close to DTS.
  WLR to vet residual gap & pre-POR selection (WW14)
Structure Health: K* alloys require additional work at E1/C1 etch
  E1 converted to Higher Ar flow (+ sputter)
  C1 UE fix for structure yield is expected to be probed WW15
  1st CR5.3 Dual-Deck read expected in WW18-20
DTS goal
Alloy6
SD.K2
CR5.3
SD.K1
DVt (1 ms)
Normal Quantile [1]
SR71 1D0 Cell RWB (Piecewise Built) S26A1 silicon (Neg Read) |  | Alloy6 CR5.3 85C [mV] | SD.K1 CR5.3 85C [mV] | Alloy14 CR5.3-based 85C [mV]
Vmd1 | DVt (1 ms) | 935 | 915 | 1340
 | SET s (Vt) | 85 | 85 | 92
 | RST s (Vt) | 101 | 100 | 120
 | SET drift (1 ms-10 s) | 220 | 220 | TBD
 | E3 GB WE | 95 | 95 | 95
 | E3 GB RD | 0.3 | 0.3 | TBD
Vmd2 | Rst drift (1 ms-3 s) | 245 | 245 | TBD
 | Set drift (10 s-48 h) | 320 | 320 | TBD
 | Gap to goal | -415 | -430 | > -95 (prj)
VT [mV]
Monolithic
Target
SD.K1
POR
Alloy6

## Slide 3: S24S Design Update
Design of bipolar decode and polarity logic complete / updates to ccell logic complete
Initial layout of new under tile circuitry fits under tile / routing updates in progress
Energy/performance impacts of new circuitry up next
On track to rev2 in WW19 and DBR in WW39
Milestone | Criteria
Rev 2 | Sheet level performance validation complete / circuits ready for layout
Rev 3 | Full chip functional and performance validation of features, specifications and test modes
DBR | Database Ready for Manufacturing
B1
B1
B1
B1
B0
B0
B0
B0
W1
W1
W1
W1
W0
W0
W0
W0

## Slide 4: SSM Pathfinding Strategy and Milestones
3D-stack
The strategy for ‘fast fail or succeed’ is built on ‘stepping-up’ is
SR71 – SSM basics switching mechanism and its reliability, symmetry and scalability
S24S – Dual deck array feature development with high volume statistical validation.
Build alpha product – Design, process and collateral initial development in order to pick an array node for die size and performance matching or better than SXP counterpart.
Develop Scaling Roadmap –
  Cost and performance: 2X density and ½ energy every generation.
  Array Architecture: Stack (SXP-like) vs. Tier (3D NAND like)
3D-tier
Deliverables for “step up” or not