## Slide 1: Vth evolution by ED
A1 reliability data
Enzo

## Slide 2: Summary
A1 lot 0173982
CD-- straight profile @WL
Reliability done on neg reading polarity
Trial | SD thk. | Ge% | As% | Se% | In% | Si% | 51 WL etch | Wf
1C | 22 ver12 | 13 | 30.4 | 48.6 | 2 | 6 | CD - - | 13,17,24
2E | 22 | 16 | 28.6 | 50.4 | 5 | 0 | CD - - | 18,20,23
3E | 22 | 16 | 26.6 | 50.4 | 7 | 0 | CD - - | 14,19,22
4E | 22 | 18.5 | 25.6 | 48.9 | 7 | 0 | CD - - | 15,16,21,25
Old POR
Best
window

## Slide 3: Best Window budget, ED4 only, 16k cycles: split 4E (85C time evolution)
Old POR with lamina
Split 4E, k*alloy
150mV only gap to cover 1us 3days @85C with single Vdm with 3.54 sigma defectivity
No issue on E1/E4 but need to extend visibility up to 4 sigma
No reset read disturb budget in this calculation but single VDM will improve also reset read disturb
Vdm1
Vdm2
E1
E2
E3
E4
Window closure @ 100s

## Slide 4: Full tile endurance (1k vs 128k, 135us IPD) : split 4E (260kb)
Pre drift distribution (1us delay)
Post drift distribution (1s delay)
Some high Vth tail appears (both E2 and E4) after 4 sigma statistic (one bit)
Huge Vth shift on upper part of set distribution non impacting RWB
400mV

## Slide 5: Tile map schematic, mean access resistance for each block [kOhm]
Block 15 – 11 show E2 / E4 tails related to 1 bit
(Low ED but not minimum)
BL driver
WL driver
BL number
WL number
BL driver
WL driver
Block 0-0 is the reference for probe

## Slide 7: Full map @ 1kCycles (median set Vth by block, 1us delay)
BL driver
WL driver
BL number
WL number
BL driver
WL driver
BL driver
WL driver
Good match with access resistance map

## Slide 8: Median Set delta Vth evolution map (1k128k Vth delta)
Some seasoning asymmetry visible at 1us, fully symmetrical at 1s delay following access resistance

## Slide 9: Median Set Vth by access resistance
Vth shift after cycling increase with ED

## Slide 10: Set Robust sigma maps

## Slide 11: Set Robust Sigma by access resistance [kOhm]
No big trend of robust sigma vs ED pre drift
[kOhm]

## Slide 12: Accelerated seasoning trial: WSiN removal (0176312)
Without WSiN we get lower Vts (faster seasoning). Major toggle is with WSiN @BL
Vt shift 1k128k cycles is much smaller for no WSiN @BL, consistent with a more effective 1k seasoning
Vt shift 1k128k cycles
SET
RESET
Median Vt
1k cycles
128k cycles
1C
2E
3E
4E
Trial | Cell stack | WSiN @ WL | WSiN @ BL
1C | 22nn ver12+2% In + T&B AlOx | Yes | Yes
2E | 22nn ver12+2% In + T&B AlOx | No | Yes
3E | 22nn ver12+2% In + T&B AlOx | Yes | No
4E | 22nn ver12+2% In + T&B AlOx | No | No
1C
2E
3E
4E
1C
2E
3E
4E
1C
2E
3E
4E
Mattia R. data

## Slide 13: Extended endurance on selected blocks along BL direction (different EDs)
Block 0,0
( BL near, WL far)
Block 7,0
( BL mid, WL far)
Block 8,0
( BL mid, WL near)
Block 15,0
( BL far, WL near)
BL driver
WL driver
WL driver
BL driver
+40% increase BL resistance

## Slide 14: Extended endurance on split 3E (No WSiN @ BL)
Block 0,0
( BL near, WL far)
Block 7,0
( BL mid, WL far)
Block 8,0
( BL mid, WL near)
Block 15,0
( BL far, WL near)
35k R access
21k R access
21k R access
35k R access
No tails up to 4M cycles for cells not near to decoders

## Slide 15: Median set and reset Vth and robust sigma evolution
Block 0,0
( BL near, WL far)
Block 7,0
( BL mid, WL far)
Block 8,0
( BL mid, WL near)
Block 15,0
( BL far, WL near)
35k R access
21k R access
21k R access
35k R access

## Slide 16: Median delta Vth shift: Reduced turnaround
35k R access
Block 0 old ref
21k R access
Block 0,0
( BL near, WL far)
Block 7,0
( BL mid, WL far)
Block 8,0
( BL mid, WL near)
Block 15,0
( BL far, WL near)
Main trend with total access resistance, BL decoder distance show some asymmetry vs WL
Need to decrease line resistance

## Slide 17: Window evolution vs ED
Window evolution strongly dictated by set seasoning

## Slide 18: Backup

## Slide 22: Median Vth [mV] set map

## Slide 23: Vth shift on typical block 0,0
Typical shift of 200mV on std block used at probe (0,0)

## Slide 24: Edge block focus, 1us delay
Small and high EDs maintain +/-150mV delta with respect to median after 128k cycles

## Slide 25: Edge block focus, 1s delay

## Slide 26: Robust sigma maps

## Slide 27: Set Vth vs BL and WL access resistance (high ED)
BL driver
WL driver
BL number
WL number
BL driver
WL driver
Higher sensitivity moving along BL for high total access resistance

## Slide 28: Set Vth vs BL and WL access resistance (low ED)
BL driver
WL driver
BL number
WL number
Higher sensitivity moving along WL for low total access resistance
BL driver
WL driver

## Slide 29: Median set Vth by ED: drift focus

## Slide 30: Set robust sigma vs ED: drift focus

## Slide 31: Set relative sigma by ED

## Slide 32: Full tile distributions (All EDs) : die screened from leakage test
SSM, 1k cycles, 4.5 sigma max statistic
Very good gaussian distribution for split 4E, no defectivity tails visible at single bit level. 128mV max sigma pre drift due to all ED convolved together (no dedicated differential seasoning)
Split 4E, SD only
S15C, cell rev 7.64. PG1T1 die
9889922, wf 25,
SXP full stack, 1Gbit statistic, full tile distribution after seasoning and after cycling
1us interlaced histo, distortion from gaussian
125 mV best set sigma pre cycling on SXP
120mV/
sigma
128mV/sigma

## Slide 33: Full tile distributions (All EDs)
Shorts filtered
Old POR with lamina
Split 2E
Very good Gaussian shape for full tile map on new POR once shorts are filtered out. Sigma are increased with respect to ED4 block typical values:
115mV/sigma on set (it is 85mV on typical ED4 block)
130mV/sigma on reset (it is 100mV on typical ED4 block)
130mV
/sigma
115mV
/sigma

## Slide 34: Cross tile components vs ED @ 85C (old POR): No spike inhibition
Robust sigma trend by access resistance [mV]
Vth trend by access resistance[mV]
1k cycles
128k cycles

## Slide 35: High window splits cycling evolution: 2E vs 4E (ED4)
Split 2E
Split 4E
84mV/sigma
EOL
105mV/sigma
EOL
No defectivity appears up to 6M cycles also for split 4E
Very good sigma stability after 6M cycles

## Slide 36: Set / Reset median delta Vth evolution (ED4)
Best performances for split 4E in term of window and Vth evolution shift
200 mV