## Slide 1: Updates from literature
Recent IEDM papers and one Science paper
Paolo

## Slide 2: Some highlights from recent papers
IEDM 2017
IBM/Macronix
on SD
F. Rao et al., Science 358, 1423 (2017)
IEDM 2017
Imec
on SD
Link

## Slide 3
They characterized the TeAsGeSi (TAGS – Ovshinky glass) also in the Se-doped version
Claim: Excellent endurance (>1010 with 50ns-pulsed 400uA On-current)  Note: this current for an unconfined device with 350nm as Bottom electrode is nothing  >300 times the area of our 20 nm cell
‘Old’ Paper with respect to our knowledge
The only significant information comes from the EDX difference between the Virgin and Formed device:
  No-segregation
  A difference in the density is highlighted

## Slide 4
On the GexSe(1-x) system:
  Mobility gap defects related to mis-coordinated Ge
Physics of Switching: Electric field modifies the atomic orbitals tending to localize/de-localize the gap states (Stark effect) and leading to the abrupt increase of the conductivity

## Slide 5: Reducing the stochasticity of crystal nucleation to enable subnanosecond memory writing (2/2)
Sb2Te3 doped with ~4% Scandium (Sc) is found to improve the SET speed down to ns
A very similar methodology to the one we used for Y:GST where the crystallization velocity is related to the presence of stable 4-fold rings in the amorphous phase acting as crystalline precursors:
  The larger is the fraction of 4-fold rings the faster is the nucleation
Comment: Doubt about the ability to reach the sub-ns scale with a wide test-structure

## Slide 6: Reducing the stochasticity of crystal nucleation to enable subnanosecond memory writing (1/2)
Authors consider the wide class of TM as dopants
Their screening scorecard based on:
  Presence of 4-fold rings in the a-structure of TMT (TM-tellurides) that geometrically match the rock-salt crystalline Sb2Te3
  Strong TM-Te bonds (to get robust crystalline precursors)
  Among the class of TM only Sc and Y are found to show chemical bonds of high strength with Te
  Sc is found to show a better geometric conformability criterion wrt Y
Sc and Y build similar bonds
Sc appears most appealing since the better geometrical fitting with Sb-Te bond length
Suppl. Info Link

## Slide 7: Some notes about Sc-GST
Sc and Y are close in the PT - III gr of TM
Simulated Partial Density of states (Sc d-states) for Sc-doped Ge2Sb2Te5 by Elliott’s group [link]
  Dashed-lines  amorphous phase
  Solid line  crystalline phase
We privileged Y, since calculations on Sc-GST lead to the suspect that Sc could close the BG instead of widening it
Thus, we de-prioritized it
Anyway, at the light of this Science work Bernasconi is going to check the band-gap thru the Tauc plot also for Sc-GST (Readout ~ wk12)
EF