## Slide 1: Vth evolution by ED
A1 reliability data
Enzo

## Slide 2: Summary
A1 lot 0173982
CD-- straight profile @WL
Reliability done on neg reading polarity
Trial | SD thk. | Ge% | As% | Se% | In% | Si% | 51 WL etch | Wf
1C | 22 ver12 | 13 | 30.4 | 48.6 | 2 | 6 | CD - - | 13,17,24
2E | 22 | 16 | 28.6 | 50.4 | 5 | 0 | CD - - | 18,20,23
3E | 22 | 16 | 26.6 | 50.4 | 7 | 0 | CD - - | 14,19,22
4E | 22 | 18.5 | 25.6 | 48.9 | 7 | 0 | CD - - | 15,16,21,25
Old POR
Best
window

## Slide 3: Best Window budget, ED4 only, 16k cycles: split 4E (85C time evolution)
Old POR with lamina
Split 4E, k*alloy
150mV only gap to cover 1us 3days @85C with single Vdm with 3.54 sigma defectivity
No issue on E1/E4 but need to extend visibility up to 4 sigma
No reset read disturb budget in this calculation but single VDM will improve also reset read disturb
Vdm1
Vdm2
E1
E2
E3
E4
Window closure @ 100s

## Slide 4: Extended full tile cycling : 2M FW
1us W2R delay
1s W2R delay
Very small defectivity tail appear after 2M FW above 4 sigma level!
No additional cross tile modification after 128k cycles

## Slide 5: Resistance / Capacitances
WL Res=4.2 Ohm/sq
BL Res= 6 Ohm/sq
BL Res= 6 Ohm/sq
WL Res=4.2 Ohm/sq
WL Cap=7aF/cell/side
WL Cap=6.2aF/cell/side
WL total cap=30 fF
BL total cap=26 fF
BL Decoder capacitance ~ 40 fF
WL Decoder capacitance ~ 9 fF
Numbers from Hernan and Jeremy:

## Slide 6: New resistance calibration check: split 4E
Total access resistance for each block [kOhm]
Median set Vth by block position

## Slide 7: Is ED the only variable for Vth evolution?
Lower Vth toward center of tile
[kOhm]
Tile effect only, same ED

## Slide 8: S26 vs SR71B: Line are driven from middle vs edge
WL0
WL0
WL0
BL0
WL0
WL0
WL0
WL0
WL0
BL0
WL0
BL0
WL0
BL1
WL0
WL0
WL0
BL1
WL0
WL1
WL0
WL1
WL0
BL0
WL0
WL1
WL0
BL1
WL0
WL1
WL0
BL1
Consider this cell on WL0 and BL0
In S15C the worst case was 3k (2k BL + 1k WL)
In S26C the worst case is 3.5k (2k WL + 1.5k BL)
S26 (Tony sketch)
SR71B
Worst case is still the same (2k + 1k)

## Slide 9: Spike vs tile position model (one decoder very close)
Min ED / max discharge
WL dec (7.2V)
BL (0V)
Med ED / lower discharge
WL decoder (7.2V)
BL (0V)
2R
R
R
R
Spike increase going toward center of WL
Spike increase going toward center of BL
R= 1k cells
Tile effect + decoder effect are added (ED change)
Intra tile contribution

## Slide 10: Spike vs tile position model (one decoder far)
WL dec (7.2V)
BL (0V)
WL dec (7.2V)
BL (0V)
2R
R
R
2R
Spike decrease going toward center of WL
Spike decrease going toward center of BL
R
2R
2R
Tile effect + decoder effect are subtracted (ED change)

## Slide 11: Moving along WL
260mV total delta
(tile and WL decoder contribution add)
80mV total delta
(tile and WL decoder contribution subtracts)
A
B
C
simulated EDs
NEXT SLIDE

## Slide 12: Moving along WL Cell current and charge during WRITE
Reverse WRITE
85C
VAPPLY = 7
VMID = 3.5
Target Write current = ~42uA
Pre-write Vth = 5.4v
VHOLD = 2.5v
1aF parallel with cell model
44ns
Charge
Current
ED of WL | Q (0s1ns) | Q (0s44ns)
A (full) | 103.6 fC | 1.98 pC
B (3/4) | 112.0 fC | 1.99 pC
C (1/2) | 121.1 fC | 2.01 pC
1ns
~1ns zoom in
Jeremy H.

## Slide 13: Moving along BL
280mV total delta
(tile and BL decoder contribution add)
150mV total delta
(tile and BL decoder contribution subtracts,
BL decoder cap seems to dominate)

## Slide 14: Conclusions
Vth evolution mainly driven by total ED (distance from decoders)
Secondary effect (spread of correlation plot) is given by intra-tile capacitance that can add or subtract to decoder capacitance
The secondary effect generally is not visible on S15C or S26A because lines are driven from the middle, so decoder contributions (ED) generally is added always to intra-tile contribution
In any case spike mitigation on both selection polarities is strongly recommended for S24S vehicle (main variable to control spike aka Vth evolution during product operation)

## Slide 15: Backup

## Slide 17: Cross shape in Vth topology ( same nominal ED )

## Slide 18: Cut along same Vth

## Slide 19: Tile map schematic, mean access resistance for each block [kOhm]
Block 15 – 11 show E2 / E4 tails related to 1 bit
(Low ED but not minimum)
BL driver
WL driver
BL number
WL number
BL driver
WL driver
Block 0-0 is the reference for probe

## Slide 21: Full map @ 1kCycles (median set Vth by block, 1us delay)
BL driver
WL driver
BL number
WL number
BL driver
WL driver
BL driver
WL driver
Good match with access resistance map

## Slide 22: Median Set delta Vth evolution map (1k128k Vth delta)
Some seasoning asymmetry visible at 1us, fully symmetrical at 1s delay following access resistance

## Slide 23: Median Set Vth by access resistance
Vth shift after cycling increase with ED

## Slide 24: Set Robust sigma maps

## Slide 25: Set Robust Sigma by access resistance [kOhm]
No big trend of robust sigma vs ED pre drift
[kOhm]

## Slide 26: Set Vth vs BL and WL access resistance (high ED)
BL driver
WL driver
BL number
WL number
BL driver
WL driver
Higher sensitivity moving along BL for high total access resistance

## Slide 27: Set Vth vs BL and WL access resistance (low ED)
BL driver
WL driver
BL number
WL number
Higher sensitivity moving along WL for low total access resistance
BL driver
WL driver

## Slide 28: Median set Vth by ED: drift focus

## Slide 29: Cross tile components vs ED @ 85C (old POR): No spike inhibition
Robust sigma trend by access resistance [mV]
Vth trend by access resistance[mV]
1k cycles
128k cycles