## Slide 1: SSM process development update
ww1812

## Slide 2: WIP status update
    SSM43 K* wave3 shows periphery failures – unexpected on the groups that ran the same alloys as on wave2 – segmentation in progress; Replacement will be needed, overall delay of 3 weeks on K* wave3; SSM44 (second lot of wave3) also is past C1 chop and might have to be replaced (the x-sections pending)
    Current process with 2nd cut Nitride cap shows high level or periphery shorts (SSM42); Potential recovery with CSOD + UV cure (SSM47)
    52 etch improvement for yield issues mitigation on 55nm E: SWL/E1 knee – SD under-etch; BL-BL – CD targeting (SSM46; SSM48)
    DD setup lot (SSM50) started at Fab4 ww12

## Slide 3: SSM43 (K* wave3 lot1)
PFA
Partition18
Partition14
Partition17
Partition13

## Slide 4: Campaign K* alloy14 (SD.k2 candidate) E1 etch
SSM POR E1 etch
SSM POR E1 etch +40% time
SSM POR E1 etch +60% time;
Higher Ar flow (+sputter)
    In rich alloys had trouble to clear at E1 etch and significant etch time/conditions adjustment was required;
    Need follow up on C1/C2 etch;
    51-52 etch x-sections are expected from PROD K* lots

## Slide 5: SSM43 (K* wave3 lot1) 51 ecth
CR5.3 baseline
K* alloy26
K*26,27
CR5.3 w/wo AlOx
K*26,27

## Slide 6: S26A- 0024692.003
Contacts: baalbertson,kyastreb
F4 RDA
SWR # 8658504
ww1731 -- S26A SSM Campaign K*, SS4
S26A- 0183082.003
SWR # 9224304
ww1809 -- S26A SSM Campaign K* wave3, SS7
VS

## Slide 8
65VIANITCMP WL-WL SHORTS
Comments: with exception of 3082-03, maps are accurate. Center shading from 3082-03 shows multiple shorts within field of view (example far right) indicating this region is massively shorted and map is not reflective of the true shorting counts. Typically inspection shorting defect look like example near right.

## Slide 9: Lot 0177752
SD: K1
Group 1C: wafer 03 W=45nm; SD=25s (AUTOSTEM link)
Group 2E: wafer05 W=55nm; SD=25s (AUTOSTEM link)
YAOJIN

## Slide 10: Inline measurement
SEM measured CD:
55nmW CD is ~1.8nm bigger than 45nm W
55nmW CD profile is different than 45nm W

## Slide 11
45nm W
55nm W
CoW
EoW
CoW
MoW
EoW
YAOJIN

## Slide 12: XSEC measurement- W CD
YAOJIN

## Slide 13: SD CD measurement
YAOJIN

## Slide 14
C2CHOOXIDEP Micro Inspect
Comments: we are seeing high percentages of blocked etch on the reviewed defects of the nitride cap wafers, 0177752.003-02E and 0134702.093. however defect counts are significantly lower on 0134702.093. these defect counts are ~ 3X of SxP baseline -> much more comparable to SxP baseline than SSM baseline. SxP baseline has also seen comparable blocked etch percentages @ this inspect.
0177752.003
0134702.093
CSOD+UV +nitride cap
CSOD+UV +nitride cap
oxide cap
CSOD no UV nitride cap
SSM47
EHSMITH

## Slide 16: 51 DE movie x-sections (CR5.3)
Post 51 FP etch + Liner dep
Post 51 LP etch
    Tapered SD profile results in liner run out at LP etch
    Liner protection remains on SD top (see the dashed line on the image), while SD bottom is narrowed by W etch
    Pre-liner DEP SD profile optimization will be required

## Slide 17: PI alignment – housekeeping rules
SWR setup/ownership:
  Use one SWR per experiment lot (all deviations in one SWR); SWR owner is responsible for the whole setup (not just in the module of ownership);
  Only one additional SWR allowed – block SWR for baseline process if not set by GeRM
  Preserve SWR naming convention
GeRM setup:
  All reasonable effort should be invested into GeRM setup to avoid misprocesses as number of lot/SWR owners grows;
  PROD block SWR is the last resort, only one block (no copies to a separate block SWR)
Module ownership:
  In addition to ownership of development in the module, please invest some time to expedite PROD WIP (mitigate holds, long idle times, un-necessary metro)
  Request DEV material (Kyle owns/coordinates DEV starts)