## Slide 1: K* campaign synopsis from both SR71 (SSM) and S26 data
Deeper insights, expectations and further directions
Contributes from Materials Team, SSM Team and Array Team

## Slide 2: K* campaign: In-SAG and In-SiSAG systems exploration
5 Lots processed for this exploration
  Note: first 2 lots were of poor quality as a consequence of the integration with larger CD (CD- instead of CD--) which lead to periphery yield loss  thus neglected from this S26 summary
All lots run following the SD-only flow with 22 nm thickness and SD liner-protected
Metrics used for the SD alloy assessment:
  L0 metrics (Thermal stability and band gap, mainly)
  Structural yield
  Forming
  VT Sigma
  Drift
  SSM window
  Leakage
  Memory Effect
  Endurance (VT stability thru cycling)
Cross-check between the two vehicles (S26 and SR71) always done, when possible

## Slide 3: Fundamentals of K* campaign: Towards a Treasure Map of the In-SAG based SD3 (including also In-SiSAG)
4C chamber configured with: As2Se3, In2Se3, Ge and Si
  Main campaign: In-SAG exploration; Si thought just to mild possible Indium drawbacks (like leakage)
  Note: when In increases As/Se decreases
Main open question: what is the maximum In% we can tolerate w/o segregation and leakage issues?
As/Se vs Indium correlation
In
As
0-11% In skew
SD1
Si
SDK1 – SSM Pre-POR
w/ 5% In and 16% Ge
Max In% to manage integration and leakage?
Max Ge% to control Drift?

## Slide 4: L0 metrics: Thermal stability and Band gap
Thermal stability largely governed by Ge content
SEM Wrinkle
Eg
Optical Eg lowers with higher Indium and Ge (more so with Ge than In)
by Swap
Ge
Ge
In

## Slide 5: Structural yield (intrinsic and extrinsic)
Structure Opens
by Lidia
by Lidia
Si increase on In-SAG matrix degrades Opens
In increase degrades vertical leakage after cycling
5% In appears safe; 7% needs deeper assessment
  PFA running on to segment the nature of vertical shorts/SWL
Warnings about alloys with CN < 2.674
Take-away:
2%
11%
9%
9%
5%
7%
7%
In%
No Si
Plot vs CN?
Opens BER after filtering from laterals
Lowest CN – Lowest Tg

## Slide 6: Sigma VT trends
In-SAG: ~20% Normalized SET sigma improvement w/ 5%
Worsening w/ Si
No clear worsening from 5% to 7-9%
  Carefully evaluate L2L
Normalized 10s Sigma vs In
S26
~ 20% improvement w/ 5% In
sVT sigma for SDK1 can be as low as 90 mV
w/ 4% Si
In-SiSAG
In-SAG shows the best sigma on both vehicles: S26 and SR71

## Slide 7: Drift trends
Not clear trends from S26
Notes:
  Indium (as Si) mitigates Drift
  InSAG comparable or worsen than SiSAG
  Possible worsening could be associated to the usual Drift-VT correlation
Same alloy SDK1 on 2 different lots
S26
PG4 test
3hrs Drift vs VT
POR
5% InSAG
S26
PG4 test
Typical trend w/ Ge

## Slide 8: Memory Effect
Memory Effect clearly trends with In content
SDK1 alloy reaches 350 mV
A trend in the decrease direction captured with Ge increase
A bell shape w/ maximum and a loss of the effect thru cycling
Memory Eff. Vs cycling
All ED mixed
by MattB

## Slide 9: SSM window trends
SSM VT window is increased with the addition of Ge% or In%
Best correlation found with total As%
Target window can be reached in the region around 20 As%
As/Se vs Indium correlation
Goal
SDK1 – SSM Pre-POR
w/ 5% In and 16% Ge

## Slide 10: Leakage trends
+25%
  Leakage increase with Indium not so critical (within 25%)
S26

## Slide 11: Endurance: some signals
  Preliminary from WLR
  More exhaustive result from bench will be available
  SDK#6 presents some advantages wrt SDv12+In:
  Smaller degradation of VT median with cycling
  Less pronounced turnaround
  Signal to be checked on the other lots
S26 - WLR

## Slide 12: K* camp: Key messages
Main upsides of the In-SAG matrix:
  FF reduction  ~1V lower
  Lower sigma  down up to 90-100mV
  Higher SSM window  up to 0.5 V gain
  Higher Memory Effect  upsides ~100mV
  Reduced VT shift w/ cycling  reduced degradation and turnaround
Also some warnings arise from the K* lots analysis:
  Drift performances not clear  it could be stable or degrade
  The intrinsic/extrinsic weakness of In-SAG alloys with In>7%  PFA running on
  The leakage increase with Indium (not critical, within 25%)
In-SAG alloy likes for SSM applications and, potentially, for 30S SxP scaling:
  K* campaign allowed finding the new pre-POR (SDK1) pure In-SAG alloy for SSM
  At first order approximation it is as SDv12 where Indium substitutes Si and lower As/Se ratio

## Slide 13: SSM perspectives and Plan
SDK1 monotg installed in the 3C to foster:
  learning about montg fabrication and stoichiometry mapped on Si
  assessment the role of AlO2 lamina on integration and performances w/ In-SAG
Possible SDK2 monotg from SD K* 2nd run  decision wk#9-10
E* target (close to GeSe4 w/ 5%As) installed in the 4C chamber to:
  segment the role of As reduction on In-SAG (that will be further explored w/ G* camp w/ fixed 5%In 3C)
  run the 3rd K* trial in order to maximize the SSM window by higher In and Ge
Recommendations:
EDX on In-SAG for both transformation function learning and to understand how segregation modulates SSM window
Deeper reliability characterization on In-SAG alloys to assess the alloys robustness
Campaigns Gantt

## Slide 14: SiSAG vs In-SAG/In-SiSAG benchmarking for SxP
Under the below assumptions (supported by the experimental picture reported in the previous slides):
  Sigma VT gain ~ 100 mV
  Memory effect gain ~ 100 mV
  Same Drift
200mV RWB gain thru the substitution of SiSAG with In-SAG can be computed
This gain can be transferred in -7nm PM thickness maintaining the same DVT (considering 28mV/nm sensitivity), w/ +3 nm SD thickness to match the same VT
Si-SAG
In-SAG
To get the same POR VT with In-SAG, we need to increase tSD by ~ 3 nm, but 7 nm reduction on PM
Actual 30S
30S w/ In-SAG
Recommendation:
SxP trial on FS with In-SAG centered on SDK1 pro 30S planned on March

## Slide 15: Back-up

## Slide 16: In-SAG opportunity for 30S
SDK#6 (In-SAG) upsides wrt SDv12+In:
  Sigma: more than 10mV sigma gain
  Memory effect: more than 100 mV larger
  Drift: equivalent up to VDM2, to be better segmented the VDM3
  Endurance: reduced E2 turnaround
  Note: all these parameters have been evaluated from SD only silicon probed with:
  The same seasoning as the one of the FS (that could not be optimum for SD-only)
  A 3E Set pulse with lower maximum current (~26 uA)
  PG4 tsense
  Process with Liner-protected SD
  About points 1, 2 segmentation in progress (MattiaB.)

## Slide 17
Actual pre-POR for SSM
In
As