## Slide 1: PM scaling for 3DXP: Y-GST status and plan
Y-GST: fundamentals, preliminary data and plan
30S Material Pathfinding

## Slide 2: PM scaling: Y-GST development
Y-GST Fundamentals:
  Yttrium doped GST  Proposal based on Atomistic Simulations – thru the collaboration with Prof. Bernasconi
  Features/Expectations of Y-GST system from simulations:
      Yttrium as effective dopant to increase EG thanks to stronger Y-Te bonds and with higher charge transfer wrt Sb-Te bonds  Enhanced DVT if EG is VT proxi
      Ability of Y to keep high the fraction of 4-membered rings acting as crystalline precursors in the a-phase  Enhanced SET-speed performances
      Stronger bonds Y-Te bonds wrt Sb-Te bonds leading to stronger thermal stability  Enhanced WD immunity
High Set speed
GIST
4-fold Rings Statistics
Enhanced Charge Transfer of Y-Te wrt Sb-Te

## Slide 3: Y-GST: L0 and L1 data
  L0 Data: Key Results
    EG trend: EG increase w/ Te- and Sb-rich and low Y % (~4%)
    Higher EG in the expected EoL composition region
    Higher crystallization temperature signature of stronger bonds
  L1 Data: Key Results
    Higher DVT as a consequence of higher EG
    Good SET-speed at CLV screening level
    Crystallization speed char thru optical measurements on going
>50mV EG contrast in EoL alloys
EG trend
Y: 2-10%
Ge
Te
S2R CLV
VT trend in line w/ EG
PM2A3 EoL
PM2A3 as dep
Y-GST EoL to be targeted
PM2A3 as dep
Y-GST targeted: stable pgr curves
EoL EG contrast
Cycled (1kc)
EG: Y-GST vs GIST
Tx increase w/ YSb
~447GST + 4%Y to intercept the highest EG @ EoL composition

## Slide 4: Y-GST: L1D status
POR 70s PM + BGM3 ArO2 SP (Cond-A)
1 step 100s, 1000Vb PM
2 step PM: 40s POR + 30s 1000Vb
1 step 100s POR PM
SD punch thru
Start with sloped PM, incomplete WL2 etch
No profile change w/ longer PM time except slight CD shrink
Slight bot PM profile improvement with 2 step PM w/ high bias 2nd PM etch
Y precipitation seems to be the cause since no known volatile, etchable compounds
  Need sputter etch
High bias (1000Vb) with longer time improved profile but SD punch thru
  Need high bias process  Tool max 1150Vb, new HW may require
  Follow up test with 1100~1150Vb and reduced time 70~80s

## Slide 5: PM scaling: Sc-GST as further opportunity
Scandium (Sc) is tight relative to Yttrium
A recent Science paper [F. Rao et al., Science 358, 1423 (2017)] shared at 30S Mat. Pathf. wk#10 showed the ability of ~4% Sc doped Sb2Te3 to improve the SET speed down to ns [link]
Authors applied a very similar methodology to the one we used for Y-GST to select Sc
Authors found:
  Strong Sc-Te bonds giving robust 4-fold rings crystalline precursors
  Among the class of TM Sc and Y are found to show chemical bonds of high strength with Te and good geometric conformability criterion (better for Sc than Y)
Follow-up:
  Prof. Bernasconi is simulating also Sc-GST (wk 12)
  Dale is asking for Sc-based target quotations
TM