## Slide 1: Enhanced segregation
Update 3/14/2018
Enrico, Hongmei

## Slide 2
Further evidences of enhanced segregation both for Sb-rich and Te-rich directions
Some indication of high resistance for very Te-rich alloys (further L0 analysis on-going)

## Slide 3
D0
enhanced Sb segregation corresponds to residual amorphous region
enhanced Te segregation corresponds to crystalline region
D1
RD
All bits fail

## Slide 4
D0 1092
D1 1092
D0 1078
D1 1078
Ge-rich
Ge-rich
Top: Ge-rich
=> colder
10M
10M
Usual segregation
Enhanced segregation
also
high OPEN
SET on SET cycling

## Slide 5
RD & SET on SET
Te-rich alloy (as Sb-rich) has lower melting (liquidus) point => progressive thermodynamic enhanced segregation,
since liquid (or hot fragile alloy) tends to enrich towards eutectic compositions (yellow arrows)
Pfa RD 2017;
Pfa-1344
100R
100SET
D1

## Slide 6
SET-on-SET bits show Vt shift, however, we don’t see residual amorphous layer formed in those SET-on-SET bits.
Those high Vt SET-on-SET bits doesn’t show high segregation index, which show good correlation with Vt.
Both Read-on-read and SET-on-SET bits show extremely higher (>70%) Te accumulation at on side of interface.
Those Te rich range form different crystalline than the main range of PM.
Does this Te rich crystalline layer has high resistance, thus cause Vt shift even it is crystalline?
Deck-1
Davide M./Hefei/Rohini
Te rich area
100R: amorph very Sb-rich + very Te-rich
100SET: very Te-rich

## Slide 7
GST phase diagrams
Very Te-rich alloy is toward Ge15Te85 :
Low melting point (<400C) (eutectic)
Reported as OTS-like (i.e. APPLIED PHYSICS LETTERS 100, 143505 (2012))

## Slide 8: Crystal refinement principle
Growth/
solidification
=> Sb-rich
x(norm)
k=L/S (slope ratio)
Multicomponent system even with small Th. gradient and no field/current component:
  depletion of one component during solidification
  => enrichment in liquid => enrichment in the last solidified
Enhanced segregation
theory

## Slide 9
alloy | S (300C) (Ohm-1 cm-1) | Rho (300C) (mOhm cm)
Te | 200 | 5
Ge10Te90 | 10 | 100
Te electrical resistivity vs carrier concentration
“Doped”-Te can have high resistivity
Element | Resistivity(Ωm) | Electrical Type
Te | 0.0001 | Semiconductor
Ge | 0.0005 | Semiconductor
Sb | 4X10-7 | Conductor
As | 3X10-7 | Conductor
Se | 1.2X10-7 | Semiconductor
Te-rich alloys conductivity

## Slide 10
+Te
Damaged film
melting
pseudobinary
+Ge
- Sb
pseudobinary
+Te
Damaged film
?
?
ρ= 10 or 100 mOhm cm?
Te-rich alloys:
Agrate Old data

## Slide 11
“Normal” Te-rich segregated alloy results with good conductivity
Very Te-rich segregation (with the associated low T precipitation)
could introduce high resistance even crystalline
<400C ?
GISTN
“normal”
Te-rich
precipitation
Very Te-rich alloy now deposited and under characterization
Sb-rich
bulk
Te-rich
DSC

## Slide 12
On going mapping of L0 on GISTN diagram (Tx, Tm, Eg, speed)
GST only
GISTN

## Slide 13
T crystal (Rs-T)
GST only
T (C )
Literature example: crystallization time is high around GST 111
Need for mapping of L0 crystallization speed (optical)

## Slide 14: PM Segregation
Higher segregation index for intermediate programming, the worst for Iprog ~ Imelt
Recovery by IRST
consistent with thermodynamic enhanced segregation mechanism
Correlation with Vth TE
Lu/Hefei
PFA-22
Vim

## Slide 15
Enhanced segregation (driven by thermodynamic driving force under thermal gradient) is active to increase Sb-enrichment and Te-enrichment, with corresponding consequence on amorphous residual (Sd-rich) and/or possible high resistance crystalline (Te-rich).
Higher the segregation, higher the impact on related failing mechanism (Vth TE, RD, WD, ..)
On cycling the modification of cell response (either by PM material or by cell thermal environment changes) can more easily enable a partial transformation and consequently the corresponding enhanced segregation, especially on not median bits, which accelerates the endurance degradation.
Mapping the impact on modifying the phase diagram (liquidus surface, physical properties) with different PM alloys (i.e. doping) can provide some visibility to mitigate segregation-based issues.
Enhanced segregation is here discussed and supported for PM but similar mechanism could occur also for SD, since is based on the presence of solid/liquid front under certain programming condition. However, contrary to PM, physical SD segregation evidence is still not assessed (but neither is well stabilized how a supposed segregation is affecting threshold switching), but electrical behavior of SD only is historically playing similarly to PM: RE Vth shift increase is enhanced at higher read current, recovered by RST.

## Slide 16
Enhanced segregation easily occurs when programming condition applies a not uniform thermal stress along the cell thickness such that a region is in a high temperature and diffusivity regime (i.e. liquid), while the adjacent region is at lower temperature and low diffusivity, relative to their local properties, in order to have a phase boundary.
Such a situation is draining from the boundary the elemental component which makes the composition more thermodynamically stable. The situation is similar to solidification refinement, when the solidification front depletes or enriches in certain components in order to minimize the energy of the system.
From the GST diagram, during solidification of an alloy with a typical composition for SXP, the last liquid to solidify tends to enrich in Sb (or Te), since the most stable form of liquid is rich in Sb (or Te) (there are eutectic points in the Sb-rich direction and in Te-rich direction)).
Such a thermodynamic driving force (temperature gradient driven) is combining with the other segregation driving forces to produce the final segregation and is considered important whenever an “intermediate” condition is produced.
Enhanced segregation mechanism

## Slide 17
element segregation on programming
Concentration
gradient
Thermal
gradient
Mechanical
stress
Mass transport can be modeled by the equilibrium of different driving forces:
Electric Field/
current
The thermal gradient component includes also thermodynamic segregation, when equilibrium solubility of one component, in a multicomponent alloy, can depend on temperature or (even more) on the phase (solid/liquid).
overview segregation on programming

## Slide 18
Additional flux across solid/liquid interface
GST Phase Segregation
Contribution from thermal gradient
During solidification on cooling, chemical potential drives the composition which solidify first;
residual liquid tends to the lowest eutectic point
For GST this is rich in Sb and poor in Ge: Sb accumulates in the liquid phase, Ge in the solid one.
Thermodynamic component
Simple implementation:
Novielli et al. IEDM 2013
TCAD extended description
on-going