## Slide 1: SD Characterization Update
Dan Gealy, Enrico Varesi
Update - March 28, 2018

## Slide 2: Summary – TEM PFA Work SD1
PFA 1357– SR71b SD1 split, completed
    WL Cut (Y-Dir) – Grounded (new)
    BL Cut (X-Dir) – replicate
  PFA 1357/TL180206001 ungrounded BL cut remain consistent
  Grounded WL-cuts still provides the best data
  BL cut (X-dir)
    Ungrounded
      Se/As segregation observed – top is As rich, bottom is Se rich
    Se/As segregation trending
      “odd bits”> virgin bits >”odd bits” – top is Se rich, bottom is As rich
      Thickness changes not prominent
  Prog assignment to be confirmed
S3 grounded WL
S1, S2 ungrounded BL

## Slide 3: Summary – TEM PFA Work SD1 (2)
PFA1357 S1 ug-BL
TL172122001 SR71b with bit placement - SD1 split
  WL cut (WL14). No grounding
  Strong Se/As segregation trending
    Even/odd bit placement is opposite
    SI: “even bits” > virgin bits > “odd bits” observed – top is Se rich, bottom is As rich. SI > 1
    Thickness changes not prominent
PFA 1357– SR71b SD1 split
  BL cut (X-dir)
    Ungrounded
      Se/As segregation observed – top is As rich, bottom is Se rich
    Se/As segregation trending
      “odd bits”> virgin bits >”odd bits” – top is Se rich, bottom is As rich
      Thickness changes not prominent
  PFA 1357/TL180206001 ungrounded BL cut are consistent
  Prog assignment to be confirmed
TL172122001

## Slide 4
Fired/Virgin Bits – SR71b PFA 1357 s3
SD1 split4E w16
  WL (Y) Cut. – Grounded
  Polarity driven segregation observed
  Little segregation in unfired bits but there is still a small offset which is additive to the polarity driven segregation
Grounded WL cut shows a smaller preparation segregation bias
Even Bits (Pos prog?)
Virgin
Odd Bits (Neg prog?)
Hefei

## Slide 5
PFA 1357 on SD1 – SI Box plots/linescans
Polarity driven segregation observed
S2 corroboration
Thickness artifacts
Chart: Ycut (grounded) s3 bit 17 cycled
Ge% | 24.8548 | 25.3799 | 25.5103 | 25.6058 | 25.8415 | 25.0495 | 24.5702 | 24.1296 | 23.63 | 24.1977 | 24.3834 | 24.5587 | 24.5235 | 24.7399 | 25.4687 | 26.1985 | 27.0421 | 27.3126 | 27.081 | 26.8534 | 27.0055 | 26.9133 | 27.0231 | 27.1363 | 26.9291 | 27.3563 | 27.7456 | 28.1173 | 28.1875 | 27.6699 | 26.9948 | 26.3225 | 25.9472 | 25.4568 | 25.0856 | 24.6836 | 24.0292 | 23.8393 | 23.5434 | 23.0121 | 22.9677 | 23.1834
As% | 37.7457 | 37.3547 | 37.2471 | 37.1699 | 36.9239 | 36.7382 | 36.4964 | 36.2723 | 36.1283 | 35.1242 | 34.1659 | 33.2656 | 32.5347 | 31.5175 | 30.0489 | 28.579 | 26.89 | 26.0798 | 25.8748 | 25.673 | 25.5206 | 25.6549 | 25.6489 | 25.6407 | 25.7039 | 24.9612 | 24.3122 | 23.6923 | 23.1666 | 23.6734 | 24.4825 | 25.2881 | 26.2995 | 27.528 | 28.3171 | 29.1722 | 30.0814 | 30.1801 | 30.6435 | 31.4792 | 31.4338 | 31.0725
Se% | 37.3996 | 37.2654 | 37.2425 | 37.2243 | 37.2346 | 38.2123 | 38.9334 | 39.5981 | 40.2416 | 40.6782 | 41.4506 | 42.1757 | 42.9418 | 43.7426 | 44.4825 | 45.2225 | 46.0679 | 46.6076 | 47.0443 | 47.4735 | 47.4739 | 47.4317 | 47.3279 | 47.2229 | 47.367 | 47.6825 | 47.9422 | 48.1904 | 48.6459 | 48.6567 | 48.5227 | 48.3893 | 47.7533 | 47.0151 | 46.5974 | 46.1442 | 45.8894 | 45.9806 | 45.8131 | 45.5087 | 45.5986 | 45.7441
Chart: Ycut (grounded) s3 bit 16 Cycled (opposite polarity)
Ge% | 23.0891 | 22.5697 | 22.3797 | 22.2 | 21.9958 | 23.0657 | 23.8513 | 24.6142 | 25.4037 | 25.6917 | 25.876 | 26.0532 | 26.4648 | 26.0796 | 25.9064 | 25.7369 | 25.3766 | 25.4031 | 25.5586 | 25.6889 | 25.8183 | 25.7348 | 25.4612 | 25.1884 | 24.9069 | 24.38 | 24.0749 | 23.7689 | 23.6641 | 24.3361 | 24.6701 | 25.0033 | 25.1453 | 25.3582 | 25.7878 | 26.358 | 26.8322 | 26.9244 | 27.3209 | 28.2453 | 32.7533
As% | 26.7578 | 26.3993 | 26.0377 | 25.6965 | 25.2542 | 24.4257 | 23.6929 | 22.9815 | 22.6073 | 22.7265 | 22.9419 | 23.1499 | 23.1265 | 23.5189 | 23.8705 | 24.2151 | 24.7737 | 25.9738 | 27.0945 | 28.1112 | 28.9467 | 30.0046 | 31.2596 | 32.5059 | 33.7171 | 34.4396 | 35.1671 | 35.8984 | 36.4459 | 37.114 | 37.6979 | 38.2794 | 39.165 | 38.7173 | 38.364 | 37.8942 | 37.647 | 37.9537 | 37.662 | 36.9846 | 30.0425
Se% | 50.1531 | 51.031 | 51.5826 | 52.1035 | 52.7499 | 52.5087 | 52.4558 | 52.4043 | 51.989 | 51.5818 | 51.1821 | 50.7968 | 50.4087 | 50.4015 | 50.2231 | 50.048 | 49.8497 | 48.6231 | 47.3469 | 46.2 | 45.235 | 44.2607 | 43.2792 | 42.3057 | 41.376 | 41.1804 | 40.758 | 40.3328 | 39.8899 | 38.5499 | 37.632 | 36.7173 | 35.6897 | 35.9245 | 35.8482 | 35.7478 | 35.5208 | 35.122 | 35.0171 | 34.77 | 37.2042
pfa-1357, ungrounded BL cut, S1, S2
pfa-1357, grounded WL cut, S3

## Slide 6
PFA 1357 on SD1 – SD Thickness
Fired bits are marginally thinner
pfa-1357, grounded WL cut, S3
pfa-1357, ungrounded BL cut, S1, S2

## Slide 7: Summary – TEM PFA Work SD1
TL180206001 – S26 virgin die - SD1 split
  WL cut (Y-dir)
    Grounded WL/BL
      Little segregation observed. SI ≈ 1
    Ungrounded
      Se/As segregation observed – top is Se rich, bottom is As rich. SI > 1
  BL cut (X-dir)
    Ungrounded
      Se/As segregation observed – top is As rich, bottom is Se rich. SI < 1
TL180108002 – S26 probed die - SD1 split
  WL cut (Y-dir) - Grounded WL/BL. “Positive” programming
  Se/As segregation observed – top is Se rich, bottom is As rich. SI > 1
S26a
Virgin bits
S26a
Positive programed /Virgin bits

## Slide 8
Job | device | Lot/wf | status | GND | Cut_dir | type | Se rich | Se/As (top/bottom)
Pfa-1357 | SR71 | 0024732/wf16 | Done | No | X | Prog2 (neg ?) | Bottom | 0.75
 |  |  |  |  |  | Virgin | Bottom | 0.95
 |  |  |  |  |  | Prog1 (pos ?) | no | 1.06
 | SR71 | 0024732/wf16 |  | Yes | Y | Neg |  | 0.74
 |  |  |  |  |  | Virgin |  | 1.12
 |  |  |  |  |  | Pos |  | 1.59
TL171222001 | SR71 | 0024732/wf16 | Done | No | Y | Neg (odd) | Top | 1.11
 |  |  |  |  |  | Virgin | Top | 1.31
 |  |  |  |  |  | Pos (even) | Top | 1.75
TL180108002 | S26 | 0024732/wf2 | Done | Yes | Y | Pos | Top | 1.62
TL180206001 | S26 | 0024732/wf2 | Done | Yes | Y | Virgin | no | 1.02
 | S26 | 0024732/wf2 | Done | No | X | Virgin | bottom | 0.86
 | S26 | 0024732/wf2 | Done | No | Y | Virgin | Top | 1.2
Pfa-1385 | S26 | 0024732/wf2 |  | Yes | Y | Pos |  | 
PFA on SD1 (only) – Summary Table

## Slide 10
Virgin Bits – S26A TL180206001
SD1 split4E, w02 Ungrounded WL/BL cuts
  Grounded WL cut shows least segregation
  Ungrounded show segregation
  Opposite segregation between WL & BL cuts
Virgin array -ungrounded BL cut
Virgin array - ungrounded WL cut
Virgin array -grounded WL cut
Hongqi

## Slide 11
W BLs were not grounded.
W BLs were grounded.
WL-BL grounding
SR71 WL cut
(Y-dir)
S26 WL cut
(Y-dir)

## Slide 12
Pos prog TL180108002
Fired/Virgin Bits – S26A TL180108002, TL180206001
Grounded WL Cuts
Hongqi
Virgin Array TL180206001
SD1 split4E, Grounded WL cuts
  w02 S26A
    Programed
    Virgin array
  Segregation on programming observed
    Se rich top, As rich bottom
  Little preparation bias

## Slide 13
Odd (Neg prog?)
Fired/Virgin Bits – SR71b TL1712222001
Even (Pos prog?)
Virgin
SD1 split4E w16
  WL Cut. No grounding
    WL 14/multiple BL’s
    Se/As segregation trending
      SI “even bits”> virgin bits >”odd bits” – top is Se rich, bottom is As rich
Hongqi
Ungrounded WL cut overlays a preparation segregation bias that adds to D0 positive programming but subtracts from D0 negative programming
TL172122001

## Slide 14
Virgin Bit Comparison – SR71b/S26a
Virgin Bits – SR71b ungrounded BL cut PFA 1357
SD1 split4E w16
  BL Cut. No grounding
  SI < 1
Virgin Bits S26a -ungrounded BL cut

## Slide 15
Pos prog
S26a
Fired Bits – SR71b TL1712222001, S26a TL180108002
SD1 split4E
  w16 SR71b
    WL Cut. No grounding
    WL 14/multiple BL’s
  w02 S26a
    WL cut. Grounded
  Data is consistent if we assume pos. programing on even bits
    Logical interpretation is that even lines are probed negatively
Even (Pos prog?) SR71b
Hongqi

## Slide 16
Odd (Neg prog?)
Fired/Unfired Bits – PFA 1357
Even (Pos prog?)
Virgin
SD1 split4E w16 - S1, S2
  BL Cut. No grounding
Hefei

## Slide 17: PFA 1357 / TL122122001 Comparison
TL172122001
  WL Cut. WL14 (1st active) - verifiied
PFA1357
  BL Cut. BL 9
Trends are opposite between PFA 1357 & TL122122001
Actual placement needs to be better understood
Assuming even bits are positively programed (not intended) WL cuts on SR71b & S26a not grounded v. grounded are consistent
TL172122001
PFA1357

## Slide 18
EDS Element Line Scan TL1712222001 Oppositely Fired Bits
33
35
34
36
37
38
33
35
34
36
37
38
Linescans not normalized

## Slide 19
EDS Element Line Scan TL1712222001 Not Fired Bits
33
35
34
36
37
38
33
35
34
36
37
38
Linescans not normalized

## Slide 20
EDS Element Line Scan TL80108002
Grounded WL/BL
Consistent with SR71B
As/Se motion
Linescans not normalized

## Slide 21: Stem Images: 0024732.003, split 4E SD1 SAG, wafer16 SR71B
Folsom
X-cut SR71 ungrounded
Significant Se enrichment at bottom for one of the two programmed cell
Opposite smooth segregation for opposite prog, compared to virgin
Prog assignment to be confirmed
Prog sequence:
pos,/neg prog seasoning
chkb positive prog (4 pulses)
line pattern:
adjacent pos and neg prog between 6 not programmable cells
Enrico

## Slide 22: Stem Images: 0024732.003, split 4E SD1 SAG, wafer16 SR71B
23
31
PFA1357
8-1
15-8
8
15
22-15
22

## Slide 23
PFA-396 (SD1)
SD1:
Stronger As/Se segregation
for SET vs RESET (time dominating)
1us
50ns
1us
50ns
50 ns | 1000 ns | 50 ns | 1000 ns
50 uA |  | 150 uA | 
1k cycles
Hefei, Enrico
  Elemental segregation with SD1
    Consistent with current direction (as with PM)
      Opposite electromigration behavior on D0 & D1
Previous SD1 Elemental Migration Work
Back

## Slide 24
D1
D0
D0, X-cut=Se bottom
D1, X-cut=Se bottom
D1, Y-cut=Se top
D1, Y-cut=Se top
X-cut=Se bottom
Y-cut=Se top
PreviousTypical
Ungrounded result

## Slide 25
device | TEM lab | cut | line | Grounding WL-BL | prog | Se/As top/bottom | Se-rich
SR71 | Folsom | X | BL 9 | no | Pos | 1.06 | 
 |  |  |  |  | Neg | 0.75 | 
 |  |  |  |  | virgin | 0.95 | bottom
SR71 | Boise | Y | WL 14 | no | Pos | 1.10 | 
 |  |  |  |  | Neg | 1.77 | 
 |  |  |  |  | virgin | 1.33 | top
S26 | Boise | Y |  | yes | Pos | 1.63 | 
Typically ungrounded:
X-cut=Se-rich at bottom
Y-cut=Se-rich at top
SR71 (ungrounded):
  Overall (virgin) main segregation modulated by cut direction (as usual)
  Opposite segregation for opposite programming compared to virgin
  Programming assignment to be confirmed
S26 (grounded pos prog): Se enrichment at top
SD1 PFA summary

## Slide 26: Linescan: 0024732.003, split 4E SD1 SAG, wafer16 SR71B
Bit 11 virgin
Bit 12 virgin
Bit 16
Bit 24
Bit 12 virgin
Bit 32
Bit 40
Bit 48

## Slide 27: Filtered normalized composition profiles
Virgin #11
Virgin #12
#16
#24
#32
#40
#48

## Slide 28
labeled in TL17222001 | As drawn BL
3 | 57
4 | 56
11 | 49
12 | 48
19 | 41
20 | 40
27 | 33
28 | 32
35 | 17
36 | 16
43 | 9
44 | 8
51 | 1
52 | 0
9
17
1
0